SECTION 09954- PAINTING - LEAD-BASED PAINT

PART 1 - GENERAL

1.1	RELATED DOCUMENTS

A.  Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2	SUMMARY OF WORK

A.  This Section includes surface preparation, and painting,

exposed interior and exterior items and surfaces.

1.  Surface preparation, priming, and finish coats

specified in this Section are in addition to surface treatments specified under other Sections.

B.  Paint exposed surfaces whether or not colors are designated in schedules, except where a surface or material is specifically indicated not to be painted or is to remain natural.  Where an item or surface is not specifically mentioned, paint the same as similar adjacent materials or surfaces.  If color or finish is not designated, the Architect will select from standard colors or finishes available.

1.  Painting includes field-painting lead-based painted surfaces, substrates from which lead-based paint has been removed, and building surfaces which were included in a hazard reduction work area.

C.  Painting is not required on pre-finished items, finished metal surfaces, concealed surfaces, operating parts, and labels.

D.  Related Sections:	The following Sections contain

requirements that relate to this Section.

1.  02065 - Removal

2.  05582 - Sheet Metal

3.  06106 - Wood Enclosures

4.  06107 - Exterior Siding & Enclosure

5.  06402 - Carpentry and Trim Work

6.  06403 - Repair of Lead-Based Painted Substrates

7.  09252 - Gypsum Wallboard Enclosure

8.  09940 - Encapsulation - Lead-Based Paint

9.  09951 - Chemical Stripping Of - Lead-Based Paint

10. 09952 - Mechanical Removal Of Lead-Based Paint

11. 09953 - Surface Preparation - Paint Stabilization Lead-Based Paint

1.3	SUBMITTALS

A.  General:  Submit the following according to Conditions of the Contract and Division 1 Specification Sections.

B.  Product data for each paint system specified, including

block fillers and primers.

1.  Provide the manufacturer's technical information including instructions for handling, storage, and application of each material proposed for use.

2.  List each material and cross-reference the specific coating, finish system, and application.  Identify each material by the manufacturer's catalog number and general classification.

3.  Submit information by the manufacturer that products supplied comply with local regulations controlling use of volatile organic compounds (VOCs).

C.  Samples for initial color selection in the form of

manufacturer's color charts.

1.  After color selection, the Architect will furnish

color chips for surfaces to be coated.

1.4	QUALITY ASSURANCE

A.  Field Samples:  On wall surfaces and other exterior and interior components, duplicate finishes of prepared samples.  Provide full-coat finish samples on at least 100 sq. ft. of surface until required sheen, color, and texture are obtained; simulate finished lighting conditions for review of in-place work.

1.  The Architect will select one room or surface to represent surfaces and conditions for each type of coating and substrate to be painted.  Apply coatings in this room or surface according to the schedule or as specified.

a.  After finishes are accepted, this room or surface will be used to evaluate coating systems of a similar nature.

1.5	DELIVERY, STORAGE, AND HANDLING

A.  Deliver materials to the job site in the manufacturer's original, unopened packages and containers bearing manufacturer's name and label, and the following information:

1.  Product name or title of material.

2.  Product description (generic classification or binder type).

3.  Manufacturer's stock number and date of manufacture.

4.  Contents by volume, for pigment and vehicle

constituents.

5.  Thinning instructions.

6.  Application instructions.

7.  Color name and number.

B.  Store materials not in use in tightly covered containers

in a well-ventilated area at a minimum ambient temperature of 45 deg F (7 deg C).  Maintain containers used in storage in a clean condition, free of foreign materials and residue.

1.  Protect from freezing.  Keep storage area neat and orderly.  Remove oily rags and waste daily.  Take necessary measures to ensure that workers and work areas are protected from fire and health hazards resulting from handling, mixing, and application.

1.6	JOB CONDITIONS

A.  Apply water-based paints only when the temperature of surfaces to be painted and surrounding air temperatures are between 50 deg F (10 deg C) and 90 deg F (32 deg C).

B.  Apply solvent-thinned paints only when the temperature of surfaces to be painted and surrounding air temperatures are between 45 deg F (7 deg C) and 95 deg F (35 deg C).

C.  Do not apply paint in snow, rain, fog, or mist; or when

the relative humidity exceeds 85 percent; or at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

1.  Painting may continue during inclement weather if surfaces and areas to be painted are enclosed and heated within temperature limits specified by the manufacturer during application and drying periods.

PART 2 - PRODUCTS

2.1	MANUFACTURERS

A.  Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated in the Work include, but are not limited to, the following:

B.  Manufacturer:  Subject to compliance with requirements,

provide products of one of the following:

1.  Devoe and Raynolds Co. (Devoe). 2.  Fuller O'Brien (Fuller).

3.  The Glidden Company (Glidden). 4.  Benjamin Moore and Co. (Moore).

5.  PPG Industries, Pittsburgh Paints (PPG). 6.  Pratt and Lambert (P & L).

7.  The Sherwin-Williams Company (S-W).

2.2	PAINT MATERIALS, GENERAL

A.  Material Compatibility:  Provide block fillers, primers, finish coat materials, and related materials that are compatible with one another and the substrates indicated under conditions of service and application, as demonstrated by the manufacturer based on testing and field experience.

B.  Material Quality:  Provide the manufacturer's best-quality trade sale paint material of the various coating types specified.  Paint material containers not displaying manufacturer's product identification will not be acceptable.

1.  Proprietary Names:  Use of manufacturer's proprietary product names to designate colors or materials is not intended to imply that products named are required to be used to the exclusion of equivalent products of other manufacturers.  Furnish the manufacturer's material data and certificates of performance for proposed substitutions.

C.  Colors:  Provide custom colors of the finished paint systems to match the Architect's samples.

D.  Colors:  Match colors indicated by reference to the manufacturer's standard color designations.

E.  Colors:  Provide color selections made by the Architect from the manufacturer's full range of standard colors.

2.3	MASONRY BLOCK FILLER

A.  Filler Coat Materials:  Provide the manufacturer's recommended factory-formulated, latex-type concrete masonry block fillers that are compatible with the finish materials indicated.

B.  Available Products:  Subject to compliance with requirements, block fillers that may be incorporated in the Work include, but are not limited to, the following:

C.  Products:  Subject to compliance with requirements,

provide one of the following:

1.  High-Performance Latex Block Filler:

a.  Devoe:  52901 Bloxfil Interior/Exterior Acrylic Latex Block Filler.

b.  Fuller: 280-00 Interior/Exterior Latex Block Filler.

c.  Glidden:	5317 Ultra-Hide Acrylic Latex Block

Filler.

d.  Moore:  Moorcraft Interior & Exterior Block Filler #173.

e.  PPG:	6-7 Latex Masonry Block Filler.

f.  P & L:  Pro-Hide Plus Block Filler.

g.  S-W:		Heavy-Duty Block Filler B42W46.

2.4  PRIMERS

A.  Primers:  Provide the manufacturer's recommended factory-formulated primers that are compatible with the substrate and finish coats indicated.

B.  Available Products:  Subject to compliance with requirements, prime coat materials that may be incorporated in the Work include, but are not limited to, the following:

C.  Products:  Subject to compliance with requirements,

provide one of the following:

1.  Exterior Primer Coating:  Exterior, alkyd wood primer.

a.  Devoe:	1102 All-Weather Alkyd House Paint

Primer.

b.  Fuller:	220-23 Exterior Wood and Masonry

Primer.

c.  Glidden:		1951 Spread Gel-Flo Base Coat.

d.  Moore:	Moorwhite Primer #100.

e.  PPG:	1-70 or 1-870 Sun Proof Exterior Wood

Primer

f.  P & L:	Permalize Exterior Primer.

g.  S-W:		A-100 Exterior ALKYD wood primer

Y24W20.

2.  Concrete and Masonry Primers:  Interior, flat, latex-based paint.

a.  Devoe:	51701 Wonder-Prime Interior All

Purpose Latex Primer Sealer & Vapor Barrier.

b.  Fuller:	202-XX Interior - Exterior Acrylic

Latex Wall Paint.

c.  Glidden:		5300 Ultra-Hide Flat Wall Paint.

d.  Moore:	Moore's Latex Quick-Dry Prime Seal

#201.

e.  PPG:	80 Line Wallhide Flat Latex Paint.

f.  P & L:	Vapex Latex Flat Wall Finish.

g.  S-W:		ProMar 200 Latex Flat B30W200.

3.  New Plaster Primers:  Interior, flat, latex-based paint.

a.  Devoe:	51701 Wonder-Prime Interior All

Purpose Latex Primer Sealer & Vapor Barrier.

b.  Fuller:	Interior Latex Enamel Undercoater.

c.  Glidden:		5019 PVA Primer Sealer.

d.  Moore:	Moore's Latex Quick-Dry Prime Seal

#201.

e.  PPG:	80 Line Wallhide Flat Latex Paint.

f.  P & L:	Vapex Latex Flat Wall Finish.

g.  S-W:		Wall and Wood Primer B49W2.

4.  Gypsum Drywall Primer:  White, interior, latex-based primer.

a.  Devoe:	50801 Wonder-Tones Latex Primer and

Sealer.

b.  Fuller:	Pro-Tech Interior Latex Wall Primer

and Sealer.

c.  Glidden:		5019 PVA Primer.

d.  Moore:	Moore's Latex Quick-Dry Prime Seal

#201.

e.  PPG:	6-2 Quick-Dry Latex Primer Sealer.

f.  P & L:	Latex Wall Primer Z30001.

g.  S-W:		ProMar 200 Latex Wall Primer

B28W200.

5.  Exterior Primer Coating:  Exterior, alkyd wood primer.

a.  Devoe:	1102 All-Weather Alkyd House Paint

Primer.

b.  Fuller:	220-23 Exterior Wood and Masonry

Primer.

c.  Glidden:		1951 Spread Gel-Flo Base Coat.

d.  Moore:	Moorwhite Primer #100.

e.  PPG:	1-70 or 1-870 Sun-Proof Exterior Wood

Primer.

f.  P & L:	Permalize Exterior Primer.

g.  S-W:		A-100 Exterior Alkyd Wood Primer

Y24W20.

6.  Exterior Primer Coating:  Exterior, alkyd wood

primer.

a.  Devoe:	1102 All-Weather Alkyd House Paint

Primer.

b.  Fuller:	220-08 Exterior Latex Wood Primer.

c.  Glidden:		3651 Spread House Paint Prime

Coat.

+a  Moore:	Moorwhite Primer #100.

e.  PPG:	1-70 or 1-870 Sun-Proof Exterior Wood

Primer.

f.  P & L:	Permalize Exterior Primer.

g.  S-W:		A-100 Exterior Alkyd Wood Primer

Y24W20.

7.  Ferrous Metal Primers:  Synthetic, quick-drying, rust-inhibiting primers.

a.  Devoe:	13101 Mirrolac Cover Up Rust

Penetrating Primer.

b.  Fuller:	621-04 Blox-Rust Alkyd Metal Primer.

c.  Glidden:		5210 Glid-Guard Universal Fast-Dry

Metal Primer.

d.  Moore:	IronClad Retardo Rust-Inhibitive Paint

#163.

e.  PPG:	6-208 Red Inhibitive Metal Primer.

f.  P & L:	Effecto Rust-Inhibiting Primer.

g.  S-W:		Kem Kromik Metal Primer

B50N2/B50W1.

8.  Ferrous Metal Primers:  Alkyd-type primers.

a.  Devoe:	41820 Bar-Ox Alkyd Shop/Field Primer

Grey.

b.  Fuller:	621-05 Blox-Rust Latex Metal Primer.

c.  Glidden:		5205 Glid-Guard Tank and

Structural Primer.

d.  Moore:	IronClad Retardo Rust-Inhibitive Paint

#163.

e.  PPG:	6-612 Speedhide Inhibitive White

Primer.

f.  P & L:	Effecto Primer Red or White.

g.  S-W:		Kem Kromik Metal Primer

B50N2/B50W1.

9.  Galvanized Metal Primers:

a.  Devoe:	13201 Mirrolac Galvanized Metal

Primer.

b.  Fuller:	621-05 Blox-Rust Latex Metal Primer.

c.  Glidden:		5229 Glid-Guard All-Purpose Metal

Primer.

d.  Moore:	IronClad Galvanized Metal Latex Primer

#155.

e.  PPG:	6-215/216 Speedhide Galvanized Steel

Primer.

f.  P & L:	P & L Interior Trim Primer.

g.  S-W:		Galvite B50W3.

10. Aluminum Primers:

a.  Devoe:	41820 Bar-Ox Alkyd Shop/Field Primer

Grey.

b.  Fuller:	621-05 Blox-Rust Latex Metal Primer.

c.  Glidden:		5229 Glid-Guard All-Purpose Metal

Primer.

d.  Moore:	Iron Clad Retard Rust Inhibitive Paint

#163.

e.  PPG:	6-712 Speedhide Inhibitive Metal

Primer, White.

f.  P & L:	Effecto Primer Red or White.

g.  S-W:		KEM Kromik Metal Primer

B50N2/B50W1

PART 3 - EXECUTION

3.1	EXAMINATION

A.  Examine substrates and conditions under which painting

will be performed for compliance with paint application requirements.  Surfaces receiving paint must be thoroughly dry before paint is applied.

1.  Do not begin to apply paint until unsatisfactory

conditions have been corrected.

2.  Start of painting will be construed as the Applicator's acceptance of surfaces and conditions within a particular area.

|aò	PREPARATION

A.  General:  Remove hardware and hardware accessories,

plates, machined surfaces, lighting fixtures, and similar items already installed that are not to be painted, or provide surface-applied protection prior to surface preparation and painting.  Remove these items, if necessary, to completely paint the items and adjacent surfaces.  Following completion of painting operations in each space or area, have items reinstalled by workers skilled in the trades involved.

B.  Cleaning:  Before applying paint or other surface treatments, clean the substrates of substances that could impair the bond of the various coatings.  Remove oil and grease prior to cleaning.  Schedule cleaning and painting so dust and other contaminants from the cleaning process will not fall on wet, newly painted surfaces.

C.  Surface Preparation:  Clean and prepare surfaces to be painted according to the manufacturer's instructions for each particular substrate condition and as specified in section 09953.

1.  Provide barrier coats over incompatible primers or remove and re-prime.  Notify Architect in writing about anticipated problems using the specified finish-coat material with substrates primed by others. a.  Determine alkalinity and moisture content of

surfaces by performing appropriate tests.  If

surfaces are sufficiently alkaline to cause the finish paint to blister and burn, correct this condition before application.  Do not paint surfaces where moisture content exceeds that permitted in manufacturer's printed directions.

3.3	APPLICATION

A.  General:  Apply paint according to manufacturer's directions.  Use applicators and techniques best suited for substrate and type of material being applied.

B.  Do not paint over dirt, rust, scale, grease, moisture, scuffed surfaces, or conditions detrimental to formation of a durable paint film.

C.  Application Procedures:  Apply paints and coatings by brush, roller, spray, or other applicators according to the manufacturer's directions.

1.  Brushes:  Use brushes best suited for the material applied.

2.  Rollers:  Use rollers of carpet, velvet back, or high-pile sheep's wool as recommended by the manufacturer for the material and texture required.

3.  Spray Equipment:  Use airless spray equipment with orifice size as recommended by the manufacturer for the material and texture required.

D.  Minimum Coating Thickness:  Apply materials no thinner than the manufacturer's recommended spreading rate. Provide the total dry film thickness of the entire system as recommended by the manufacturer.

3.4	CLEANING

A.  Cleanup:  At the end of each work day, remove empty cans, rags, rubbish, and other discarded paint materials from the site.

1.  After completing painting, clean glass and paint-spattered surfaces.  Remove spattered paint by washing and scraping.  Be careful not to scratch or damage adjacent finished surfaces.

3.5	PROTECTION

A.  Protect work of other trades, whether being painted or not, against damage by painting.  Correct damage by cleaning, repairing or replacing, and repainting, as acceptable to Architect.

B.  Provide "Wet Paint" signs to protect newly painted

finishes.  Remove temporary protective wrappings provided by others to protect their work after completing painting operations.

1.  At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

END OF SECTION 09954