## Slide 1: Wood Design Background Kelly Cobeen, S.E.
Disclaimer
Includes materials developed by Peter Somers S.E. and Steve Pryor, S.E.
Notes: Graphic shows cover of the NEHRP Provisions FEMA P-1052.
This slide set provides background on wood design in order to complement the wood design problems in Chapter 14 of the FEMA P-1051 NEHRP Recommended Design Provisions: Design Examples

## Slide 2: Wood Design Background Outline
Basic wood properties
Introduction to wood design and construction
Shear Walls
Diaphragms
Anchorage of concrete and masonry walls
Notes: This presentation will cover the following five topics

## Slide 3: Basic Wood Properties
Notes: The graphic shows the section of a wood log with various wood framing member sections to be cut and their respective shrinkage patterns.
We start with our discussion of basic wood properties

## Slide 4: Basic Wood Properties
Unique, independent, mechanical properties in 3 different directions
Varies with moisture content
Main strength axis is longitudinal - parallel to grain
Radial and tangential are "perpendicular" to the grain - substantially weaker
Longitudinal
Radial
Tangential
Wood is orthotropic
Notes: Graphic shows block of wood with radial, tangential and longitudinal directions identified with arrows.
Read slide text

## Slide 5: Basic Wood Properties
Sample Douglas Fir-Larch longitudinal design properties (reference resistance):
Modulus of elasticity: 1,700,000 psi
Tension parallel to grain: 575 psi
Bending: 900 psi
Compression parallel to grain: 1,350 psi
Notes: As noted, the primary strength of wood members is in the longitudinal direction, parallel to grain. These are some representative reference resistances for Douglas Fir-Larch framing members loaded parallel to grain.

## Slide 6: Basic Wood Properties
Sample Douglas Fir-Larch perpendicular to grain design properties (reference resistance):
Tension (perpendicular to grain): no recognized design value
Compression (perpendicular to grain): 625 psi. Note that this is derived from a serviceability limit state of ~ 0.04” permanent deformation under stress in contact situations.
Notes: In contrast these are perpendicular to grain properties.

## Slide 7: Basic Wood Properties
(Wood Handbook, p. 58)
Shrinkage
Wood will shrink with changes in moisture content
This is most pronounced in the radial and tangential directions (perpendicular to grain)
May need to be addressed in detailing
Tangential
Radial
Notes: A graphic is provided on the left labelinA graphic on the right shows the section of a wood log with various wood framing member sections to be cut and their respective shrinkage patterns. This is taken from the WWPA Wood Handbook, and is the same graphic as used on the title slide for this section.
g radial and tangential directions on a block of wood.
We are reminded that in addition to having different strength in the three directions, the shrinkage of wood as it dries from saturated surface dry to equilibrium moisture content is not equal in all three directions, and can be specific enough that it needs to be planned for in detailing.

## Slide 8: Introduction to Wood Design and Construction
Notes: The graphic is a photo of a single-family wood light-frame residence under construction.
Next we will provide an introduction to wood design and construction for those that might be less familiar with typical practice.

## Slide 9: Wood Design and Construction
Walls feature continuous studs from foundation to roof framing
Floors supported by ledgers on walls or lapped with studs
Common in very early wood light-frame construction
Stopped being common early in 1900s
Platform Balloon
Walls are interrupted by floor "platforms"
Floors support walls
Most common type of light-frame construction today
Economical and allows use of commonly available stud lengths
Notes: The graphic on the left shows a diagram of a three-story building with platform construction, in which the studs extend from the top of floor to the underside of floor or roof framing above. The graphic on the right side shows balloon framing where the studs are continuous full height.
There are two major types or categories of wood light-frame construction, platform framing and balloon framing. This slide explains the two types.

## Slide 10: Wood Design and Construction
Roof Purlins
Roof Sheathing
Floor Joists
Floor Sheathing
Notes: The graphic shows a section of a two-story wood light-frame building with roof and floor sheathing and framing labeled.
These are some of the common elements of wood light-frame construction.

## Slide 11: Wood Design and Construction
Vertical elements
Resultant inertial forces
Horizontal elements
Notes: Graphic shows a simple box type building with horizontal diaphragm elements and vertical wall elements labeled.
In wood light-frame construction the two primary elements resisting lateral (wind and seismic) forces are floor and roof systems acting as horizontal diaphragms and carry forces to the shear walls, and walls that carry the lateral loads from the diaphragms to the foundations and supporting soils.

## Slide 12: Wood Design and Construction
ε
Stress in the wood
Tension parallel to the grain: not ductile, low energy dissipation
σ
Notes: Graphic shows a plot of load and deflection, illustrating brittle failure.
Tension, compression and flexure failures of wood members all exhibit brittle failures. In addition, wood properties are variable and design capacities are set such that 95% of members will be stronger, with some portion of the members being significantly stronger. For these reasons, it is not normally desirable or achievable for wood members to be designed as weak links or sources of ductility in wood systems. As a result, ductility and weak links are intended to occur in connections and fasteners.

## Slide 13: Wood Design and Construction
Inertial Force
Resisting Force
Ledger Failure
Tension perpendicular to grain results in brittle failures at low loads
Does not provide a reliable load path
Notes: Graphic shows a tilt-up wall panel connection to a wood diaphragm. The wall anchorage uses bolts in a wood ledger. When the wall pulls one way at the ledger bolt, and the plywood pulls the top of the ledger in the other direction, this causes cross grain tension in the ledger, resulting in failure of the ledger.
Tension perpendicular to grain is known to be particularly brittle and unreliable, having been the cause of failures of anchorage of tilt-up panels in a number of earthquakes.

## Slide 14: Wood Design and Construction
Positive Wall Tie
Notes: This detail shows use of a tie-down type device to make a direct tension connection between diaphragm framing and the wall, thereby avoiding the cross-grain loading of the ledger seen in the previous slide.

## Slide 15: Wood Design and Construction
Sheathing to framing fastening
Nailed joint between sheathing and framing is source of majority of ductility and energy dissipation for nailed wood structural panel shear walls
The energy dissipation is a combination of yielding in the shank of the nail, and crushing in the wood fibers surrounding the nail
Since wood crushing is nonrecoverable, this leads to a partial "pinching" effect in the hysteretic behavior of the joint.
The pinching isn’t 100% because of the strength of the nail shank undergoing reversed ductile bending yielding in the wood.
As the joint cycles, joint resistance climbs above the pinching threshold when the nail "bottoms out" against the end of the previously crushed slot forming in the wood post
Notes: Because wood members cannot provide a source of ductility and energy dissipation for seismic loading, the ductility is commonly provided in the fasteners. For wood structural panel sheathed shear walls and diaphragms, the ductility is provided in the nails fastening sheathing to framing, as described in this slide.

## Slide 16: Wood Design and Construction
Individual nail test
600
500
400
300
200
100
0
-100
-200
-300
-400
-500
-600
-0.6 -0.5 -0.4 -0.3 -0.2 -0.1 0 0.1 0.2 0.3 0.4 0.5 0.6
DEFLECTION (INCHES)
NAIL SHEAR (POUNDS)
Full-scale shear wall test
3
2.5
2
1.5
1
0.5
0
-0.5
-1
-1.5
-2
-2.5
-3
-4
-3
-2 -1 0 1 2
TOP OF WALL DEFLECTION (INCHES)
3
4
APPLIED LOAD AT TOP OF WALL (KIPS)
Notes: Graphics show load-deflection plots with hysteresis curves typical of wood structural panel elements.
These load-deflection plots were generated by reverse-cyclic loading, performed to determine the seismic resisting capacity of bracing elements. The plot on the right hand side shows the hysteretic loops generated by testing a single nailed connection between sheathing and framing. The plot on the left hand side is from a full shear wall. The close resemblance of the two makes the point that the shear wall nailing is the primary source of ductility. Overall, wood structural panel shear walls are categorized as one of the more ductile seismic bracing systems, as indicated by the common R-factor of 6.5. Based on the more limited testing available, wood structural panel diaphragms are thought to be similarly ductile.

## Slide 17: Wood Design and Construction: Prescriptive
Traditionally, many simple wood structures have been designed without "engineering"
Over time, rules of how to build have been developed, most recently in the International Residential Code (IRC)
For the lateral system, the "dedicated" vertical element is referred to as a
braced wall panel, which is part of a braced wall line
Based on SDC and number of stories, rules dictate the permissible spacing between braced wall lines, and the spacing of braced wall panels within braced wall lines
Also referred to as “Conventional Construction”
Notes: Graphic shows photograph of single-family dwelling
Two primary categories of wood light-frame design and construction exist. One is prescriptive construction, or conventional light-frame construction, where construction is defined by prescribed rules and tables, rather than engineering calculations. Some characteristics of prescriptive construction are:

## Slide 18: Wood Design and Construction: Engineered
If a structure does not meet the code requirements for "prescriptive" or "conventional" construction, it must be "engineered"
As in other engineered structures, wood structures are only limited by the application of good design practices applied through principles of mechanics (and story height limitations in the code)
A dedicated system of horizontal and vertical elements, along with complete connectivity, must be designed and detailed.
Notes: Graphic shows a multi-family residential complex that would be designed using engineered methods.
The other primary category is engineered design and construction, based on engineering calculation of demands and capacities. Characteristics are:

## Slide 19: Wood Design and Construction
ASCE 7-16
AWC NDS, 2015 Edition – wood framing and connections
AWS SDPWS, 2015 Edition – shears, diaphragms, and anchorage
Notes: Graphics show covers of NDS and SDPWS documents.
In addition to building code requirements, the primary standards for engineered design of wood light-frame construction are:

## Slide 20: Wood Design and Construction
Supports ASD and LRFD
Framing and connections
  ASD: F’x = FxCDCyCz etc
  LRFD: F’x = FxKDxCyCz etc
Shear walls and diaphragms
  vASD = vs / 2
  vLRFD = Dvs = 0.8vs
Notes: The basic format used in the NDS includes the tabulated reference resistance Fx. The reference resistance is modified by a series of adjustment factors relating to end use conditions, resulting in an adjusted resistance F’x that can be compared to demand.
The SDPWS uses a different. Approach. The shear wall and diaphragm tables provide nominal resistances that are divided by two for use is ASD methods, or multiples by 0.8 for use in LRFD methods. Adjustments may still be required, including for framing member species.

## Slide 21: Lateral Systems (Bearing Walls)
Seismic Force Resisting System | Response Modification Coefficient, R | Seismic Design Category
Shear walls with wood structural panels | 6 ½ | B & C: NL D – F:65 ft max
Shear walls with other materials | 2 | B & C: NL D:35 ft max E & F: NP
Walls with flat strap bracing | 4 | B & C: NL D – F: 65 ft max

## Slide 22: Lateral Systems (Building Frame)
Seismic Force Resisting System | Response Modification Coefficient, R | Seismic Design Category
Shear walls with wood structural panels | 7 | B & C: NL D – F: 65 ft max
Shear walls with other materials | 2 1/2 | B & C: NL D: 35 ft max E & F: NP
Notes: For structures with a complete gravity load-resisting frame, the seismic design parameters are slightly different:
Graphic is table with two systems and associated parameters.

## Slide 23: Wood Design and Construction
Flexible vs Rigid Diaphragm – complexity:
Neither rigid nor flexible diaphragm assumptions truly represent the distribution of seismic forces in a typical structure – both are simplifications and the actual behavior is “semi-rigid”
Stiffness of the diaphragm relative to walls is important in determining whether behavior is more like rigid or more like flexible
Notes: One of the significant decisions that a designer will make is whether the horizontal diaphragm is idealized as flexible, idealized as rigid, or modeled as semi-rigid. This will affect horizontal distribution of seismic forces to the vertical seismic force-resisting elements, as well as diaphragm design. This decision will greatly affect the complexity of the analysis required to distribute forces. Some background that adds complexity to this decision includes:

## Slide 24: Wood Design and Construction
Flexible vs Rigid Diaphragm – more complexity:
Rigid diaphragm analyses ignore the stiffness of interior and exterior wall finishes, limiting the accuracy of results
“Glued and screwed" floor sheathing makes floors more rigid than flexible, and exterior walls can act as "flanges", further stiffening the diaphragm
Rigid diaphragm analysis may encourage the design of structures with torsional response
Notes: Additional sources of complexity include:
Because of these complexities, designers most often use ASCE 7 provisions that permit idealizing as flexible or idealizing as rigid.

## Slide 25: Diaphragms Idealized As Flexible
• ASCE 7 Sec. 12.3.1.1: Diaphragms constructed of untopped steel deck or wood structural panels are permitted to be idealized as flexible if any of the following conditions exist:
In structures where vertical elements are steel braced frames, steel and concrete composite braced frames, or concrete, masonry or steel and concrete composite walls
In one- and two-family dwellings
In structures of light-frame construction where all of the following conditions are met
  Nonstructural topping not greater than 1-1/2 inch
  Each line of vertical elements complies with drift limits
Notes: Applicable to wood light-frame construction, ASCE provides prescriptive provisions allowing diaphragms to be idealized as flexible. These are:

## Slide 26: Diaphragms Calculated As Flexible
• ASCE 7-05 Sec. 12.3.1.3:
“… the computed maximum in-plane deflection of the diaphragm under lateral load , dMDD, is more than two times the average story drift of adjoining vertical elements of the lateral force-resisting system of the associated story, DADVE, under equivalent tributary lateral load.”
Notes: The drawing shows a untopped wood structure panel, showing the maximum diaphragm deflection and average drift of vertical element.
ASCE 7 also provides provisions by which diaphragms can be determined to be flexible based on calculation. This method is:

## Slide 27: 2015 SDPWS Horizontal Distribution of Shear
  The SDPWS 2015 Modifications:
  Coordinating with ASCE 7 flexible, rigid, and semi-rigid diaphragm designations
  Providing greater clarity to provisions for open front and torsionally irregular buildings
  Buildings with cantilevered diaphragms are open-front
  Requiring rigid or semi-rigid diaphragm analysis for torsionally irregular buildings (Sec. 4.2.5.1)
  Require rigid or semi-rigid diaphragm analysis for diaphragm cantilevers in excess of six feet (Sec. 4.2.5.2)
  Limit diaphragm cantilevers to maximum of 35 feet
Notes: While ASCE 7 provisions would allow the vast majority of diaphragms to be idealized as flexible, permitting horizontal distribution of seismic forces by tributary area, the AWC wood design standards committee decided that more restrictive provisions were needed. The 2015 SDPWS require the use of rigid or semi-rigid diaphragm analysis when torsional irregularities occur, and when diaphragm cantilevers exceed six feet.

## Slide 28: Complete Load Path
Provision of a complete load path is essential to performance of wood light-frame seismic force-resisting systems
Due to nature of wood construction, this involves a number of connections
Will be discussed in detail for shear walls and diaphragms
Notes: Graphic is an elevation of a shear wall.
Read notes.

## Slide 29: Shearwalls
Notes: Graphic shows a photograph of a wood structural panel shear wall.
The next topic of discussion will be shear walls

## Slide 30: Shear Walls
Instructional Material Complementing FEMA P-751, Design Examples
Three types of shear walls:
Notes: Graphic shows elevations of three types of shear walls: segmented shear walls, shear walls designed for continuity around openings, and perforated shear walls.
SDPWS recognizes three distinct types of shear walls. Each has distinctive assumed behavior and distinctive design and detailing requirements. We will discuss these one at a time.

## Slide 31: Shear Walls
Segmented shear wall:
Notes: Graphic shows a segmented shear wall with two full-height wall segments, and tie-down anchors at each end of each segment
When designing a segmented shear wall, design only considers the portions of the wall with full height sheathing. Sheathing above and below windows and doors is ignored. Each full-height sheathed segment is designed as an individual shear wall. Overturning anchorage, where required, is provided at each end of each full-height segment.

## Slide 32: Shear Walls
Continuity around openings:
Notes: Graphic shows a shear wall designed and detailed for continuity around openings. The wall has two full-height piers and one window opening. Two tie-downs are provided, one at each end of the overall wall. Strapping and blocking is provided for the full length of the wall above and below the window opening.
Shear walls designed for continuity around openings consider the sheathing above and below openings to act as coupling beams. The coupling beams allow global overturning of the wall, including openings, to be developed, so that tie-downs are only required at the ends of the overall wall, rather than each full height segments. Special detailing, including strapping and blocking is required to develop the coupling beams.

## Slide 33: Shear Walls
Perforated shear wall:
Notes: The graphic shows a perforated shear wall with two full-height segments. Two tie-downs are provided, one at each end of the overall wall.
The perforated shear wall also considers the sheathing above and below the openings, and provides tie-downs at the ends of the overall wall. Rather than providing the added strapping and blocking to develop coupling beams, the perforated wall is used with a reduction in capacity. In concept, one full-height segment of each perforated shear wall has full overturning anchorage provided by a tie-down, and reaches full capacity as a result. The balance of the piers achieve partial anchorage due to the sheathing above and below openings, and have a reduced capacity and unit shear as a result.

## Slide 34: Shear Walls
Per AF&PA Sec. 4.3, design provisions include
Deflection determination
Unit shear capacities (shear wall tables)
Aspect ratios
Anchorage
Construction requirements
Notes: Graphic is photo of wood structural panel shear wall.
The primary requirements for shear walls are given in SDPWS Section 4.3 These include:

## Slide 35: Shear Walls
Shear wall table information
Nominal unit shear capacities
Tables are for DF-L or SP – need to adjust values if framing with wood species with lower specific gravities
Major divisions:
Structural I vs. Rated Sheathing
Panels applied directly to framing vs. panels applied over gypsum wallboard
Seismic and wind tabulated separately
Unblocked edges allowed in some conditions
Notes: The following are reminders about the nominal unit shear capacities in the SDPWS wood structural panel shear wall table:
DF-L is an abbreviation for the Douglas fir-Larch species group.
SP is an abbreviation for the Southern Pine species.

## Slide 36: Shear Walls
Aspect ratios
Application varies by shear wall type
Notes: Graphic shows elevations of three types of shear walls, taken from SDPWS
One of the limitations specified in SDPWS Sec. 4.3 are upper limits on aspect ratio of shear walls. Application of these aspect ratios is slightly different for the different shear wall types.
-Full height segment aspect ratios are limited for segmented and perforated shear walls
-Both wall pier and overall wall aspect ratios are limited for walls with continuity around openings
-Unit shear reductions are required for wood structural panel walls or segments with aspect ratios between 2.5 and 3.5.

## Slide 37: Design Example: Shear Walls
Section & Elevation
Plan
Typical apartment
partitions
Post & beam
lines
148'-0"
28'-0"
8'-0"
112" Lightweight concrete over plywood deck on joists at 16" o.c.
148'-0"
Corridor walls
Stairs
56'-0"
9'-0"
30'-0" 13'-0"
26'-0"
30'-0"
15'-0" 26'-0"
Sheathed
wall
Glazed wall
4'
9' 9' 9'
8'-0"
Doors
3-story apartment building
Stick framed with plywood shear walls and diaphragms
Seismic Design Category D
ASCE 7-05 Simplified Procedure
Notes: Graphic shows plan, section and elevation of the example building used in Exapmle Problem 14.1
Example Problem 14.1 illustrates the seismic design of two of the three types of shear walls, using a three story wood light-frame apartment building. We will use one of these walls to discuss seismic design of shear walls.

## Slide 38: Design Example: Shear Walls
.
•148'-0"
•56'-0"
•25'-0"
•25'-0"
•A
•30'-0"
•30'-0"
•15'-0"
•30'-0"
•15'-0"•30'-0"
•Solid interior
•wall
•Solid end
•wall
•Perforated
•exterior wall
•55 feet of net shear wall
•length, each side of
•corridor, distributed over
•length of building.
•56'-0"
•84'-0"
Interior shear wall, 25 feet long, solid
Notes: Graphic shows a plan of the apartment building with a center transverse wall circled in red.
The wall we will look at is a segmented wall resisting seismic forces in the transverse direction.

## Slide 39: Design Example: Shear Walls
9' 9' 9'
27'-0"
25'-0"
22.09 k
v = 0.883 k/ft
v = 0.704 k/ft
v = 0.346 k/ft
Wall design for in-plane shear
Horizontal shear load path
Overturning load path
Notes: Graphic shows elevation of the example three-story shear wall.
We will look at three major aspects of shear wall design:

## Slide 40: Design Example: Shear Walls
  Seismic Force to Center 50% Each Wall(strength level) x0.50 x0.50
  FROOF = 30.0 kips = 15.0 kips = 7.50 kips
  F3RD = 46.7 kips = 23.35 kips = 11.68 kips
  F2ND = 46.7 kips = 23.35 kips = 11.68 kips
Notes: Graphic shows elevation of three-story segmented shear wall.
From the example problem, the total seismic forces by story and the forces to this particular segmented shear wall are shown as:

## Slide 41: Design Example: Shear Walls
First floor design for shear:
V = 7.5 + 11.68 + 11.68 = 30.86 kips
For 25 foot shear wall shown
Unit Shear v1st = 30.86 kips/25 ft = 1.236 klf
This is strength level demand
Notes: The summed story shear for the first floor of the segment shear wall is…
Dividing by the 25 foot length, the unit shear is calculated to be…

## Slide 42: Design Example: Shear Walls
Capacity From SDPWS Table 4.3A for blocked wood structural panel shear walls
19/32 rated sheathing on Hem-Fir studs at 16” o.c.
Nominal unit shear capacity vs = 1.740 klf
F = 0.80 (SDPWS Sec. 4.3.3)
Adjustment for stud species with S.G. = 0.43
  = 1 – (0.5 – 0.43) = 0.93 (SDPWS Table 4.3A footnote)
Adjusted capacity = (0.93)(0.8)(1.740) = 1.294 > 1.236 OK
This shear wall requires 3x or stitched 2-2x framing members at abutting panel edges to avoid framing splitting during nail driving (SDPWS Sec. 4.3.7.1, Item 4)
Design shear anchorage to the foundation
Notes: The calculated demand is compared to the unit shear capacity based on SDPWS Table 4.3A:

## Slide 43: Design Example: Shear Walls
Strength level load combinations:
= 1.38D + 1.0QE + 0.5L + 0.2S (compression critical)
= 0.72D – 1.0QE (tension and uplift critical)
Notes: Graphic shows an elevation of the three-story segmented shear wall, with applied seismic horizontal loading causing overturning and dead load providing overturning resistance.
Following design for shear, the shear wall will need to be designed for overturning. The two applicable load combinations are:
The first combination will create critical compression loads due to overturning
The second combination will create critical uplift loads

## Slide 44: Design Example: Shear Walls
Diaphragm to shear wall / shear transfer through floor
Notes: Graphic to the left is a construction detail of framing and fastening required at the second floor level. Graphic to the right is the elevation of a shear wall with arrows to illustrate the transfer of shear from above the second floor to below the second floor.
As already noted, design of complete load path is important. The detail shown provides transfer of horizontal shear from the wall above the second floor to the wall below the second floor. The required nailing, other fastening or connections, is calculated based on the shear wall unit shears. Similar anchorage is made at the bottom of the shear wall to the foundation.

## Slide 45: Design Example: Shear Walls
Shear wall overturning / transfer of vertical forces through floor
Notes: Left graphic shows details of framing and connectors commonly used to transfer overturning from a shear wall above a floor level to a shear wall below a floor level. Right graphic shows the elevation of a shear wall with arrows indicating where this type of load path is typically required.
In addition to the shear load path, a load path needs to be maintained for tension and compression forces due to overturning on the shear wall.

## Slide 46: Design Example: Shear Walls
Overturning tension/compression to foundation
Notes: Left graphic shows details of framing and connectors commonly used to transfer overturning from a shear wall to the foundation. Right graphic shows the elevation of a shear wall with arrows indicating where this type of load path is typically required.
The overturning load path is also applicable at the shear wall to foundation interface.

## Slide 47: Diaphragms
Notes: Graphic shows an isometric of a wood structural diaphragm, including framing, sheathing and typical nailing.
The next topic to be discussed is diaphragms.

## Slide 48: Diaphragms
Diaphragm simplifying assumptions:
-Sheathing resists shear
-Chord resists tension, compression like beam flange
-Boundary element at every sheathing edge
Notes: Graphic shows a plan sketch of a diaphragm, next to it a section of an analogous steel beam, and below it a simple-span loading diagram.
Wood structural panel diaphragms are most often designed using the simplifying assumption that the sheathing carries shear only, analogous to the web of an wide-flange beam, and the chords carry tension and compression only, similar to flanges. Because the sheathing is assumed to only carry shear, a boundary member needs to be provided at every edge of the sheathing.

## Slide 49: Diaphragms
Continuous Panel Edge Parallel to Load
Unblocked Edge
Continuous Panel Edge
“Field” nailing Supported Edge
Diaphragm Boundary
“Edge” nailing
Diaphragm Sheathing
Notes: This isometric detail illustrates some of the components of a wood structural panel diaphragm

## Slide 50: Diaphragms
Diaphragm simplifying assumptions:
-Collector resists tension & compression
- Continuity assumption may vary at interior vertical element
Notes: Upper graphic is a plan view of an l-shaped building with three lines of shear walls, two exterior and one interior. Chords are shown at edges perpendicular to load direction, and collectors at edges parallel and at the interior shear wall line. Graphic below shows typical loading assumption, with two simple-spans.
Boundary elements at the edges of sheathing include chords along the edges perpendicular to the direction of load, and resisting moment from the diaphragm. Also, collectors along the edges parallel to the load as shown here. Collectors are also needed to move load from the diaphragm into interior vertical elements, as seen in the upper figure.

## Slide 51: Diaphragms
Diaphragm sheathing:
Blocked
Notes: Graphic shows an isometric of a blocked diaphragm.
Two primary types of wood structural panel diaphragm exist. One, shown here, is referred to as a block diaphragm. Framing is put behind every edge of every wood structural panel sheet, and edge nailing at a spacing of six inches on center or closer is provided at every edge in addition to field nailing,

## Slide 52: Diaphragms
Diaphragm sheathing:
Unblocked
Notes: Graphic shows anisometric of an unblocked diaphragm.
The other type is unblocked diaphragms. In this type ends of sheathing panels are supported on and fastened to sheathing, but other diaphragm edges do not necessarily fall on framing.

## Slide 53: Diaphragms
Diaphragm boundary elements:
Common chords and collectors
Notes: Graphic shows a detail of a roof diaphragm supported on the top of the shear wall and labels common members and fastening.
In many wood light-frame buildings, double top plates in the framed walls can serve as chords and collectors, as shown in this detail. In some cases top plates are not present, or chord and collector forces are larger than can reasonably be revisited by top plates and other chord and collector members must be added.

## Slide 54: Diaphragms
Design of Boundary Elements
  Tension force in one load direction, compression when reversed
  Every panel edge at exterior or interior is diaphragm boundary
  Collectors parallel and perpendicular to primary framing direction
Notes: The graphic shows a collector at an interior shear wall where the framing is perpendicular to the shear wall and straps and blocking need to be added to resist collector tension and compression forces.
Some reminders for design of collectors are:

## Slide 55: Diaphragms
Diaphragm boundary elements:
Common collectors
Notes: Collectors are sometimes provided in the wall rather than in the diaphragm, and can be designed by graphic load diagram methods like those shown.
The top graphic shows a wall elevation. The bottom graphic shows a load diagram of uniform shear coming into the wall from the diaphragm over the full length, and uniform shear going into the shear walls over partial lengths. The bottom diapgram shows the collector tension or compression at every location along the collector length.

## Slide 56: Diaphragms
Diaphragm boundary elements:
Detailing at diaphragm openings
Notes: Graphic shows the plan view of a diaphragm with a significant opening, and boundary members at each side of the opening and extending beyond.
The designer is reminded that boundary members need to be provided at internal openings in diaphragms, and extend beyond to distribute tension and compression forces back into the diaphragm. APA The Engineered Wood Association publishes technical guidance on design of diaphragms with openings.

## Slide 57: Diaphragms
Subdiaphragms providing diaphragm continuous ties at concrete or masonry walls
Notes: Graphic shows a plan view of a diaphragm in which smaller subdiaphragms are identified.
Subdiaphragms are an important part of the system anchoring concrete or masonry walls for seismic out-of-plane forces. These will be discussed in the last section of this presentation.

## Slide 58: Diaphragm Seismic Design Forces
Diaphragm Seismic Design Forces
Inertial forces
  generated by the seismic weight tributary to the diaphragm
Notes: New under ASCE 7-16 there are two methods to calculate diaphragm inertial forces generated at each floor level due to the tributary mass. As in past editions of ASCE 7, the basic method is shown here and is addressed in Sec. 12.10.1. New with ASCE 7-16 is the alternate diaphragm design methodology of Section 12.10.3. This method specifically considers the ductility and displacement capacity of each diaphragm system, and assigned a diaphragm “R-factor, noted as Rs

## Slide 59: Diaphragm Seismic Design Forces
Diaphragm Seismic Design Forces
Inertial forces
Transfer forces
  generated by discontinued vertical elements or
  generated by changes in stiffness of vertical elements over height of structure
Notes: Graphic is a photo of a dingle family dwelling with offsets between second story and first story shear walls. The dwelling has transfer forces in the diaphragm due to the second floor shear wall shear being transferred by the diaphragm from the bottom of the second floor walls to the top of the first floor walls.
In addition to inertial forces, it is important that forces transferred from one shear wall line to another (transfer forces) are accounted for in determining diaphragm design seismic forces.

## Slide 60: Diaphragm Seismic Design Forces
Diaphragm Seismic Design Forces
Diaphragm design must be consistent with diaphragm classification – rigid, semi-rigid, flexible
Sheathing
  Design for in-plane shear in accordance with SDPWS
Boundary members and connections
  Design for tension and compression in accordance with NDS
  No overstrength forces for chords
  No overstrength forces for collectors for structures or portions thereof braced entirely by light-frame shear walls (ASCE 7-10, Sec. 12.10.2)
Notes: Some reminders for design of diaphragms are:

## Slide 61: Diaphragm Seismic Design Forces
Per SDPWS Sec. 4.2, design provisions include:
Deflection determination
Unit shear capacities (diaphragm tables)
Aspect ratios
Boundary members
Construction requirements
Notes: Graphic shows isometric of diaphragm.
The primary design provisions for diaphragms are found in SDPWS Section 4.2. topics covered include:

## Slide 62: Design Example: Diaphragm
SPAN = 88 ft
W = 0.202 klf
Horizontal distribution of seismic force at roof:
VROOF = 30 kips - wTRANS = 30/ 148 ft. = 0.202 klf
Notes: Graphic shows floor plan with diaphragm span of interest highlighted, a uniform load applied and reactions at interior and exterior shear walls.
Example 14.1 illustrates design of floor and roof diaphragms in the three-story apartment building. This slide illustrates the application of uniform diaphragm loading to an 88 foot diaphragm span.

## Slide 63: Design Example: Diaphragm
Horizontal distribution of seismic force at roof:
VROOF = 30 kips
wTRANS = 30/ 184 ft. = 0.202 klf
For 88 foot span shown
R = w(L)/2 = 0.202(88 ft)/2 = 8.93 kips
Unit Shear vROOF = 8.93 kips/56 ft = 0.160 klf
This is strength level demand
Notes: From these loading and span assumptions, diaphragm reactions and unit shears are calculated.

## Slide 64: Design Example: Diaphragm
For 88 foot span shown
Unit Shear vROOF = 8.93 kips/56 ft = 0.160 klf
This is strength level demand
Capacity From SDPWS Table 4.2C for unblocked wood structural panel diaphragms
Construct as load case 1 for transverse load direction, since this is longest span
15/32 rated sheathing on 2x DF-L framing
Nominal unit shear capacity vs = 0.480 klf
F = 0.80 (SDPWS Sec. 4.2.3)
Adjusted capacity = (0.8)(0480) = 0.384 > 0.160 OK
Notes: This is compared to the LRFD allowable shear, taken in this case from Table 4.2C for unblocked diaphragms. The adjusted capacity is then compared to the calculated LRFD unit shear.

## Slide 65: Design Example: Diaphragm
SPLICE IN TOP PLATE
TWO ROWS 16d @ 6” O.C. EA. ROW, STAGGER (14 NAILS MINIMUM)
TWO ROWS 16d @ 6” O.C. EA. ROW, STAGGER (14 NAILS MINIMUM)
For 88 foot span shown
Chord = M/56 ft = 197/ 56 ft = 3.51 kips T/C
Use 2- 2x6 top plates as chord. Splice top plates with 16d common nails
Reference (tabulated) nail capacity Z = 0.122 kips/nail (NDS Table 12N)
Z’ = ZKFFl = (0.122)(3.32)(0.65)(1.0) = 0.263 kips/nail
Number of nails = 3.51 kips/ 0.263 = 13.3, use 14 min
Notes: Graphic shows double top plate with centered splice in upper top plate, and fastening to either side of the splice to transfer the chord force.
Similarly, simple calculations can the used to determine chord forces in the double top plates, and fastening required at splices in the top plates as shown here.

## Slide 66: Anchorage of Concrete and Masonry Walls
Notes: The figure shows anchorage of Concrete and Walls.
The last section of this presentation addresses the seismic forces for design of concrete and masonry wall anchorage to diaphragms. This includes both the force requirements of ASCE 7 Section 12.11.1, applicable for all wall types, and the additional requirements of Section 12.11.2, applicable to concrete and masonry walls in SDC C and higher.

## Slide 67: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: The right hand photos shows tilt-up walls collapsed and partial roof collapses due to the failure of wall anchorage. The left hand photo shows a wall that has separated from the roof diaphragm, but not fallen, and supported by shoring installed following the earthquake.
These photos illustrate the poor seismic performance from past earthquake of the anchorage of tilt-up concrete walls to wood diaphragms. The types of failures shown have been repeated in virtually every US earthquake starting with the 1964 Alaska Earthquake.

## Slide 68: Wall-to-Diaphragm Anchorage and Continuous Ties
Inertial Force
Resisting Force
Ledger Failure
Tension perpendicular to grain results in brittle failures at low loads
Does not provide a reliable load path
Notes: Graphic shows a tilt-up wall panel connection to a wood diaphragm. The wall anchorage uses bolts in a wood ledger. When the wall pulls one way at the ledger bolt, and the plywood pulls the top of the ledger in the other direction, this causes cross grain tension in the ledger, resulting in failure of the ledger.
Seen earlier in this presentation, this graphic shows one of the common failure mechanisms in older tilt-up wall building where positive tension anchorage direct from the wall to the perpendicular framing member was not provided.

## Slide 69: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: Graphic shows the bottom of a shear wall, with sheathing and sill plate. The sill plate is anchored at mid-width with an anchor bolt. The plywood sheathing and nailing pulls up on one edge of the sill, causing cross-grain tension.
This shows a very similar mode of failure that affects shear wall sill plates when steel plate washers are not provided. The mechanism of cross-grain tension in the sill plate is exactly the same.

## Slide 70: Wall-to-Diaphragm Anchorage and Continuous Ties
Design Considerations
  Substantial experience w/ earthquake performance
  Numerous studies on seismic demand on these connections
  Even more recent construction may required retrofit
  Objective is tie between exterior walls
Notes: Graphic shows plan of diaphragm with subdiaphragms designated.
There are two equally important portions of the design to anchor concrete and masonry walls to wood diaphragms.
-Wall anchorage per Section 12.11.2.1
-Continuous ties from wall anchorage across the entire width of the diaphragm per Section 12.11.2.2.3
Both of these provisions have come from substantial experience with poor performance in earthquakes

## Slide 71: Wall-to-Diaphragm Anchorage and Continuous Ties
For walls anchored to flexible diaphragms, wall anchorage force per ASCE 7-05 Sec. 12.11.2.1 and Eq. 12.11-1 is:
Fp = 0.4SDSkaIeWp
Where
ka = 1.0 + Lf/100 <= 2.0
Lf = diaphragm span = 200 ft
Ka = 1.0 + 200/100 = 3.0, use 2.0 max
Notes: Graphic shows masonry wall with anchorage to a wood diaphragm.
Example 14.2 provides details of calculation of wall anchorage forces in accordance with ASCE 7, as seen in this slide.

## Slide 72: Wall-to-Diaphragm Anchorage and Continuous Ties
Fp = 0.4SDSkaIeWp
Where
ka = 2.0
SDS = 1.43
Ie = 1.0
Transverse walls:
Wp= 65 psf(16ft)= 1.04 klf
Fp = 0.4(1.43)(2.0)(1.0)1.04 = 1.19 klf
Anchors at 4 ft = 1.19 (4.0)= 4.76 kips
Notes: Graphic shows a masonry wall with anchorage to a wood diaphragm.
From Problem 14.2, this shows the calculation of an anchorage force for a wall anchor spacing of 4 feet. It should be noted that the wall anchorage is at a very high force level compared to the base shear for the overall structure.

## Slide 73: Wall-to-Diaphragm Anchorage and Continuous Ties
Detailing Considerations - Wood
  Often want anchor to carry both tension and compression
  Anchors typically at 4 to 8 feet on center
  Preference is for symmetrical connections
Notes: Graphic shows a concrete wall anchored to a wood diaphragm with a tie-down device.
This detail shows one of several typical configurations of wall to diaphragm anchors. Note that a block is added for transfer both tension and compression loads.

## Slide 74: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: Graphic on the left shows a section and plan view of double tie-downs installed symmetrically on either side of a framing member. Graphic on the left hand side shows anchorage with threaded steel rods and wood blocks.
These are additional common details for wall to diaphragm framing anchors.

## Slide 75: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: Graphic is a concrete wall anchored to a wood roof beam with a tie-down device.
This is an installed wall anchor suing a tie-down device.

## Slide 76: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: This is a close-up of the device previously shown.

## Slide 77: Wall-to-Diaphragm Anchorage and Continuous Ties
The subdiaphragm concept:
Cannot run tension ties at 4 ft on center across entire length of building, so develop into subdiaphragm
Design subdiaphragm for anchorage force level
Subdiaphragm reaction goes to major beam line
Design continuous tie connections across major beam lines for anchorage force level
Notes: As noted previously, ASCE 7 requires that continuous ties from wall anchorage be run across the entire width of the diaphragm. This is required due to concerns that a small portion of the diaphragm could be pulled away from the main diaphragm due to high anchorage loads. To avoid this, the continuous ties distribute the wall anchorage forces across the full diaphragm depth. This, however , is not practical to do at 4 feet on center….

## Slide 78: Wall-to-Diaphragm Anchorage and Continuous Ties
The subdiaphragm concept:
Wall anchorage to subdiaphragm at 4 ft.
Subdiaphragm approx. 20 ft. x 20 ft.
Glulam beams and connections act as continuous ties
Notes: Graphic shows plan of roof diaphragm with continuous ties in the longitudinal direction. Wall anchorage is shown with blue lines, sub diaphragms are shown with red boxes, and continuous ties on main beam lines are shown with green lines.
In this plan view of the diaphragm, wall anchors (blue) are extended across the depth of the sub diaphragm (red). The sub diaphragms are design for wall anchorage level forces. The subdiaphragms transfer wall anchorage forces into the major beam lines (green) that act as continuous ties across the diaphragm. This approach satisfies the ASCE 7 requirements. The same type of system must be provided in the perpendicular direction for the longitudinal walls.

## Slide 79: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: Graphic shows two beams abutting each other and pairs of tie-down devices used to create a direct-tension connection from beam to beam.
This detail illustrates a beam-to-beam connection where the beams serve as a continuous tie.

## Slide 80: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: This detail illustrates a beam-to-beam connection where the beams serve as a continuous tie. In this case the beams on either side are connected through a girder.
Graphic shows two beams abutting each other and pairs of tie-down devices used to create a direct-tension connection from beam to beam.

## Slide 81: Wall-to-Diaphragm Anchorage and Continuous Ties
Notes: This photo shows installed a continuous tie beam-to-beam connection like the one just discussed.

## Slide 82: Wall-to-Diaphragm Anchorage and Continuous Ties
Important items for wall anchorage of concrete and masonry walls SDC C and up (Section 12.11.2.2):
Continuous ties required between diaphragm chords
Subdiaphragms permitted as part of continuous tie system provided subdiaphragm aspect ratio <=2.5
Wall anchor forces required through the entire continuous tie system
Forces multiplied by 1.4 for steel elements of anchorage
Diaphragm wood structural panel sheathing not permitted to be loaded in tension to provide continuous tie
Embedded tension straps to be wrapped around or anchored to wall reinforcing
Notes: In addition to the requirements for continuous ties, ASCE 7 Section 12.11.2.2 has additional requirements for anchorage of concrete and masonry walls in SDC C and higher.

## Slide 83: Questions?

## Slide 84: DISCLAIMER
NOTICE: Any opinions, findings, conclusions, or recommendations expressed in this publication do not necessarily reflect the views of the Federal Emergency Management Agency. Additionally, neither FEMA nor any of its employees make any warranty, expressed or implied, nor assume any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, product or process included in this publication.
The opinions expressed herein regarding the requirements of the NEHRP Recommended Seismic Provisions, the referenced standards, and the building codes are not to be used for design purposes. Rather the user should consult the jurisdiction’s building official who has the authority to render interpretation of the code.
Any modifications made to the file represent the presenters' opinion only.