## Slide 1: Masonry Structures James Robert Harris, PE, PhD, and Fredrick R. Rutz, PE, PhD
Disclaimer
Edited by David Sommer, PE, SE
Includes materials originally developed by
Richard Klingner, PE, PhD
Notes: Title slide, consisting of an image of the cover of the data disk containing the 2015 NEHRP Recommended Seismic Provisions.
Title Slide for Masonry Structures

## Slide 2: SEISMIC DESIGN OF MASONRY STRUCTURES
Notes: In this first slide, we see examples of different applications of masonry : on the left, a low-rise bearing-wall building of reinforced masonry; in the center, a high-rise bearing-wall building of reinforced masonry; and on the right, stone and clay unit veneer over a frame structure.
Topic 13 deals with the seismic design of masonry structures.

## Slide 3: NEHRP Recommended Provisions Masonry Structures:
Shear wall in-plane design
Masonry walls out-of-plane
Overstrength concepts
Details
Simplified design for wall-type structures
Shear wall design example
Context in the Provisions
Reference standards
Masonry basics
Masonry behavior
Organization of TMS 402 Code
Types of shear walls
Notes: This slide presents an overview of the presentation.
This is a list of topics covered in this review module on masonry design according to the NEHRP Recommended Provisions, which is developed for the Federal Emergency Management Agency (FEMA) by the Building Seismic Safety Council (BSSC) of the National Institute of Building Sciences (NIBS).

## Slide 4: Objectives of Module
Basics of masonry behavior
The TMS 402 Building Code and TMS 602 Specification and the relationship of NEHRP Recommended Provisions documents to it
Earthquake design of masonry structures and components using the 2013 TMS 402 Code and TMS 602 Specification
Example of masonry shear wall design
Notes: This slide lists the objectives of the presentation.
Because many in the intended audience may not have studied masonry recently, the module begins with a review of the basic components of masonry and of the basic behavior of wall-type structures. It then addresses the specification of masonry units, mortar, grout, and accessory materials. It continues with the rudiments of the mechanical behavior of masonry. It then reviews The Masonry Society (TMS) Code and Specification, which is the fundamental technical resource behind the NEHRP Recommended Provisions. It concludes with the design and detailing of a reinforced masonry shear wall.

## Slide 5: NEHRP Recommended Provisions Masonry Design
Basic Documents
NEHRP Recommended Provisions
ASCE 7-16, Minimum Design Loads for Buildings and Other Structures
TMS 402-13, Building Code Requirements for Masonry Structures
TMS 602-13, Specification for Masonry Structures
IBC 2015, International Building code
Notes: This slide lists references used for the design of reinforced masonry.
This is a list of topics covered in this review module on masonry design according to the NEHRP Recommended Provisions, which is developed for the Federal Emergency Management Agency (FEMA) by the Building Seismic Safety Council (BSSC) of the National Institute of Building Sciences (NIBS).

## Slide 6: NEHRP Recommended Provisions Masonry Design
Masonry Basics
Notes: This slide is the intro slide to the masonry basics section of the presentation.
This is a list of topics covered in this review module on masonry design according to the NEHRP Recommended Provisions, which is developed for the Federal Emergency Management Agency (FEMA) by the Building Seismic Safety Council (BSSC) of the National Institute of Building Sciences (NIBS).

## Slide 7: Review Masonry Basics
Basic terms
Units
Mortar
Grout
Accessory materials
  Reinforcement (may or may not be present), connectors, flashing, sealants
Typical details
Notes: This slide lists an overview of topics covered for the masonry basics section.
Let’s start by reviewing masonry basics. Masonry is made up of units, mortar, grout, and accessory materials. The mortar holds the units together as well as apart, compensating for their dimensional tolerances. The grout is a fluid concrete mixture used to fill voids in the masonry and to anchor deformed reinforcement.

## Slide 8: Basic Terms
Running bond
Stack bond
1/3 Running bond
Flemish bond
bed
joints
head
joints
Bond patterns (looking at wall):
Notes: This figure illustrates common types of masonry bond patterns, including running bond, stack bond, 1/3 running bond, and flemish bond.
Masonry units can be laid in different bond patterns. The most common of these is 1/2 running bond, often called simply “running bond.” Horizontal bed joints are continuous; vertical head joints alternate courses, and the head joint of one course aligns with the middle of the unit on the adjacent courses. In stack bond (referred to in TMS 402 and Specification as “other than running bond”), the head joints are continuous between adjacent courses.

## Slide 9: Masonry Units
Concrete masonry units (CMU):
  Specified by ASTM C 90
  Minimum specified compressive strength (net area) of 2000 psi (average)
  Net area is about 55% of gross area
  (varies with size)
  Nominal versus specified versus actual dimensions
  Type I and Type II designations no longer exist
Notes: This picture presents basics of concrete masonry units (CMU)
Masonry units have three basic systems of dimensions: nominal, specified, and actual.
Nominal dimensions are used to lay out a structure. A common size C90 unit has nominal dimensions of 8 by 8 by 16 inches.
Specified dimensions are nominal dimensions minus one-half the thickness of a joint on all sides of the unit. Since masonry joints are normally 3/8-in. thick, the specified dimensions of a nominal 8 x 8 x 16-in. unit are 7-5/8 by 7-5/8 by 15-5/8 inches.
Actual dimensions are what the unit actually measures and should lie within the specified dimensions, plus or minus the specified dimensional tolerance.

## Slide 10: Masonry Units
Clay masonry units:
  Specified by ASTM C 62 or C 216
  Usually solid, with small core holes for manufacturing purposes
  If cores occupy  25% of net area, units can be considered 100% solid
  Hollow units are similar to CMU - can be reinforced
Notes: This picture presents basics of brick masonry units
Clay masonry units are specified by ASTM C62 (building brick) or C216 (facing brick). They are usually solid and may have small core holes to facilitate drying and firing. Because clay masonry units usually have more than enough compressive strength, the core holes are ignored unless they occupy more than 25% of the area of the units.

## Slide 11: Masonry Mortar
Mortar for unit masonry is specified by ASTM C 270
Three cementitious systems
  Portland cement + lime + sand (“traditional”)
  Masonry cement mortar (lime is included in cement)
  Mortar cement mortar (lime is included in cement, higher air contents)
Notes: This slide introduces the basics of masonry mortar
Mortar for unit masonry is specified by ASTM C270. In specifying mortar, the designer must make three decisions:
The first decision involves the cementitious system to be used. Three cementitious systems are available: portland cement-lime mortar; masonry cement mortar; and mortar cement mortar.

## Slide 12: Masonry Mortar
Plastic mortar properties
  Workability Important for good bond
  Water retentivity
  Rate of hardening
Hardened mortar properties
  Bond Important, seldom specified
  Compressive strength
  Volume stability
  Durability
Notes: This slide lists desirable properties of masonry mortar
Mortar for unit masonry is specified by ASTM C270. In specifying mortar, the designer must make three decisions:
The first decision involves the cementitious system to be used. Three cementitious systems are available: portland cement-lime mortar; masonry cement mortar; and mortar cement mortar.

## Slide 13: Masonry Mortar
Within each cementitious system, mortar is specified by type (M a S o N w O r K):
  Going from Type K to Type M, mortar has an increasing volume proportion of portland cement. It sets up faster and has higher compressive and tensile bond strengths.
  As the volume proportion of portland cement increases, mortar is less able to deform when hardened.
  Types M and S are specified for modern structural masonry construction.
  Type N for non-loadbearing and for brick veneer
  Type O or K for historic masonry repairs
Notes: This slide lists the different types of mortar and their uses
Within each cementitious system, the designer must specify the mortar type. Mortar type describes the amount of cement in the mortar compared to the amount of other constituents.
The designations for mortar type were intentionally selected as alternating letters in the phrase “mason work,” avoiding the connotations that might be associated with designations such as “A,” “B,” “C,” and “D.”
Going from Type K to Type M, mortar has an increasing volume proportion of portland cement or other cements. It sets up faster and has higher compressive and tensile bond strengths. As the volume proportion of portland cement increases, mortar is less able to deform when hardened.
Types N and S are specified for modern masonry construction.

## Slide 14: Grout
Grout for unit masonry is specified by ASTM C 476
Two kinds of grout:
  Fine grout (cement, sand, water)
  Coarse grout (cement, sand, pea gravel, water)
ASTM C 476 permits a small amount of hydrated lime, but does not require any. Lime is usually not used in plant – batched grout.
Notes: This slide introduces the basics of masonry grout.
Grout for unit masonry is specified by ASTM C 476, which addresses two kinds of grout: fine grout which is composed of cement, sand and water and coarse grout, which is composed of cement, sand, pea gravel and water. The fairly common practice of specifying grout as concrete is acceptable but only if the resulting mixture proportion conforms to C476.
ASTM C 476 permits a small amount of hydrated lime but does not require any. Lime is usually not used in plant-batched grout because lime is not available in such plants.

## Slide 15: Grout
The proportion of water is not specified. The slump should be 8 to 11 in.
Masonry units absorb water from the grout decreasing its water-cement ratio and increasing its compressive strength. High-slump grout will still be strong enough.
Notes: This slide lists basics of grout in masonry.
The proportion of water in grout is not specified. The slump should be 8 to 11 inches.
Masonry units absorb water from the grout, decreasing its water-cement ratio and increasing its compressive strength. High-slump grout will still be strong enough.

## Slide 16: Role of fm
Concrete:
  Designer specifies value of fc
  Compliance is verified by compression tests on cylinders cast in the field and cured under ideal conditions
Masonry
  Designer specifies value of fm
  Compliance is verified by “unit strength method” or by “prism test method”
Notes: This slide compares the use of f’m in masonry to f’c in concrete.
In designing and specifying masonry according to TMS 402, the role of f’m is analogous to that of f’c for concrete.
For concrete, the designer states an assumed value of fc and compliance is verified by compression tests on cylinders cast in the field and cured under ideal conditions.
For masonry, the designer states an assumed value of fm and compliance is verified either by the “unit strength method,” or by the “prism test method.”

## Slide 17: Application of Unit Strength Method (Specification Tables 1, 2)
Designer determines required material specification:
  Designer states assumed value of fm
  Specifier specifies units, mortar and grout that will satisfy “unit strength method”
  Compliance with fm can be verified with no tests on mortar, grout, or prisms (but need verification of units’ compressive strength)
Notes: This slide lists the procedure to comply with the specified f’m using the unit strength method.
If compliance with the specified f’m is verified by the unit strength method and compliance with ASTM C270 (mortar) and ASTM C476 (grout) is verified by proportion), no job-specific testing whatsoever is required.

## Slide 18: Procedure for Strength Design of Reinforced Masonry Shear Walls
Select trial design.
Compute factored design moments and shears for in- and out-of-plane loading. Include p-d for out-of-plane deflection and moment.
Design flexural reinforcement as controlled by out-of-plane loading.
Design flexural reinforcement as controlled by in-plane loading and revise design as necessary.
Check to ensure ductility.
Check shear capacity and revise if required.
Check detailing.
Notes: This slide lists the typical procedure for strength design of reinforced masonry shear walls.

## Slide 19: Component Design: Design of walls
Out-of-plane forces, Fp
Out-of-plane
bending and shear
Notes: This picture shows a wall subject to out of plane forces deflecting out in the direction of the force. The wall boundary conditions are shown acting as not restraining rotation.
This loading applies to all masonry walls, whether “participating” or not. If not participating, the connections at the top must allow relative motion in the plane of the wall.

## Slide 20: Component Design basics
T - beam section assumed to resist out-of-plane flexure
(Masonry laid in running bond)
beff = 6t < s < 72”
s s
- -
Notes: This slide shows Tee-beam design grouted wall.
Tee-beam design is much the same as in reinforced concrete.

## Slide 21: Component Design basics
Force distributed according to relative stiffness
In-plane force
Notes: This slide shows a wall subject to an in plane force distributed to wall segments of various length.
Basic concept of analysis for distribution of seismic forces; the unit force will be higher in the stiffer elements.

## Slide 22: NEHRP Recommended Provisions Masonry Design
Masonry Behavior
Notes: This slide is the introductory slide to the Masonry Behavior subject in the presentation.
This is a list of topics covered in this review module on masonry design according to the NEHRP Recommended Provisions, which is developed for the Federal Emergency Management Agency (FEMA) by the Building Seismic Safety Council (BSSC) of the National Institute of Building Sciences (NIBS).

## Slide 23: Masonry Behavior
On a local level, masonry behavior is nonisotropic, nonhomogeneous, and nonlinear.
On a global level, however, masonry behavior can be idealized as isotropic and homogeneous. Nonlinearity in compression is handled using an equivalent rectangular stress block as in reinforced concrete design.
A starting point for masonry behavior is to visualize it as very similar to reinforced concrete. Masonry capacity is expressed in terms of a specified compressive strength, fm, which is analogous to fc.
Notes: This slide lists basics of masonry behavior.
In the context of the TMS 402/602 Code and Specification as referenced by the NEHRP Recommended Provisions, masonry is composed of units held together by mortar. The masonry is usually reinforced (either by prescription or by design methodology), and the reinforcement is surrounded by grout. The result is an integral material very similar to reinforced concrete.

## Slide 24: Masonry Behavior
Running bond
- half units
Stacked bond
- only mortar
Head joint weakness
Notes: This slide shows three illustrations. The first is a plan view of a masonry wall. The second is an elevation of a wall with stack bond, and a section showing that head joints with mortar create a continuous vertical plane. The third is an elevation of a wall with running bond, and a section showing that head joints with mortar are interrupted by units in a vertical plane.
Head joints are weak because the mortar shrinks. In contrast to bed joints, there is no gravity action to maintain the contact.

## Slide 25: Masonry Behavior
Crowded cells make grout flow difficult
Notes: Slide shows cell with congested reinforcement making it difficult to flow grout into place.

## Slide 26: Masonry Behavior: out-of-plane
flexural
strength
anchorage
Notes: Slide shows possible out-of-plane failures (flexural strength and anchorage failures) in masonry walls, which includes a figure of masonry wall, a masonry all fail with flexural failure, and a masonry wall fail with anchorage failure.

## Slide 27: Summary of Masonry Behavior
4-Way Composite Action
Units, mortar, reinforcement, grout
Compression
High strength
Brittle -- low ductility
Confinement difficult to achieve
Tension
Good strength when reinf. takes tension
Very little strength without reinf.
(continuous joints are a plane of weakness)
Notes: This slide lists a summary of masonry behavior.
Summary of Masonry Behavior

## Slide 28: Design Implications from Masonry Behavior
Unreinforced
Design as elastic / brittle material
R factors very low
Design force = EQ force
Reinforced
Design similar to reinforced concrete
Confinement, ductility difficult to achieve
R factors lower than concrete
Notes: This slide lists design implications for masonry structures
Design implications for masonry structures

## Slide 29: NEHRP Recommended Provisions Masonry Design
Organization of TMS 402 Code
Notes: This slide is the introduction slide to the section of the presentation on Organization of TMS 402 Code.
This is a list of topics covered in this review module on masonry design according to the NEHRP Recommended Provisions, which is developed for the Federal Emergency Management Agency (FEMA) by the Building Seismic Safety Council (BSSC) of the National Institute of Building Sciences (NIBS).

## Slide 30: Seismic Design for Masonry Hierarchy of Standards
NEHRP
Recommended
Provisions
ASCE7
ASCE/SEI
TMS 402
MSJC
IBC
ICC
Building Code
Local law
ASTM Standards
Material & Test Methods
TMS 602
MSJC
Project Documents
Dwgs & Specs
TMS 402
TMS 602
Notes: Slide is a diagram of design standards used for Masonry structures.

## Slide 31: Organization of 2013 TMS 402 Code
Part 1, General
Chapters 1-3
Ch. 8,
Allowable
Stress
Design
Ch. 9, Strength Design
Ch. 10,
Pre-
stressed
Masonry
Ch. 12,
Veneer
Ch. 13,
Glass
Block
Ch. 14,
Partitions
8.1, General ASD
8.2, URM
8.3, RM
6.1, General
6.2, Anchored
6.3, Adhered
9.1, General SD
9.2, URM
9.3, RM
TMS 602
Specification
Ch. 11, AAC
Part 2, Design Requirements
Chapters 4-7 (Analysis and Design, Elements,
Reinforcement, Seismic)
Part 3, Engineered Design Methods
Chapters 8-11
Part 4, Prescriptive Design Methods
Chapters 12-14
Appendices
A, B, and C
Notes: This slide shows the organization of TMS 402.
This slide shows the organization of TMS 402. It is linked to the TMS 602 Specification.
TMS 402-13 has been significantly reorganized from previous editions. It is now divided into four main parts; General, Design Requirements, Engineered Design Methods, and Prescriptive Design Methods.

## Slide 32: Organization of 2013 TMS 602 Specification
TMS 402 Code
Part 1
General
Part 2
Products
Part 3
Execution
1.6 Quality
assurance
3.1 - Inspection
3.2 - Preparation
3.3 - Masonry erection
3.4 - Reinforcement
3.5 - Grout placement
3.6 - Prestressing
3.7 - Field quality control
3.8 - Cleaning
2.1- Mortar
2.2 - Grout
2.3 - Masonry Units
2.4 - Reinforcement
2.5 - Accessories
2.6 - Mixing
2.7 - Fabrication
TMS 602
Specification
Notes: This slide shows the organization of TMS 602.
TMS 602 is referenced by and linked to TMS 402. The Specification has three articles governing general provisions, products, and execution, respectively.

## Slide 33: Organization of TMS 402 Code Part 1 – General
Chapter 2
2.1 Notation
2.2 Definitions
Chapter 3
3.1 Quality assurance program
3.2 Construction
Chapter 1
1.1 Scope
1.2 Contract documents and calculations
1.3 Special systems
1.4 Reference standards
Notes: This slide lists the sections in Part 1 of TMS 402
Part 1 of TMS 402 gives general requirements, notation and definitions, and QA and Construction requirements. As with other slides, the sections marked in orange are emphasized in the slides that immediately follow.

## Slide 34: Organization of TMS 402 Code Part 2 – Design Requirements
Chapter 4
4.1 Loading
4.2 Material properties
4.3 Section properties
4.4 Connections to structural frames
4.5 Stack bond masonry
Chapter 5
5.1 Masonry assemblies
5.2 Beams
5.3 Columns
5.4 Pilasters
5.5 Corbels
Chapter 6
6.1 Details of reinforcement
6.2 Anchor bolts
Chapter 7
Seismic design requirements
Notes: This slide lists the sections in Part 2 of TMS 402
Part 2 of TMS 402 gives design requirements and criteria that apply independent of which analysis method is used.

## Slide 35: Code 4.2, Material Properties
Prescriptive modulus of elasticity:
  Em = 700 f’m for clay masonry
  Em = 900 f’m for concrete masonry
  or
  Chord modulus of elasticity from tests
Shear modulus, thermal expansion coefficients, and creep coefficients for clay, concrete, and AAC masonry
Moisture expansion coefficient for clay masonry
Shrinkage coefficients for concrete and AAC masonry
Notes: This slide is a summary of the material property provisions in TMS 402.
Code Section 4.2 deals with material properties to be used for design. It specifies the values of chord modulus of elasticity, shear modulus, thermal expansion coefficients, and creep coefficients for clay, concrete, and AAC masonry. It also gives moisture expansion coefficients to be used for clay masonry and shrinkage coefficients to be used for concrete and AAC masonry.

## Slide 36: Code 4.3, Section Properties
Use minimum (critical) area for computing member stresses or capacities
  Capacity is governed by the weakest section; for example, the bed joints of face-shell bedded hollow masonry
Notes:   The figure shows the bed joints of face-shell bedded hollow masonry.
TMS 402 uses two different ways of computing section properties. To compute member stresses or capacities, use the weakest section. For hollow unit masonry bedded on the outside only (face-shell bedding), this is the area of the face shells only.

## Slide 37: Chapter 7, Seismic Design
General analysis
  Element interaction
  Refer to ASCE7-10, Sec. 1.4, General Structural Integrity:
    Load path connections
    Notional lateral forces
    Connection to supports
    Anchorage of walls
Notes: This slide is a summary of the general analysis seismic design provisions in TMS 402.
Basics of seismic design

## Slide 38: Chapter 7, Seismic Design
General analysis
  Drift limits: Use legally adopted building code or ASCE7
  Drift limits assumed satisfied for many wall types
    Special Reinforced Masonry walls are the exception to this rule
Notes: This slide is a summary of the general analysis seismic design provisions in TMS 402.
Basics of seismic design.

## Slide 39: Chapter 7, Seismic Design
Seismic Design Category C:
  Empirical and plain not permitted, all other types of shear walls permitted:
    Ordinary reinforced
    Intermediate reinforced
    Special reinforced
  Participating walls shall be reinforced
  Non-participating walls must meet minimum prescriptive requirements for horizontal or vertical reinforcement
  At least 80% of lateral resistance in a given line shall be by shear walls
Notes: This slide is a summary of the seismic design provisions in TMS 402 for SDC C.
In Seismic Design Category C, all walls must be considered shear walls unless isolated. Shear walls must meet minimum prescriptive requirements for reinforcement and connections (ordinary reinforced, intermediate reinforced, or special reinforced) and other walls must meet minimum prescriptive requirements for horizontal or vertical reinforcement.

## Slide 40: Chapter 7, Seismic Design
Seismic Design Category D:
  Only special reinforced type of shear wall permitted
  Shear walls must meet minimum prescriptive requirements for reinforcement and connections (special reinforced)
  Type N mortar and masonry cement mortars are prohibited in the lateral force-resisting system
  “Non-participating” walls must meet minimum prescriptive requirements for horizontal and vertical reinforcement
Notes: This slide is a summary of the seismic design provisions in TMS 402 for SDC D.
In Seismic Design Category D, masonry that is part of the lateral force resisting system must be reinforced so that v + h  0.002, and v and h  0.0007. Type N mortar and masonry cement mortars are prohibited in the lateral force resisting system. Shear walls must meet minimum prescriptive requirements for reinforcement and connections (special reinforced) and other walls must meet minimum prescriptive requirements for horizontal and vertical reinforcement.

## Slide 41: Chapter 7, Seismic Design
Seismic Design Category D:
Extra caution against brittle shear failure for Special Reinforced Masonry Shear Walls (7.3.2.6.1.1):
  Design shear strength shall exceed the shear corresponding to the development of 1.25 times the nominal flexural strength, but
  nominal shear strength need not exceed 2.5 times required shear strength
Notes: This slide is a summary of the seismic design provisions in TMS 402 for SDC D.
Basics of seismic design.

## Slide 42: Minimum Reinforcement for Special Reinforced Shear Walls
roof
diaphragm
roof connectors
@ 48 in. max oc
#4 bar (min) within
16 in. of top of parapet
Top of Parapet
#4 bar (min) @ diaphragms continuous through control joint
#4 bar (min) within 8 in. of all control joints
control joint
Min. #4 bars @ 4 ft oc max. or W1.7 @ 16 in oc
Min. #4 bars @ 4 ft oc max.
#4 bar (min) within 16 in. of corners & ends of walls
24 in. or 40 db past opening
#4 bars around openings
r total both ways = 0.002
Notes: This slide illustrates the minimum reinforcement requirements for special reinforced masonry shear walls.

## Slide 43: Chapter 7, Seismic Design
Seismic Design Categories E and F:
  Additional reinforcement requirements for non-participating stack-bond masonry
Notes: This slide is a summary of the seismic design provisions in TMS 402 for SDC E and F.
In Seismic Design Categories E and F, additional requirements are imposed for stack-bond masonry because it is inherently weaker in flexure across continuous head joints.

## Slide 44: Minimum Reinforcement, SW Types
SW Type | Minimum Reinforcement | Permitted in SDC
Empirically Designed | none | A
Ordinary Plain | none | A, B
Detailed Plain | Vertical reinforcement = #4 at corners, within 16 in. of openings, within 8 in. of movement joints, maximum spacing 10 ft; horizontal reinforcement W1.7 @ 16 in. or #4 in bond beams @ 10 ft | A, B
Ordinary Reinforced | same as above | A, B, C
Intermediate Reinforced | same as above, but vertical reinforcement @ 4 ft | A, B, C
Special Reinforced | same as above, but horizontal reinforcement @ 4 ft, and  ≥ 0.002 (sum of horiz + vert) | A,B,C,D, E, F
Notes: This slide summarizes the requirements for different shear wall types and the Seismic Design Categories in which each type is permitted to be used.

## Slide 45: Organization of TMS 402 Code Chapter 9, Strength Design
Bearing strength
Compressive strength
Modulus of rupture
Strength of reinforcement
Unreinforced masonry
Reinforced masonry
Fundamental basis
Design strength
f factors
Deformation requirements
Anchor bolts
Notes: This slide lists the content in Chapter 9 of TMS 402, Strength Design
Now let’s move to Chapter 9 of TMS 402 dealing with strength design. It is this chapter that first addresses the fundamental basis for strength design.

## Slide 46: Fundamental Basis for Strength Design
Factored design actions must not exceed nominal capacities, reduced by f factors
Load factors come from ASCE7
Quotient of load factor divided by f factor is analogous to safety factor of allowable-stress design, and should be comparable to that safety factor.
Notes: This slide lists fundamental basics for strength design.
Factored design actions must not exceed nominal capacities, reduced by f factors. The quotient of load factor divided by f factor is analogous to safety factor of allowable stress design and should be comparable to that safety factor.

## Slide 47: Code 9.1.4, Strength-reduction Factors (f) for Strength Design
Action | Reinforced Masonry | Unreinforced Masonry
combinations of flexure and axial load | 0.90 | 0.60
shear | 0.80 | 0.80
bearing | 0.60 | 0.60
Notes: The table of this slide summarizes the capacity reduction factors used by TMS 402. For reinforced masonry, they are quite similar to those of ACI 318.

## Slide 48: Code 9.3, Reinforced Masonry
Masonry in flexural tension is cracked
Reinforcing steel is needed to resist tension
Similar to strength design of reinforced concrete
Compressive strength of reinforcement shall be ignored unless the reinforcement is tied in compliance with Code 5.3.1.4
Notes: This slide lists assumptions made for reinforced masonry for TMS 402.
Masonry in flexural tension is considered to be cracked. Flexural tension is to be resisted entirely by reinforcing steel. Design is similar to strength design of reinforced concrete.
The compressive strength of reinforcement is to be ignored unless the reinforcement is tied in compliance with Code 5.3.1.4.

## Slide 49: Code 9.3.2, Design Assumptions
Continuity between reinforcement and grout
Equilibrium
mu = 0.0035 for clay masonry, 0.0025 for concrete masonry
Plane sections remain plane
Elasto-plastic stress-strain curve for reinforcement
Tensile strength of masonry is neglected
Equivalent rectangular compressive stress block in masonry, with a height of 0.80 fm and a depth of a = 0.80 c
Notes: This section lists design assumptions for reinforced masonry per TMS 402.
The basic assumptions of flexural design in reinforced masonry are quite similar to those of reinforced concrete.
Continuity between reinforcement and grout is assumed. Equilibrium must be satisfied. The maximum usable strain is to be taken as mu = 0.0035 for clay masonry and 0.0025 for concrete masonry.
Plane sections are assumed to remain plane. An elastoplastic stress-strain curve is used for for reinforcement; and the tensile strength of masonry is to be neglected.
The compressive stress block is idealized as an equivalent rectangle with a height of 0.80 fm and a depth of 0.80 c.

## Slide 50: Code 9.3.3.5, Maximum Reinforcement (Flexural Ductility Check)
a = 1.5 Ordinary
3 Intermediate
4 Special
mu = 0.0035 clay
0.0025 concrete
C
T
s = y
fy
Reinforcement
0.80 fm
Does not apply if Mu/Vud <1.0 and R ≤1.5
Locate neutral axis based on extreme-fiber strains
Calculate compressive force, C (may include compressive reinforcement)
Tensile reinforcement + axial load = C
Notes: The figure shows the stain distribution and equivalent rectangular stress block for the flexural design of reinforced masonry.
This slide discusses the maximum reinforcement allowed and shows stress and strain distributions over a wall section subject to axial load and flexure.
This slide illustrates the principle behind the maximum reinforcement limitations of Section 9.3.3.5 of TMS 402. Assumed is a critical strain gradient, whose maximum value on the compression side of the element is the maximum useful strain in masonry and whose maximum value on the tension side of the element is a multiple of the specified yield strain in that reinforcement. That multiple depends on the expected flexural ductility demand on the element. In contrast to the calculation of flexural capacity, the contribution of compressive reinforcement can be considered.
That critical gradient defines the location of the neutral axis and the dimensions of the compressive stress block. That, in turn, gives the maximum compressive capacity of that block. The combination of tensile steel area (acting at a stress limited by fy) and axial compression must not exceed that compressive capacity. The intent of this provision is to prevent compressive crushing of that block and, therefore, ensure tension-controlled behavior.

## Slide 51: Code 9.3.4, Nominal Shear Strength
Vn = (Vnm + Vns)gg
Vn shall not exceed:
  Mu / Vu dv  0.25 Vn  6 An  fm
  Mu / Vu dv  1.0 Vn  4 An  fm
  Linear interpolation between these extremes
  Objective is to avoid crushing of diagonal strut
  Objective is to preclude critical (brittle) shear-related failures
gg = 1.0 for fully grouted walls
= 0.75 for partially grouted walls
Notes: This slide shows the equation and limits for nominal shear strength.
Section 9.3.4 of TMS 402 addresses nominal shear strength of reinforced masonry in a way that is quite similar to design of reinforced concrete. Nominal shear resistance is taken as the summation of resistance from masonry, plus resistance from shear reinforcement, multiplied by a gg factor to account for lower tested strength in partially grouted walls. To prevent diagonal crushing of masonry, upper limits are imposed on Vn (and thereby on Vs).

## Slide 52: Code 9.3.4, Nominal Shear Strength
Empirical – from research
(9-25)
(9-24)
Vm and Vs are given by:
Notes: This slide gives the equations for shear strength of the masonry and of the reinforcing steel.
Nominal shear resistance due to masonry depends on the aspect ratio of the element, and varies from 2.25 to 4 times the product of the square root of f’m, and the cross-sectional area of the element.
Nominal shear resistance due to shear reinforcement is computed similarly to reinforced concrete as the product of the number of layers of shear reinforcement crossing a 45-degree crack, the cross-sectional area of each layer of reinforcement, and the specified tensile yield strength of the reinforcement. TMS 402 uses an efficiency factor to account for the fact that shear reinforcement does not yield uniformly over the height of a wall element.

## Slide 53: Code 9.3.5, Design of Walls for Out-of-Plane Loads
Maximum reinforcement by Code 9.3.3.5
Procedures for computing out-of-plane moments and deflections considering secondary effects (P – D) or using a moment magnifier
Note 9.3.5.4.2 – M and D equations are based on simple supports top & bottom. If other support conditions, use appropriate calculations. Don’t treat code as a cook-book!
Notes: This slide lists requirements for design of walls for out of plane loads.
Maximum reinforcement requirements are given by Section 3.3.3.5 of TMS 402. Slenderness effects are addressed (for walls loaded out of plane only) by computing a magnified moment based on computed out-of-plane deflections, or with a magnifier factor based on Euler buckling strength.

## Slide 54: Code 9.3.6, Design of Walls for In-plane Loads
pure flexure
Pn
Mn
pure compression
balance point
Pn max. per
ductility
requirement
Excluded portion
non-ductile
Capacity under combinations of flexure and axial load is based on the assumptions of Code 9.3.2
Interaction diagram:
Notes: This figure shows a basic interaction diagram for masonry. The maximum axial load on the interaction diagram is limited by ductility requirements to be below the balance point.
Flexural design of walls for in-plane loads is again handled using a strength interaction diagram. Because such walls have multiple layers of reinforcement over their depth, hand computations are tedious, and hand approximations (see design example at the end of this module) or computer spreadsheet calculations are preferable.

## Slide 55: NEHRP Recommended Provisions Masonry Design
Simplified Design for Wall-type Structures
Notes: This slide is the introduction slide for simplified design for wall-type structures.
Most practicing engineers are very familiar with the behavior of frame-type structures. Many, however, may never have formally studied the behavior of wall-type structures. For that reason, it is appropriate to review that behavior. The following series of slides presents the basic starting point for design of wall-type structures and their components.

## Slide 56: Essential Function of Walls in Resisting Lateral Forces
Vertical strips of walls perpendicular to lateral forces resist combinations of axial load and out-of-plane moments, and transfer their reactions to horizontal diaphragms
Bond beams transfer reactions from walls to horizontal diaphragms and act as diaphragm chords
Walls parallel to lateral forces act as shear walls
Notes: This slide shows a graphic of a building with horizontal load applied at the roof and distributed to the parallel walls. The perpendicular wall is highlighted for design of out of plane forces.
This slide shows how wall-type structures resist lateral loads.
Vertically spanning strips in the walls oriented perpendicular to the direction of lateral load resist combinations of axial load (from self-weight and roof bearing) and moments from out-of-plane wind.
Reactions from those strips are transferred to horizontal diaphragms that must resist in-plane shears and moments. The load transfer to diaphragms and the in-plane resistance are accomplished with the help of the bond beams that act as diaphragm chords.
The diaphragms, in turn, transfer their reactions to walls oriented parallel to the direction of lateral load, which then act as shear walls.

## Slide 57: Design of Vertical Strips in Perpendicular Walls
M = P e
M = P e / 2
Mwind, eq
~
Moments and axial forces due to combinations of gravity and lateral load
Notes: This slide shows a graphic of a building with horizontal load applied to the roof. Moment diagrams are shown for moment due to eccentricity and for wind or seismic loading.
Vertically spanning strips in walls perpendicular to the direction of lateral load are subjected to axial load and possibly to eccentric gravity load from the roof.
If the strips are assumed to be simply supported at the level of the slab, the moment diagram due to eccentric gravity load varies linearly from its maximum value at the roof, to zero at the slab. These moments must be combined with moments from out-of-plane wind and earthquake forces.
This example shows the effect on the moment diagram due to a parapet and also shows that wind can act in either direction.

## Slide 58: Distribution of Shears to Shear Walls
Classical approach
  Determine whether the diaphragm is “rigid” or “flexible”
  Carry out an appropriate analysis for shears
Notes: This slide shows a graphic of a building with horizontal load applied and a discussion of the distribution of shears to shear walls.
In designing low-rise masonry buildings for lateral load, it is also necessary to compute the distribution of lateral loads to shear walls.
The classic approach is to first determine whether the diaphragm is “rigid” or “flexible” compared to the lateral force resisting system and then to carry out the appropriate analysis for wall shears. In the next few slides, the appropriate analysis for each case is briefly explained.
At the end, however, the designer is encouraged to reduce design effort by simplifying the analysis for each case and finally by bounding the shears from each case.

## Slide 59: Design Flexural Reinforcement as Governed by Out-of-plane Loading
Practical wall thickness is governed by available unit dimensions:
  8- by 8- by 16-in. nominal dimensions is most common
  Specified thickness = 7-5/8 in.
  One curtain of bars, placed in center of grouted cells
Practical wall thickness = 7-5/8 in.
Can have nominal 6” through 12”
Proportion flexural reinforcement to resist out-of- plane wind or earthquake forces
Notes: The next step is to design the flexural reinforcement as governed by out-of-plane loading, which usually will govern over the reinforcement necessary to resist in-plane loading.
The practical wall thickness is governed by available unit dimensions. Using concrete masonry units, nominal dimensions of 8 by 8 by 16 in. are most common. This implies a specified thickness of 7-5/8 in., and a single curtain of reinforcement, placed in the center of grouted cells.
The specified wall thickness is 7-5/8 in.
Proportion flexural reinforcement to resist out-of- plane wind or earthquake forces. Because axial loads are small, the necessary reinforcement can be estimated by dividing the maximum factored design moment from out-of-plane loads by the product of the specified steel yield strength and the internal lever arm.

## Slide 60: Design Flexural Reinforcement as Governed by In-plane Loading
Axial Capacity
Flexural Capacity
Construct moment – axial force interaction diagram
  Initial estimate (more later)
  Computer programs
  Spreadsheets
  Tables
Notes: A simplified axial load-moment interaction diagram for masonry is shown.
The next step is to design flexural reinforcement as governed by in-plane loading. A moment-axial force interaction diagram can be computed by hand or by spreadsheet. As an initial estimate for hand calculations, the approach of Cardenas and Magura can also be used, and is discussed in a few more slides.

## Slide 61: Revise Design as Necessary
If flexural reinforcement required for out-of-plane moments is less than or equal to that required for in-plane moments, no adjustment is necessary. Use the larger amount.
If flexural reinforcement required for out-of-plane moments exceeds that required for in-plane moments, consider making the wall thicker so that in-plane flexural capacity does not have to be increased. Excess in-plane reinforcement increases shear demand.
Notes: This slide lists considerations for revising the design if necessary.
After determining the reinforcement required to resist out-of-plane loads, and the reinforcement required to resist in-plane loads, the greater of the two requirements governs. If out-of-plane requirements considerably exceed in-plane requirements, consider making the wall thicker. In-plane over-capacities in flexure can lead to an unacceptable increase in shear demand if capacity design is used (see subsequent example).

## Slide 62: Check Shear Capacity (1)
shears and moments
corresponding to
probable flexural capacity
shears and moments from factored design loads
WALL
MOMENTS
WALL
SHEARS
M / V
shears and moments corresponding to nominal flexural capacity
Elastic structures or those with considerable shear overstrength:
  Compute factored design shears based on factored design actions.
Inelastic structures:
  Compute design shears based on flexural capacity
Notes: A graphic of wall shears and moments is shown with shears and moments from factored design loads, corresponding to nominal flexural capacity, and corresponding to probably flexural capacity.
In checking shear capacity, the first step is to estimate the design shear.
If the structure is essentially elastic, factored design shears should be computed based on factored design actions.
If the structure is expected to have significant inelastic flexural deformation, then capacity design should be used. Design shears should be computed based on flexural capacity.
In the above figure, the gray diagrams represent shears and moments from factored design loads. The black diagrams represent shears and moments corresponding to nominal flexural capacity. They are the gray diagrams,divided by the capacity reduction factor for flexure. The red diagrams represent the shears and moments corresponding to the probable flexural capacity. They are the black diagrams, multiplied by the ratio of the probable yield strength of the flexural reinforcement divided by the specified yield strength and also multiplied by the ratio of the probable area of reinforcement divided by the required reinforcement.

## Slide 63: Check Shear Capacity (2)
45 o
 Av fy
V
Vn = (Vnm + Vns)gg
Vnm depends on (Mu / Vudv) ratio
Vns = (0.5) Av fy (note efficiency factor when combining Vnm and Vns)
gg = 1.0 for fully grouted walls
Notes: This slide shows a free body diagram of force in the rebar due to horizontal shear is shown.
As discussed previously, shear resistance is calculated similarly to that of reinforced concrete.

## Slide 64: Design Example (1)
Refer to NEHRP Design
Examples (FEMA P-751)
Ch. 13, Masonry
Shear Wall:
Next slide
Notes: The figure shows the exterior end wall elevation of the 5-bay, 1-story example structure. The story height is 28’-0” with a 2’-0” parapet above, for a total building height of 30’-0”. The overall elevation is 100’-0” long. A continuous stem wall and footing are shown below grade. There are 5 door openings spaced evenly across the elevation; the openings are 12’-0” wide and 12’-0” tall. The two end piers are 4’-0” wide and the four interior piers are 8’-0” wide. The wall is labeled 12” masonry.
Slide shows elevation of wall for example problem in P-751.

## Slide 65: Design Example (1)
Refer to NEHRP
Ch. 13, Masonry
Shear Wall
Notes: The figure shows a free body diagram of a single 8’ wide x 12’ tall pier. At the top of the pier the forces are Ptop = 45.1 kips, Vtop = 41.0 kips, and Mtop = 523 ft-kip for axial, shear, and moment respectively. At the bottom of the pier the forces are Rbot = 55.0 kips, Vbot = 43.6 kips, and Mbot = 0 for axial, shear, and moment respectively.
Slide shows a pier of the wall and forces acting on pier.

## Slide 66: Design Example (1)
Trial design: (6) cells w/ (2) #6
Refer to NEHRP
Ch. 13, Masonry
Notes: The figure shows a section through the length of a single pier with the grouted cells filled in. Overall length of the pier is 8’-0” = 96”. Distance ‘d’ from the extreme compression fiber to the outermost steel is 92”. Axial load is distributed uniformly across the length of the wall with the resultant P = (Pf + Pw) acting at the center of the wall length.
Slide shows section of wall with grouted cells and reinforcement.

## Slide 67: Design Example (1)
Refer to NEHRP
Ch. 13, Masonry
Note: a = 4
for Special
Reinforced
Masonry Shear
Wall
Ductility Check
Notes: The figure shows a section through the length of a single pier with the grouted cells filled in as in the previous slide. Overall length of the pier is 8’-0” = 96”. Distance ‘d’ from the extreme compression fiber to the outermost steel is 92”. Axial load is distributed uniformly across the length of the wall with the resultant P = (Pf + Pw) acting at the center of the wall length. A strain diagram is shown below the section with the extreme compressive strain em = 0.0025, and the tensile strain at the steel at the end of the wall 4ey = 0.0083, and a linear strain variation between these two points. The neutral axis (dimension ‘c’) is located 21.3” from the extreme compression face. The strain at the steel along the length of the wall is shown on the strain diagram. The compression strains in the steel in the first two cells are 0.0020 and 0.0011 acting at 17.3” and 9.3” from the neutral axis respectively. The tensile strains in the steel are, in order, 0.0017, 0.0045, 0.0073 and 0.0083 as previously mentioned. The respective distances of the tension steel to the neutral axis are 14.7”, 38.7”, 62.7”, and 70.7”.
Slide shows strain profile on wall section.

## Slide 68: Design Example (1)
Refer to NEHRP Ch. 13, Masonry
Ductility Check (cont.)
Notes: The figure shows two stress diagrams. The first stress diagram shows the masonry compressive stress with a magnitude of 0.8f’m and a length ‘a’ of 17.0”. The resultant force Cm is located 12.8” from the neutral axis. The second stress diagram shows the steel tensile and compressive stresses. The steel stresses are shown for each steel location. Steel stresses in tension and compression are capped at the yield stress of fy = 60 ksi. Stresses Cs1, Cs2, and Ts3 are shown in the linear elastic stress range, while Ts2 and T­s1 are shown at the yield stress.
Slide shows stress profile on wall section.

## Slide 69: Design Example (1)
Refer to NEHRP Ch. 13, Masonry
Ductility Check (continued)
SC > ST + P
Cm + Cs1 + Cs2 > Ts1 + Ts2 + Ts3 + Ts4 + P
315.5 + 53.6 + 28.1 > 52.8 + 52.8 + 52.8 + 43.4 + 45.1
397 kips > 247 kips OK
OK because comp capacity > tension capacity
Notes: Slide shows ductility check calculations.

## Slide 70: Design Example (1)
P = 0 Case
Refer to NEHRP Ch. 13, Masonry
Notes: The figure shows a section through the length of a single pier with the grouted cells filled in as in previous slides. Overall length of the pier is 8’-0” = 96”. Distance from the center of the pier to the outermost steel is 44”. Two stress and strain profiles are shown below the section.
Stress and strain profiles are shown for the P = 0 case. The strain diagram is shown superimposed on the stress diagram with the extreme compressive strain em = 0.0025, and a linear strain variation discontinued below the tensile yield strain of the steel ey = Fy/E = 0.00207. The neutral axis (dimension ‘c’) is located 14.2” from the extreme compression face. The masonry compressive stress is shown with a magnitude of 0.8f’m and a length ‘a’ of 11.3”, with the resultant force Cm acting at 42.35” from the center of the pier. All the steel in tension is shown at yield. Ts4 and Ts3 are 12” on either side of the pier centerline. Ts2 is 36” from the centerline, and Ts1 was previously defined at 44” from the centerline.
Slide shows analysis of section with zero axial load.

## Slide 71: Design Example (1)
Balanced Case
Refer to NEHRP Ch. 13, Masonry
Notes: The figure shows a section through the length of a single pier with the grouted cells filled in as in previous slides. Overall length of the pier is 8’-0” = 96”. Distance from the center of the pier to the outermost steel is 44”.
Stress and strain profiles are shown for the balanced case. The strain diagram is shown superimposed on the stress diagram with the extreme compressive strain em = 0.0025, and a linear strain variation to a maximum tensile strain equal to the tensile yield strain of the steel ey = Fy/E = 0.00207. The neutral axis (dimension ‘c’) is 50.3”, which is 2.3” past the centroid of the pier. The masonry compressive stress is shown in three components, each with a magnitude of 0.8f’m with a total dimension ‘a’ of 40.3”. The first component is for the first two grouted cells over a length of 16” with the resultant force Cm1. The second component is over a length of 16” for the next two cells which are ungrouted with the resultant force Cm2. The third component is for the next grouted cell over a length of 8.3” with the resultant force Cm3. The steel in the first grouted cell is shown at yield stress with resultant Cs1. The steel in the second grouted cell is in the linear elastic range with a resultant Cs2. The steel in the next grouted cell is marked by * and not labeled further. The tension steel in the grouted cell at the end of the pier is at yield with a resultant Ts1. The tension steel in the second grouted cell is in the linear elastic range with a resultant Ts2. The steel in the next grouted cell is marked by * and not labeled further.
Slide shows strain profile under balanced conditions.

## Slide 72: Design Example (1)
Pn = SC - ST = 534 kips
fPn = (0.9)(534) = 481 kips
S Mcl = 0:
Mn = = 23,540 in.-kips
fMn = (0.9)(23,540) = 1,765 ft-kips
Refer to NEHRP Ch. 13, Masonry
Notes: Slide provides calculations for wall axial strength and corresponding flexural strength.

## Slide 73: Design Example (1)
Refer to NEHRP Ch. 13, Masonry
ɸMn
Notes: The figure shows the low-axial load portion of a simplified axial load – moment interaction diagram. The x-axis is fMn with units of ft-kips, and the y-axis is fPn with units of kips. The curve is formed from coordinates (fMn = 988, fPn = 0) and the balance point (fMn = 1765, fPn = 481). fPn max for ductility = 223 kips is shown as a dashed horizontal line. The curve continues above the balance point with decreasing moment capacity with increasing axial load but the curve is cut off. Demands are shown at a moment Mu = 523 ft-kips with axial loads Pu,min = 41 kips and Pu,max = 67 kips. Both points are within the bounds of the interaction curve. A horizontal line is drawn from Pu,max to the curve, where fMn = 1096 ft-kips.
Diagram determining if wall has adequate strength.

## Slide 74: Web sites for more information
BSSC = www.bssconline.org
TMS = www.masonrysociety.org
ACI = www.concrete.org
ASCE / SEI = www.seinstitute.org
MSJC = www.masonrystandards.org
NCMA = www.ncma.org
BIA = www.bia.org
Notes: Further information on the topics presented here is given in these web sites.

## Slide 75: Acknowledgements
This presentation was adapted from material prepared by Prof. Richard E. Klingner, University of Texas at Austin and by Dr. James Harris, J.R. Harris & Co.
Some of the material originally prepared by Prof. Klingner was for a US Army short course.
Some of the material originally prepared by Prof. Klingner was for The Masonry Society and is used with their permission.
The material originally prepared by Dr. Harris was for FEMA, The Building Seismic Safety Council, and the American Society of Civil Engineers.
Notes: This slide shows acknowledgements for the presentation.

## Slide 76: Questions?
Notes: Slide is a questions slide with a graphic of a CGI person sitting on a large question mark.
Slide prompts participants for questions

## Slide 77: DISCLAIMER
NOTICE: Any opinions, findings, conclusions, or recommendations expressed in this publication do not necessarily reflect the views of the Federal Emergency Management Agency. Additionally, neither FEMA nor any of its employees make any warranty, expressed or implied, nor assume any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, product or process included in this publication.
The opinions expressed herein regarding the requirements of the NEHRP Recommended Seismic Provisions, the referenced standards, and the building codes are not to be used for design purposes. Rather the user should consult the jurisdiction’s building official who has the authority to render interpretation of the code.
Any modifications made to the file represent the presenters' opinion only.