## Slide 1: Structural Steel Design
Disclaimer
by Rafael Sabelli, S.E.
Notes: Graphic shows cover of NEHRP document.

## Slide 2: Part 1: Background/Theoretical
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Braced frames
Other topics
Summary
Notes: Table of contents. Note that most of the substance, except the first two items, is taken from the AISC 341 Seismic Provisions for Steel Buildings, which is referenced by the Standard.
Some of the examples in this topic draw heavily on the FEMA 1051 Design Examples CD. Please see this CD for additional details.

## Slide 3: Steel Design: Context in Provisions
Design basis: Strength limit state
Using the 2015 NEHRP Recommended Provisions, Refer to ASCE 7 2016:
  Chap. 11: Seismic Design Criteria
  Chap. 12: Seismic Design Requirements (Buildings)
  Chap. 13: Nonstructural components
  Chap. 14: Design of steel structures
    Refers to AISC Specification (AISC 360-16)
    Refers to AISC Seismic (AISC 341-16)
Notes: The Provisions requirements affect design loads, limit states, and specific details required for members and connections. The bulk of the detailing rules are in the reference documents; the BSSC steel technical committee and the AISC seismic committee have been structured to work very closely together; thus, BSSC’s recommendations are incorporated into AISC Seismic very quickly.

## Slide 4: Seismic Resisting Systems
Unbraced Frames
Connections are:
  Fully Restrained Moment-resisting
  Partially Restrained Moment-resisting
Seismic classes are:
  Special Moment Frames
  Intermediate Moment Frames
  Ordinary Moment Frames
  Systems not specifically detailed for seismic response
Braced Frames
Ordinary Concentric Braced Frames
Special Concentric Braced Frames
Eccentrically Braced Frames
Buckling Restrained Braced Frames
Special Plate Shear Walls
Systems not specifically detailed for seismic response
Notes: Graphic shows frame elevations: gable frame; 10-story moment frame; 4-story eccentrically braced frame; 10-story concentrically braced frame.
Unbraced ("moment resisting") frames resist lateral forces through flexural actions of members framing into (fully or partially) rigidly connected joints. Concentrically braced frames (no moment resisting connections) resist lateral forces through truss action that causes axial forces in members. Eccentric bracing creates high moments and shears in short links intended to yield first. Overall structural deformation in tall buildings: "shear building" pattern for unbraced frame but flexural pattern in braced frame.

## Slide 5: Monotonic Stress-Strain Behavior
Notes: Graphic shows steel stress-strain curve with marked yield point and inelastic range.
Stress-strain diagram for mild steel. Note the elastic range, yield point, plastic range, and region of strain hardening. Define ductility ratio; note values of 100 or more. Compare high- and low-strength steels.

## Slide 6: Plastic Hinge Formation
Plastic hinge in beam
Notes: Graphic shows beam-to-column connection test specimen after flexural test. Yielding of flanges and web is visible as the whitewash has flaked off.
From Modern Steel Construction – Photograph formation of a plastic hinge in a laboratory test of a RBS (reduced beam section) specimen. Yielding may be observed from flaking of whitewash from surface of steel. Very distinctive flange buckling is also visible.

## Slide 7: Behavior Modes For Beams
Moment
Deflection
Mp
Mr
O
M
L
A
I
G
D
J
F
B
C
E
K
H
elastic LTB
inelastic LTB
strain hardening
idealized behavior
Notes: Graphic shows moment-deflection diagram for beams with different governing limit states: lateral-torsional buckling (elastic and inelastic) and flexural yielding with strain hardening. Flexural yielding maintains high flexural strength over a relatively long range of deformation.
Note the various possible limit states (as on slide).
Strain hardening behavior is typical if hinge occurs in a region of significant shear (moment diagram is not constant). This is the typical situation, whereas the constant moment diagram in previous slide is really a laboratory idealization. Mr is the yield moment that includes the effects of residual stress.

## Slide 8: Flexural Ductility of Steel Members - Practical Limits
Lateral torsional buckling
  Provide sufficient lateral or torsional bracing
Local buckling
  Limit width-to-thickness ratios for compression elements
Fracture
  Avoid by proper detailing to allow inelastic strain
Notes: Recall from prior lesson (inelastic behavior) that structural ductility < section ductility < material ductility. Structural ductility of steel members further limited, as noted on slide, by local and lateral torsional buckling.

## Slide 9: Lateral Torsional Buckling
L
u
f
0
Me
My
Mp
D
C
B
A
E
Laterally unbraced length
Resisting moment
inelastic buckling
elastic buckling
buckling with
strain-hardening
Notes: Graphic shows moment capacity versus unbraced length. In the low unbraced length region the moment capacity is high and is governed by flexural yielding followed by local buckling with strain hardening. It decreases with increasing length, governed by inelastic later-atorsional buckling, then by elastic LTB.
Effect of lateral-torsional buckling on moment capacity. Diagram for uniform bending of simple beam. Capacity above Mp due to strain hardening.

## Slide 10: Local Buckling
Substituting  = 0.3 and rearranging:
Classical plate buckling solution:
b
t
Notes: Graphic shows a wide-flange shape with flange half-width b and thickness t denoted.
Example correlates width-to-thickness limits for compression flanges with ductility ratios. The mathematical derivation is not truly correct because linear mechanics are extrapolated beyond the yield level by using strain as a substitute for stress. The point is to show that stability depends on width-to-thickness ratios and that high strains require stubby elements.

## Slide 11: Width-thickness ratios
M
q
Mp
Increasing compactness
(decreasing element slenderness)
Slender elements
Elastic local buckling
Noncompact elements
Inelastic local buckling
Compact elements
Yielding
Highly compact elements
Significant strain
Notes: Graphic shows moment-rotation relationships for cross sections of different compactness. Slender elements achieve low rotation before losing strength. Flexural strength and rotation capacity increase with compactness. Both compact and highly compact sections achieve the full flexural strength, but the more compact shapes undergo greater rotation before losing strength.

## Slide 12: Restraint
Example:
Beam flange to (thick) column flange T joint
Highly restrained
Notes: Graphic shows a diagram of a T joint with a CJP weld, and a photograph of a beam-flange-to-column-flange welded joint.
Highly restrained conditions do not allow strain transverse to the direction of loading. Thus transverse stress occurs as the result of Poisson’s effect, and the steel material may not yield. Rather, the stress may continue to increase and rupture may occur at very low strain.

## Slide 13: Toughness and energy absorption
  Ductile yielding (or even achieving full strength) can be precluded by failure of low-toughness material
Minimum toughness is required for seismic design at critical locations
X
Displacement
Load
Low toughness
High toughness
X
Notes: Graphic shows a load-displacement diagram for both low-toughness and high-toughness material. The low-toughness material ruptures at a low displacement. The high-toughness material achieves larger displacement and inelastic displacement.

## Slide 14: The “k region”
Welds to this region are proscribed in seismic design
Rotary straightening of flanges strain-ages this area of the web, leading to reduced toughness.
Welds in this area have led to fracture during fabrication.
Notes: Graphic shows the K region of the beam web inside of the radiused fillet web-to-flange transition.

## Slide 15: Variability and predictability
Liu et al.
Specified minimum yield
Measured yield
Notes: Graphic shows yield strength of multiple test specimens graphed as a function of their b/t ratios. The graph shows substantial scatter, with generally higher strength for lower b/t.

## Slide 16: Expected strength
RyFy
Expected (mean) yield strength for material
NOT maximum yield strength
Determined by AISC using industry-wide data

## Slide 17: Welded Beam to Column Laboratory Test - 1960s
Notes: Graphic shows beam-to-column connection diagram with welded top and bottom plates, and moment-displacement diagram with the hysteresis somewhat similar to a parallelogram, but with a curved transition from elastic to yielding.
Load-deflection diagram for repeated reversed loads on welded joints performed under laboratory conditions in late 1960s and early 1970s. It shows relative stability of connection and its large capacity to absorb energy. Tests of joints with welded flanges and bolted webs showed similar stability and essentially same capacity. Northridge earthquake and subsequent laboratory testing have shown serious problems with particular welded joints. It turns out that it is somewhat difficult to actually achieve the behavior represented on this diagram.

## Slide 18: Pre-Northridge Standard
Notes: Graphic shows beam-to-column connection diagram with welded top and bottom flanges and a bolted single-plate connection at the web. Notes indicate the column to be stronger than the beam in flexure, and continuity plates if required. Backing is shown at flange welds.
The Northridge earthquake revealed serious flaws in the performance of welded joints in steel moment frames. The drawing illustrates the particular detail that had received prescriptive acceptance for seismic-resistant design in the decade prior to Northridge. The only real variable was the weld from the shear tab to the beam web, which was required in beams in which the web represented more than 30% of the plastic flexural capacity.

## Slide 19: Backing
Backing used to support and retain molten filler metal
Backing – also called “weld backing,” “backing bars,” “back-up bars”, and “backing strips”
Fusible backing– weld is intended to bond to backing (e.g. steel backing)
Non-fusible backing– weld not intended to bond to backing (e.g. ceramic and copper)
Notes: Graphic shows detail of steel backing at a complete joint penetration groove weld with multiple weld passes.

## Slide 20: Northridge Failure
Column
flange
Backup bar
Beam flange
and web
Notes: The photo shows a cut and polished specimen with a crack at the fusion line between the weld and the column flange. Note that the backup bar is not attached to the column flange, which creates a notch normal to the stress in the flange. The section is cut at the centerline of the beam; thus, the beam web beyond the weld access hole appears as the upward curving line at the right. Note that at the instant the beam flange is in tension due to lateral sway, the column flange at the weld is also likely to be in tension.

## Slide 21: Northridge Failure
Following the 1994 Northridge earthquake, numerous failures of steel beam-to-column moment connections were identified. This led to a multiyear, multimillion dollar FEMA-funded problem-focused study undertaken by the SAC Joint Venture. The failures caused a fundamental rethinking of the design of seismic resistant steel moment connections.
Notes: The photograph shows a fracture resulting in a divot being removed from the column flange adjacent to the toe of the full penetration weld at the beam flange.

## Slide 22: Northridge Failures
Lamellar Tear
Heat Affected Zone
Column Flange
Column Divot
Weld Fusion
Weld
Notes: Graphics: 6 diagrams show fractures at beam bottom-flange to column-flange welded joints.
Weld: fracture is through weld material.
Weld fusion: Fracture is at weld-column boundary.
Column divot: fracture is within column flange, going from the bottom of the weld and above the joint.
Column flange: fracture is across column flange.
Heat affected zone: fracture is across beam flange.
Lamellar tear: fracture is within column flange, but extending above and below the joint.
The figures are abstracted from Interim Guidelines: Evaluation, Repair, Modification and Design of Welded Steel Moment Frame Structures, the early SAC report (95-02) on the problems found at Northridge. It is also available as FEMA 267, August 1995. The majority of the cracks began at the root of the weld directly above the notch at the end of the backup bar. Subsequent investigation determined that significant cracks exist in such joints that have not been exposed to seismic ground motion -- due to a combination of restraint of weld shrinkage, a ready-made notch, use of materials that are not “notch tough,” difficulties in inspection at the point in question, and other factors.

## Slide 23: Flexural Mechanics at a Joint
1
2
1
2
Beam Moment
Fw
Fy
2
1
1
2
Cross Sections
Fw
Fy
Notes: Graphics show:
Beam-column frame with beam section at column face (1) and slightly further from column face (2).
Bema moment diagram with high moment at section 1 and lower at section 2.
Cross section 1 is only the flanges; cross section 2 is the full wide-flange shape.
Section 1 has high stress at flanges. Section 2 has stress distribution across entire section, with yielding at the flanges.
One of the inherent weaknesses of the joint is that the flange welds must be strong enough to develop substantial yielding in the beam away from the flange in order to dissipate significant energy. The plastic section modulus is less at the welds and the gradient in the moment as one moves away from the column flange both combine to require that the ultimate strength of the weld be substantially more than the yield of the beam. Another factor is that most available beams now have yield strengths of about 50 ksi (even though sold under A36 specification) whereas the tests done at the time the joint was developed were made on material much closer to 36 ksi yield; the strength of weld metal has not changed in the same fashion.

## Slide 24: Welded Steel Frames
Northridge showed serious flaws. Problems correlated with:
  - Weld material, detail concept and workmanship
  Beam yield strength and size
  Panel zone yield
Repairs and new design
  Move yield away from column face (cover plates, haunches, reduced beam section)
  - Verify through tests
SAC Project: FEMA Publications 350 through 354
AISC 358
Notes: The slide summarizes the major points learned in the first phase of the SAC project (a FEMA-funded joint venture of SEAOC, ATC, and CUREE, which is California Universities for Earthquake Engineering). The second phase of the SAC project, also funded by FEMA, was a very substantial undertaking, and much more was learned. The profession and the steel industry will continue to feel profound effects of the Northridge event for years to come. For the reduced beam section (RBS) the beam flange width is reduced (by cutting) at a point away from the column face in order to force first yield at that point.

## Slide 25: Reduced Beam Section (RBS) Test Specimen SAC Joint Venture
Graphics courtesy of Professor Chia-Ming Uang, University of California San Diego
Notes: A beam-to-column joint test that utilizes the reduced beam section (RBS) detail is shown in the photograph. The experimental hysteresis plot is also shown. The RBS detail has been recognized as a pre-qualified connection in FEMA 350 and subsequent AISC documents. The behavior of this connection (actually member) detail is ductile and forces the inelasticity to occur in the beam section away from the beam-to-column welding and bolting. Graphics courtesy of Professor Chia-Ming Uang, University of California San Diego.

## Slide 26: Extended Moment End-Plate Connection Results
Photo courtesy of Professor Thomas Murray, Virginia Tech
Notes: Photo is of a laboratory test specimen of an extended moment end-plate connection. Beam flanges have buckled. The “thick plate” behavior results in the development of a plastic hinge at the end of the stiffened section of the beam as the significant local flange and web buckling illustrate. The photograph is courtesy of Professor Thomas Murray, Virginia Tech.

## Slide 27: Ductility of Steel Frame Joints
Welded Joints
  Brittle fracture of weld
  Lamellar tearing of base metal
  Joint design, testing, and inspection
Bolted Joints
  Fracture at net cross-section
  Excessive slip
Joint Too Weak For Member
  Shear in joint panel
Limit States
Notes: Other failures not on slide were due to crushing or buckling of column web, distortion of column flange, or panel zone shear yielding or buckling.

## Slide 28: Multistory Frame Laboratory Test
Notes: Graphic shows elevation of frame with vertical loads indicated, as well as induced horizontal rotation. Hysteresis shows parallelogram behavior.
Load deflection plot for three-story, single-bay frame test. Heavier axial loads would limit stability at large lateral deflections.

## Slide 29: Axial Strut Laboratory test
Notes: Plot of axial load versus axial deflection. The hysteretic shape is complicated and shows significant degradation on the compression side. On the tension side some degradation is also apparent, and larger displacements occur at each cycle.
Plot representative of column or brace. Plot of axial load versus axial deflection for low-to-medium slenderness member (L/r = 45). Tension in upper right quadrant and compression in lower left. Theoretical buckling load reached on only the first cycle. Note the degrading stiffness, decreasing compressive strength, and permanent set caused by tension yielding. Other testing has shown prevention of local buckling is crucial to maintaining any post-buckling strength.

## Slide 30: Cross Braced Frame Laboratory test
Notes: Graphic shows frame force-displacement behavior with significant pinching and larger displacements required at each cycle to achieve the full strength.
Overall performance of concentrically braced frame governed by axial behavior of braces. Frame has braces in both directions. Fatness of loops depends on slenderness of bracing members; lower slenderness ratios give fatter loops. Note the degrading stiffness.

## Slide 31: Eccentrically Braced Frame Lab test of link
Notes: Yield in eccentrically braced frames occurs in link (short portion of beam between braces). Shear yielding produces very fat and stable hysteresis loops. Braces, beams, and columns designed to remain elastic at load level that causes link yielding.

## Slide 32: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Notes: Table of contents: Reference standards and design strength. The Provisions references commonly accepted codes for each material and indicates how requirements in those standards must be modified for use with the NEHRP Recommended Provisions seismic design procedure. Special additional provisions are also included in each materials chapter.

## Slide 33: Steel Design Specifications
AISC 341:
Seismic Design Provisions for Structural Steel Buildings
AISC 360:
Specification for Structural Steel Buildings
Notes: Graphic shows covers of the AISC Steel Construction Manual and Seismic Design Manual.
The referenced standard for structural steel (hot rolled shapes and plates, and sections built up from hot rolled shapes and plates) is the Specification for Structural Steel Buildings, (2016). The specification governing seismic design of steel buildings is Seismic Provisions for Structural Steel Buildings.
The pictured copies are the Manuals using the 2010 Specification and Seismic Provisions, as the Manuals based on the 2016 editions will not be available in print until 2017 and 2018.

## Slide 34: Using Reference Standards Structural Steel
Both the AISC LRFD and ASD methodologies are presented in a unified format in both the Specification for Structural Steel Buildings and the Seismic Provisions for Structural Steel Buildings.
Notes: Slide discusses reference standards.

## Slide 35: Cold Formed Steel Standard
Notes: Graphic shows cover of AISI North American Specification for the Design of Cold-formed Steel Structural Members .
Reference standard for cold formed steel is the AISI North American Specification for the Design of Cold-formed Steel Structural Members (shown on slide). It includes both ASD and LRFD.

## Slide 36: Other Steel Members
Steel Joist Institute
  Standard Specifications, 2010
Steel Cables
  ASCE 19-2010
Steel Deck Institute
  Diaphragm Design Manual, DDM04, 2015
Notes: For design of other specialized steel members, the Provisions refers user to standards published by Steel Joist Institute and the ASCE 19 standard for cables. The Provisions indicates how SJI allowables should be increased to maximum strengths for use in seismic resistant design and give guidelines for modification of cable allowables. Note the Steel Deck Institute’s Diaphragm Design Manual is no longer referenced in the Provisions although it is a good source (do not use the 2.75 “factor of safety”). There are also other sources for steel deck diaphragms.

## Slide 37: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Notes: Table of contents: Moment resisting frames.

## Slide 38: Steel Moment Frame Requirements
Notes: i is shorthand for the total (elastic plus inelastic) rotation at the beam-to-column connection. Elastic drift at yield is on the order of 0.01 radians. The capacity is very sensitive to detail; thus, the requirement for testing representative joints. AISC Seismic includes an appendix with a testing protocol.

## Slide 39: Moment frames
Fuses
Encourage
Avoid
Encourage
  Flexural hinging in beams
Avoid
  Flexural hinging in columns
    (occurs at base)
  Connection failure
  Excessive column panel-zone yielding
Notes: Graphic shows:
Diagram of moment frame with plastic hinges in beams at every level.
Diagram of moment frame with plastic hinges in columns at the top and bottom of the first level.

## Slide 40: Panel Zones
Special and intermediate moment frame:
Shear strength demand:
  1.1 to 1.4RyMp of beams
  Thickness (for buckling)
  Use of doubler plates
  (not economical, try to increase col. size instead)
Notes: Graphic shows:
Beam-column connection with beam moments acting on column shown.
Panel shear often controls, and this may require larger column or "doubler" plate on web, which is expensive to fabricate. SAC testing has shown that panel zone yield contributes to fracture of beam flange welds, apparently due to the concentration of strains at that location. However, some yielding in the panel zone is considered to be a good way to dissipate energy. The final SAC recommendations require that the yield strength of the shear panel zone be at least strong enough to reach the beginning of yield in the beam flexural hinge areas but not full development of the flexural hinge.

## Slide 41: Steel Moment Frames
Beam shear: 1.15RyMp + gravity
Beam local buckling
  Smaller b/t than for plastic design
Continuity plates for smaller columns
Strong column - weak beam rule
  Prevent column yield except in panel zone
  Exceptions: Low axial load, strong stories, top story, and non-SFRS columns
Notes: Note the tighter restrictions on b/t and h/t than required for plastic design. Beam flange continuity plates are now required if included in the test specimens. It is not an analytical check. The b/t limit rules out a few common beam shapes for grade 50 steel.

## Slide 42: Steel Moment Frames
Lateral support of column flange requirements
  Top of beam if column elastic
  Top and bottom of beam otherwise
  Amplified forces for unrestrained
Lateral support of beams requirements
  Both flanges
  Spacing < 0.095ryE/RyFy
Notes: Limits to prevent member buckling. The limit is for special frames and it is different from the general limits in the main spec, which applies to the compression flange and depends on the square root of Fy. The Commentary to the AISC 341 includes the following:
“Spacing of lateral braces for beams in SMF systems is specified not to exceed 0.086 ry E / Fy. This limitation, which is unchanged from previous editions, was originally based on an examination of lateral bracing requirements from early work on plastic design and based on limited experimental data on beams subject to cyclic loading. Lateral bracing requirements for SMF beams have since been investigated in greater detail in Nakashima, Kanao and Liu (2002). This study indicates that a beam lateral support spacing of 0.086ryE/Fy is appropriate, and slightly conservative, to achieve an interstory drift angle of 0.04 radian.”

## Slide 43: Prequalified Connections
ANSI/AISC 358, Prequalified Connections for Special and Intermediate Steel Moment Frames for Seismic Applications
  Reduced Beam Section Connections
  Bolted Stiffened and Unstiffened Extended Moment End Plate Connections
  Bolted Flange Plate
  Welded Unreinforced Flange-Welded Web (WUF-W)
  Kaiser Bolted Bracket
  CONXL
Notes: FEMA 350 resulted from the SAC Joint Venture project. Subsequently, an ANSI/AISC committee was established to create ANSI/AISC 358. The work by this committee is continuing and additional connections are being addressed. The ANSI/AISC 358 standard is available for download from the AISC website.

## Slide 44: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Seismic design category requirement
Moment resisting frames
Braced frames
Notes: Table of Contents: braced frames.

## Slide 45: Concentrically Braced Frames Basic Configurations
K
V
(Chevron)
Inverted V
(Chevron)
K
Diagonal
X
Notes: Graphic shows:
Six frames with different brace configurations.
K bracing will introduce bending into columns following buckling of compression brace and is often prohibited. V and inverted V bracing require continuity of beams.

## Slide 46: Concentrically Braced Frames
Special AISC Seismic R = 6
AISC 341 Section F2
Ordinary AISC Seismic R = 3.25
AISC 341 Section F1
Not Detailed for Seismic R = 3
AISC 360
Notes: The special and ordinary systems are similar. Chapter F.1 and Chapter F.2 refer to sections AISC 341.

## Slide 47: Concentrically braced frames
Fuses
Encourage
  Yielding of braces
  Buckling of braces
Avoid
  Flexural hinging in columns (story mechanisms)
  Buckling of beams or columns
  Connection failure
Notes: Graphic shows concentrically braced frames:
With braces at all levels buckling or yielding;
With braces buckling or yielding at the first level only and columns with plastic hinges at that level;
With column buckling at the first level; and
With brace connections fracturing at the first level and columns with plastic hinges at that level;

## Slide 48: Eccentrically Braced Frames
Link
Brace
Beam
Notes: Graphic shows eccentrically braced frames, with braces, beams and links identified.
Eccentrically braced frames. Define terms.

## Slide 49: Eccentrically braced frames
Fuses
Encourage
  Yielding of link
Avoid
  Flexural hinging in columns (story mechanisms)
  Buckling of braces, beams or columns
  Connection failure
Notes: Graphic shows eccentrically braced frames:
With links at all levels yielding;
With link yielding at the first level only and columns with plastic hinges at that level;
With column buckling at the first level; and
With brace connections fracturing at the first level and columns with plastic hinges at that level;

## Slide 50: Buckling-Restrained Braced Frames (BRBFs)
Type of concentrically braced frame
Beams, columns and braces arranged to form a vertical truss. Resist lateral earthquake forces by truss action
Special type of brace members used: Buckling-Restrained Braces (BRBs). BRBS yield both in tension and compression - no buckling !!
Develop ductility through inelastic action (cyclic tension and compression yielding) in BRBs.
System combines high stiffness with high ductility
Notes: BRBFs are concentrically braced frames, consisting of beams, columns and braces arranged to form a truss. BRBFs resist lateral load primarily through truss action, with member response dominated by axial force (tension and compression).
Unlike conventional concentrically braced frames, BRBFs are constructed with a special type of brace member: Buckling-Restrained Braces (BRBs).
BRBs have the unique quality that they do not buckle when loaded in compression. Consequently, BRBs yield in a ductile manner in both tension and compression. The use of BRBs results in a frame that combines high elastic stiffness with excellent ductility.
BRBFs are considered to be a high ductility framing system, and is assigned high R-factors in ASCE-7.
Per ASCE-7, the R-factors for BRBFs are: R=7 for BRBF with non-moment resisting beam-to-column connections.
R=8 for BRBF with moment resisting beam-to-column connections.
These are the same as the R-factors assigned to EBFs.

## Slide 51: Buckling-Restrained Braced Frames (BRBFs)
Steel Core
Casing
Buckling- Restrained Brace: Steel Core + Casing
Notes: Graphic shows:
Buckling-restrained brace assembly diagram;
Casing; and
Steel core.
The key feature of a BRBF is the use of Buckling-Restrained Braces (BRBs).
A BRB consists of a steel core and a casing. The casing covers the steel core.

## Slide 52: Bracing Configurations for BRBFs
Two Story X- Bracing
V- Bracing
X- Bracing
Inverted V- Bracing
Single Diagonal
Notes: Graphic shows five frame elevations:
Single diagonal; Inverted V- Bracing; V- Bracing; X- Bracing, and 2-story X- Bracing. X bracing is barred.
Various bracing arrangements are possible for BRBFs, as is the case with conventional braced frames.
Single story X-bracing is generally not possible for BRBFs because of the difficulty in crossing the two BRBs at their centers. Also, K-braced BRBFs are not permitted (see Section F4.4).

## Slide 53: Buckling restrained braced frames
Fuses
Encourage
  Yielding of braces
Avoid
  Flexural hinging in columns (story mechanisms)
  Buckling of beams or columns
  Connection failure
Notes: Graphic shows buckling-restrained braced frames:
With braces at all levels yielding;
With braces yielding at the first level only and columns with plastic hinges at that level;
With column buckling at the first level; and
With brace connections fracturing at the first level and columns with plastic hinges at that level;

## Slide 54: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Braced frames
Other topics
Notes: Table of contents: other topics.

## Slide 55: Special Truss Moment Frame
Buckling and yielding in special section
Design to be elastic outside special section
Deforms similar to EBF
Special panels to be symmetric X or Vierendeel
Notes: Graphic shows elevation of Special truss moment frame. Bay length (L), length of special segment (Ls), and length of panel (Lp) are indicated.
Special truss moment frames are a new introduction to seismic resistant construction. The concept is that a set of panels near midspan of horizontal trusses, where the gravity load shear is low, are design to yield and buckle in a controlled manner to dissipate energy of strong ground shaking. It should be anticipated that the bucked members may have to be replaced following strong ground shaking.

## Slide 56: Special Truss Moment Frame
Notes: Two photos of special truss moment frame experimental test specimen. Special segments have cross-braced panels.
This specimen was part of a research program at the University of Michigan under the direction of Professor Subash Goel. This research led to the inclusion of the STMF as a recognized structural system in the NEHRP Recommended Provisions. Photo courtesy of Nucor Research and Development.

## Slide 57: General Seismic Detailing
Materials:
  Limit to lower strengths and higher ductilities
Bolted Joints:
  Fully tensioned high strength bolts
  Class-A (or better) faying surface)
  Limit on bearing
Notes: Seismic detailing per AISC Seismic is more than simply the rules for the specific systems. There are also general rules for several subjects that apply to all types of steel seismic resisting systems.

## Slide 58: General Seismic Detailing
Welded Joints:
  AWS requirements for welding procedure specs
  Filler metal toughness
    CVN > 20 ft-lb @ 0°F
  Warning on discontinuities, tack welds, run offs, gouges, etc.
Columns:
  Strength using o
  Splices: Requirements on partial penetration welds and fillet welds
Notes: The requirements for weld metal toughness are new. The reference to AWS welding procedure specs is a new emphasis. It is likely that structural engineers will have to become more well educated about welding in the future. The rules on columns are intended to prevent premature failure in these vulnerable components.

## Slide 59: Qn = 0.5 Asc ( fc’ Ec)1/2  Rg Rp Asc Fu Rg = stud group adjustment factor
*0.85 if wr /hr < 1.5
Rg = 0.7
Rg = 0.85
Rg = 1.0*
Rg = 1.0
  Shear Studs
  Group Adjustment Factor
Notes: Graphics show:
Beam with single stud through deck (flutes transverse to beam axis).
Beam with single stud through deck (flutes parallel to beam axis).
Beam with two studs through deck (flutes transverse to beam axis).
Beam with three studs through deck (flutes transverse to beam axis).
This slide illustrates the application of the group adjustment factor, Rg. The first, third, and fourth figures illustrate “beam” applications – that is the deck is perpendicular to the steel section. The second figure illustrates a “girder” for which the deck is parallel to the steel section. A narrow rib in the girder application, as defined by the wr /hr ratio being less than 1.5, results in a reduction in Rg to a value of 0.85.

## Slide 60: Quality and Welding
AISC 341
  Appendix Q
    Basic Quality Assurance Plan
    Inspection tables
      Welding
      Bolting
  Appendix W
    Welding quality
      Details
      Inspection

## Slide 61: Quality and Welding
AISC 341
  Addresses:
    Quality Control - Fabricator/Erector
    Quality Assurance - Owner
    Non-Destructive Testing
  Uses:
    Observe and Perform (AISC Seismic Provisions)

## Slide 62: Inspection and Testing Shop Certification
Domestic:
  AISC
  Local jurisdictions
Foreign:
  No established international criteria
Notes: AISC can certify fabricating shops. Program includes scheduled and surprise inspections to review quality control procedures, personnel, and results. Some local jurisdictions have adopted similar certification procedures. As there is no internationally accepted quality certification, foreign fabricated steel should be given close inspection.

## Slide 63: Chapter 9: Structural Steel Design
Part 2: Design Examples

## Slide 64: Chapter 9: Structural Steel Design
Part 2: Design Examples:
Special Moment Frame

## Slide 65: Special Moment Frames Seven Story Office Building, Los Angeles
Perimeter Moment Frames, all bays engaged
SDS=1.0
SD1=0.6
Occupancy Category II
Seismic Design Category D
Design Parameters (Table 12.2-1)
  R=8
  Cd=5.5
  W0=3.0
Notes: The information on the following several slides are taken from Example 6.2 (Alternate A) of the NEHRP Design Examples volume (FEMA 1051). FEMA 1051 was written based on the 2015 NEHRP Recommended Provisions. The example complies with the AISC 341.

## Slide 66: Special Moment Frame Example
Structural Materials:
  Concrete (all floors) = 3.0 ksi lightweight
  Other Concrete = 4.0 ksi normal weight
Steel:
  Wide Flange Sections= ASTM A992 Grade 50
  HSS= ASTM A500 Grade B
  Plates= ASTM A36
Notes: Structural Materials

## Slide 67: Special Moment Frames Plan of Building
Notes: Graphic shows: a full floor plan of the building. There are seven bays in the E-W direction and five bays in the N-S direction. The design is illustrated for loads acting in the E-W direction.

## Slide 68: Special Moment Frames Elevation of Building
Notes: Graphic shows: an elevation showing the North face of the building. There are seven full stories, plus a partial penthouse.

## Slide 69: Special Moment Frames Perimeter Moment Frames with RBS
System Designed
Reduced Beam Section
Notes: Graphic shows:
Detail of reduced beam flange.
Plan diagram of building with moment frames on 4 perimeter lines. Line 6 is highlighted showing that is the frame designed in the example.
The perimeter special moment frames are shown on this diagram. The seven-bay frame that acts in the E-W direction is designed in this example.

## Slide 70: Special Moment Frames
The following design steps will be reviewed:
Compute Lateral Loads
Select preliminary member sizes
Check member local stability
Check deflection and drift
Check torsional amplification
Check the column-beam moment ratio rule
Check shear requirement at panel zone
Select connection configuration
Notes: The design steps in this slide will be briefly reviewed in the subsequent slides. Additional explanation and detail is available in the FEMA 1051. A portion of the East-West frame at level two will be used to illustrate various calculations.

## Slide 71: Special Moment Frames
Building Weight:
Penthouse Roof = 94 kips
Lower Roof = 1,537 kips
Typical Floor = 1,920 kips
Total = 94 + 1,537 + 6(1,920) = 13,151 kips
Building Period:
Ta=Cthnx =(0.028) (102.3)0.8 = 1.14 sec.
T=CuTa = (1.4)(1.14)=1.596 sec. Design Base Shear:
Cs=SD1/(T/(R/I)=0.6/(1.596/(8/1))=0.047 <<< CONTROLS
Cs,min = 0.044 SDSI=0.044(1.0)(1)=0.044
V=CsW=0.047(13,151)=618 kips.
Notes: Building weights are given for the entire building.

## Slide 72: Special Moment Frames
Select preliminary member sizes – The preliminary member sizes are given in the next slide for the frame in the East-West direction. These members were selected based on the use of a 3-Dimensional model analyzed using the program ETABS. As will be discussed in a subsequent slide, the drift requirements controlled the design of these members.
Notes: Checking preliminary sizes for special moment frames.

## Slide 73: SMF Example – Preliminary Member Sizes
Notes: Graphic shows:
Elevation of frame on line 6 with column and beam member sizes (preliminary).
The preliminary member sizes were determined from the use of a structural analysis model and were based on satisfying the drift limits for this design. FEMA 1051 indicates that the drift requirements govern over the strength requirements, which is often the case for SMF designs.
Note that this example is based on Chapter 6.2 of the FEMA 1051 Examples document.

## Slide 74: SMF Example – Check Member Local Stability
bf
tf
tw
hc
OK
Upper limit:
Check beam web:
OK
Upper limit:
Check beam flange:
(W33x141 A992)
Notes: Graphic shows a wide-flange shape with flange half-width b and thickness t denoted, and the web height (hc) and thickness (tw).
The beam flange local stability limits are prescribed in the AISC Seismic specification, which is more stringent for the W shape in the SMF application. The web local stability limits are prescribed in the AISC Specification for Structural Steel Buildings. The column check is similar. Note that the provision for checking the web slenderness under combined bending and compression no longer appears in the AISC Specification for Structural Steel Buildings.

## Slide 75: SMF Example – RBS Details
c=0.20bf
b=0.75db
a=0.625bf
Notes: Graphic shows a detail of the reduced beam flange with dimensions indicated:
a distance of beginning of cut from column face
b length of cut
c width of cut on each side
The Reduced Beam Section details are shown in this slide.

## Slide 76: SMF Example – Check Deflection and Drift
Therefore, there is no vertical irregularity.
The frame was checked for an allowable story drift limit of 0.020hsx. All stories in the building met the limit. Note that the NEHRP Recommended Provisions Sec. 4.3.2.3 requires the following check for vertical irregularity:
Notes: Calculation showing drift check.

## Slide 77: SMF Example – Check Deflection and Drift
Building Satisfies Drift Limits
 | Elastic Displacement at Building Corner, From Analysis |  | Expected Displacement (=δeCd) |  | Design Story Drift Ratio |  | Allowable Story Drift Ratio
Level | de E-W (in.) | de N-S (in.) | d E-W (in.) | d N-S (in.) | D E-W/h (%) | D N-S/h (%) | D/h (%)
Level 7 | 2.92 | 3.18 | 16.0 | 17.5 | 1.2 | 1.2 | 2.0
Level 6 | 2.66 | 2.89 | 14.7 | 15.9 | 1.4 | 1.7 | 2.0
Level 5 | 2.33 | 2.47 | 12.8 | 13.6 | 1.6 | 2.0 | 2.0
Level 4 | 1.91 | 1.95 | 10.5 | 10.7 | 1.9 | 2.0 | 2.0
Level 3 | 1.41 | 1.40 | 7.76 | 7.70 | 1.8 | 1.8 | 2.0
Level 2 | 0.90 | 0.88 | 4.96 | 4.85 | 1.2 | 1.2 | 2.0
Level 1 | 0.55 | 0.52 | 3.04 | 2.89 | 1.1 | 1.1 | 2.0
1.0 in. = 25.4 mm. |  |  |  |  |  |  | 
Table 9.2-1 Alternative A (Moment Frame) Story Drifts under Seismic Loads
Notes: Calculation showing drift check. Note that drifts are checked at the building corners, although this is not required for a torsionally regular building. P-Delta effects are directly included in the computations.

## Slide 78: SMF Example – Check Torsional Amplification
The 3D analysis results, as shown in FEMA P-1051, indicate that none of the max / avg ratios exceed 1.2; therefore, torsional amplification is not required.
The torsional amplification factor is given below. If Ax < 1.0 then torsional amplification is not required. From the expression it is apparent that if max / avg is less than 1.2, then torsional amplification will not be required.
Notes: The torsional amplification equation given in the slide is described FEMA 1051. As noted, the structural analysis results indicate that torsional amplification need not be considered in this design. This is not surprising given the regularity (symmetry) of the floors and frames (placed around the perimeter.) The same regular and symmetrical building with braced frames in the core (and no moment frames) falls into the “extreme torsional irregularity” category.

## Slide 79: SMF Example – Member Design NEHRP Guide
Column Design Considerations - Columns must be adequate for:
  Combined bending and axial under basic load combinations
  Axial only under overstrength load combinations
The frame in this example is controlled by drift. So, with both strength and drift requirements satisfied, we will check the column-beam moment ratio and the panel zone shear.
Notes: The content of this slide is taken directly from FEMA 1051.

## Slide 80: SMF Example – Column-Beam Moment Ratio
where M*pc = the sum of the moments in the column above and below the joint at the intersection of the beam and column centerlines. ΣM*pc is determined by summing the projections of the nominal flexural strengths of the columns above and below the
joint to the beam centerline with a reduction for the axial force in the column.
M*pb = the sum of the moments in the beams at the intersection of the beam and column centerlines.
Per AISC Seismic Sec. E3.4a
Notes: It is permitted to take ΣM*pc = ΣZc(Fyc-Puc/Ag) (LRFD). ΣM*pb is determined by summing the projections of the expected flexural strengths of the beams at the plastic hinge locations to the column centerline. It is permitted to take ΣM*pb = Σ(1.1RyFybZb+Muv). Refer to AISC Seismic specification Sec. E3.4a for remainder of definitions.

## Slide 81: SMF Example – Column-Beam Moment Ratio
Column – W24x146; beam – W21x73
Notes: The story height for the first story is 268 in. (top of concrete to mid-depth of first floor beam and the clear height is 251.35 in. The values for the second story are 160 in. and 128.44 in. For diagrams and additional details the reader is referred to FEMA 1051 and the AISC Seismic specification.

## Slide 82: SMF Example – Column-Beam Moment Ratio
where
Mpr=CprRyFy Ze
Ze = effective Z (RBS)
Ve= 2 Mpr / L’
Sh= dist. from col. centerline to plastic hinge
For beams:
Notes: Graphic shows a free-body diagram of the beam segment between plastic hinge locations. Forces acting on the beam are:
W Distributed gravity load
Vp Shear force at each end
Mp Moments at each end
Segment length is L’
Calculations for Vp. Figure from FEMA 1051. The calculation for the factored uniform dead load, w, is given and is found to be 1.406 klf.

## Slide 83: SMF Example – Column-Beam Moment Ratio
Other ratios are also computed to be greater than 1.0
The ratio of column moment strengths to beam moment strengths is computed as:
Notes: The column-beam strength ratio for all the other stories are determined in a similar manner.

## Slide 84: SMF Example – Panel Zone Check
The AISC specification is used to check the panel zone strength. From analysis shown in the NEHRP Design Examples volume (FEMA 451), the factored strength that the panel zone at Story 2 of the frame in the EW direction must resist is 794 kips. The shear transmitted to the joint from the story above, Vc, opposes the direction of Ru and may be used to reduce the demand. Previously calculated, this is 102 kips at this location. Thus:
Ru = 794 – 102 = 692 kips.
Notes: The calculations shown use the AISC 341 methodology.

## Slide 85: SMF Example – Panel Zone Check
Since fv = 1, fvRb = 547 kips, which is less than the required resistance, 692 kips. Therefore, doubler plates are required. The required additional strength from the doubler plates is 692 – 547 = 145 kips. The plates must be at least ¼” thick as the strength of the double plates is:
Notes: The calculations shown use the AISC 341 methodology.

## Slide 86: SMF Example – Connection Configuration
Notes: The text on this slide is taken from the AISC Seismic Provisions. Connections that accommodate the required interstory drift angle within the connection elements and provide the measured flexural resistance and shear strengths specified above are permitted. In addition to satisfying the requirements noted above, the design must demonstrate that any additional drift due to connection deformation can be accommodated by the structure. The design must include analysis for stability effects of the overall frame, including second-order effects.

## Slide 87: SMF Example – Connection Configuration
Notes: The following is taken from the AISC Seismic specification. This provision specifically permits the use of prequalified connections meeting the requirements of ANSI/AISC 358, Prequalified Connections for Special and Intermediate Steel Moment Frames for Seismic Applications (AISC, 2016a) to facilitate and standardize connection design. Other prequalification panels may be acceptable but are subject to the approval of the authority having jurisdiction. Use of connections qualified by prior tests or project specific tests may also be used although the engineer of record is responsible for substantiating the connection. Published testing, such as that conducted as part of the SAC project and reported in FEMA 350 and 355, or project-specific testing may be used to satisfy this provision.

## Slide 88: Special Moment Frames Summary
Beam-to-column connection capacity
Select preliminary member sizes
Check member local stability
Check deflection and drift
Check torsional amplification
Check the column-beam moment ratio rule
Check shear requirement at panel zone
Select connection configuration
  Prequalified connections
  Testing
Notes: Review SMF requirements. FEMA 350 is the current best resource for prequalified connections. AISC will eventually become the official repository for such information. FEMA 350 is available electronically for download at the AISC ePubs site (www.aisc.org).

## Slide 89: Questions
Notes: Slide to initiate questions from the participants.

## Slide 90: DISCLAIMER
NOTICE: Any opinions, findings, conclusions, or recommendations expressed in this publication do not necessarily reflect the views of the Federal Emergency Management Agency. Additionally, neither FEMA nor any of its employees make any warranty, expressed or implied, nor assume any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, product or process included in this publication.
The opinions expressed herein regarding the requirements of the NEHRP Recommended Seismic Provisions, the referenced standards, and the building codes are not to be used for design purposes. Rather the user should consult the jurisdiction’s building official who has the authority to render interpretation of the code.
Any modifications made to the file represent the presenters' opinion only.