## Slide 1: REINFORCED CONCRETE STRUCTURES
Disclaimer
Notes: Title slide, consisting of an image of the cover of the data disk containing the 2015 NEHRP Recommended Seismic Provisions
This topic is the seismic design of reinforced concrete structure. During this presentation you will learn the basics of seismic design of reinforced concrete buildings.
The examples in this topic draw heavily on the examples in the FEMA P-752 Design Examples CD.

## Slide 2: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 3: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 4: Unconfined Concrete Stress-Strain Behavior
Notes: This slide presents stress-strain diagrams for unreinforced, unconfined concrete in compression.
Behavior is relatively linear up to about one-half of the maximum compressive stress. Concrete exhibits no precise yield point. Strain at maximum strength is close to 0.002 regardless of maximum stress. Lower strength concrete can have strains at crushing that exceed 0.004, however a typical design value is 0.003 at crushing. Stronger concretes are more brittle.

## Slide 5: Confined Concrete Stress-Strain Behavior
Pitch of
¼ in. dia.
spiral
Tests of
6 in. x 12 in.
cylinders
Notes: This figure presents stress-strain behavior of confined concrete section.
This slide shows the benefits of confinement on concrete behavior. Presented are stress-strain diagrams for confined concrete in compression. The specimens were 6 in. by 12 in. cylinders. Confinement was provided by spiral reinforcement. Reducing spiral pitch (or hoop spacing) increases maximum concrete stress and strain capacity (ductility).

## Slide 6: Reinforcing Steel Stress-Strain Behavior
Notes: This figure shows typical stress-strain behavior of common grades of reinforcing steel.
The most commonly used is Grade 60 which shows a distinct yield plateau and strain hardening at between 0.5% and 1% elongation. For common analysis of reinforced concrete behavior, strain hardening is ignored. For seismic design, it is important that the actual yield strain of the steel is not significantly higher than the value used in design.

## Slide 7: Reinforced Concrete Behavior
Notes: This figure shows stages of behavior of a reinforced concrete beam.
At low loads the section is uncracked and an analysis using uncracked-transformed section properties can be used to predict behavior. After the concrete cracks, the concrete on the tension side of the beam is neglected, and a cracked-transformed section analysis can be used to predict behavior. However, this method is only valid as long as both the steel and the concrete stress-strain behaviors are linear. Concrete can be assumed to have a linear stress-strain behavior up to approximately 50% of maximum concrete stress (f’c).
After the concrete stress exceeds about 50%f’c, a strain compatibility approach can be used, using a realistic concrete stress-strain model. After the steel yields, there is typically an extended plateau in which the displacement increases significantly with very little increase in applied load. A commonly used indicator of member ductility is the ratio of the displacement at ultimate to the displacement at first yield. This is known at the displacement ductility, and for seismic design in particular, bigger is better.

## Slide 8: Typical Moment Curvature Diagram
f x 10-5 in-1
0
100
200
300
0
100
200
300
400
500
600
700
w/ strain hardening
w/o strain hardening
M, in-kip
f’c = 4 ksi
fy = 60 ksi
b = 8 in
d = 10 in
r = 0.0125
Notes: This figure shows moment-curvature diagrams for a rectangular section in flexure.
Strain hardening in the tension steel increases the final strength. A concrete strain of 0.003 corresponds to maximum strength.

## Slide 9: Moment-Curvature with Confined Concrete
Notes: This figure presents moment-curvature behavior of a confined concrete section.
The presence of confining reinforcement can significantly increase the maximum achievable curvature. After the strain on the compression face exceeds 0.003, the cover over the confining steel will spall, however the concrete within the core will remain intact. A model such as the Kent and Park model presented earlier can be used with the strain compatibility method to calculate moments and corresponding curvatures.

## Slide 10: Moment-Curvature with Confined Concrete
Notes: This figure presents the results of the analysis of a beam, whose dimensions and reinforcing details are given on the slide.
As you can see, the addition of the confining reinforcing increases the usable curvature from just under 500 microstrain per inch to just over 1600. The Scott, Park, and Preistley model was used to model the behavior of the confined concrete. This model accounts for the increase in concrete compressive strength. In addition the compression steel was able to yield, and strain hardening was considered in the tension steel. These three factors combined to result in an increase in moment capacity from the confining steel, even though the cover concrete was lost.

## Slide 11: Plastic Hinging
Notes: This figure shows how spreading plasticity can significantly increase plastic rotation and displacements.
The curvature diagram shows a region of very high curvatures (beyond the yield curvature, y) at maximum moment and elastic response in other regions. The region of curvatures past yield curvature is known as the plastic hinge region. The irregular curvature on the “actual” curve is due to cracking.
The plastic rotation and the tip displacement can be calculated from the “actual” curvature diagram, or from the idealized curvature diagram. The idealized diagram is based on a bi-linear approximation of the moment-curvature diagram and an assumed length of the plastic hinge, lp.

## Slide 12: Strategies to Improve Ductility
Use low flexural reinforcement ratio
Add compression reinforcement
Add confining reinforcement
Notes: This slide presents strategies to improve ductility.
The previous discussion presented three strategies for improving ductility. These are summarized in this slide.

## Slide 13: Other Functions of Confining Steel
Acts as shear reinforcement
Prevents buckling of longitudinal reinforcement
Prevents bond splitting failures
Notes: This slide presents other functions of confining steel.
Confining reinforcing also has other useful functions that are presented in this slide.

## Slide 14: Structural Behavior Frames
Story Mechanism
Sway Mechanism
Notes: This figure presents failure mechanisms of frame due to lateral load, story mechanism and sway mechanism.
With an understanding of reinforced concrete member behavior, reinforced concrete systems can be designed to ensure acceptable behavior in a seismic event. We will now discuss desirable system behaviors.
The goal in design of structural frames is to size and reinforce members such that when subjected to large lateral displacements the hinges form in the beams adjacent to the columns, but the columns remain relatively undamaged. This is known as the “strong column-weak beam” approach that is illustrated in the right frame in this slide. A “weak column-strong beam” design can result in the undesirable story mechanism, also known as a soft story, that is shown in the left illustration.

## Slide 15: Structural Behavior - Walls
Sliding on
construction
joint
Sliding on
flexural cracks
Horizontal
tension
Flexural
failure
Notes: This figure shows types of failures in structural walls. The left figure shows a flexural failure with a plastic hinge zone at the base of the wall. The second figure shows that severe cracking necessitates that web reinforcement carries the horizontal shear force. The last two figures show types of sliding failures: sliding along full depth flexural cracks or along construction joints.
The most desirable is the flexural failure with other modes precluded. With proper detailing, the wall can exhibit good strength and ductility without excessive drift or collapse.

## Slide 16: Structural Behavior - Columns
Ultimate
yield
Moment, M, in-kip
Curvature, f, rad/in
Axial load, P, kip
0
200
400
600
800
1000
0
400
800
1600
1200
0
0.001
0.002
1.75”
bending axis
Notes: This figure presents the axial force-moment interaction curve on the left and the axial force-curvature interaction curve on the right.
In strong column-weak beam design, undesirable failures in the columns must be precluded through proper design and detailing. This slide presents the P-M curve on the left and the P-curvature curve on the right. Note that the presence of large axial loads reduces the curvature at ultimate. Axial loads above the balanced point reduce ductility of beam-columns since the reinforcing steel on the tension side of the column never yields. Confinement reinforcement improves axial ductility, but this plot shows curvature ductility, which is more important in frames. The strong column-weak beam design approach ensures that failure will initiate in ductile beams rather than in brittle columns.

## Slide 17: Influence of Hoops on Axial Strength
After spalling-
P = Acore(f’c + 4 flat)
Before spalling-
P = Agf’c
After spalling  Before spalling
Notes: This slide present influence of hoops on axial strength of a circular section.
The strength of an unconfined concrete column is the gross area times the unconfined compressive strength. After the concrete outside the spiral, hoops or ties has spalled, the strength of the column is the core area times the enhanced compressive strength. Work done in the 1920s by Richart et al. indicated that confined concrete strength is roughly the unconfined strength plus 4 times the confining pressure, flat. The goal in designing the hoops is to ensure that the strength after cover spalling is not less than the strength before spalling.

## Slide 18: Hysteretic Behavior of Well Confined Column
Notes: The figure presents a chart showing hysteretic behavior of well confined column.
This type of hysteresis loop shows good performance of a column with generous confinement reinforcement. The preferred type of hysteresis loop shows only small degradation of moment strength with increased imposed drift. Also the loops remain “fat” which indicates good energy dissipation.

## Slide 19: Structural Behavior Columns
D
M1
M2
V
P
M
Mo
Mpr
Range
of P
V
V
M1
M2
L
Notes: This slide presents structural behavior of column at lateral displacement.
To ensure strong column-weak beam behavior, shear failures of columns must also be precluded. Shear is maximum in a column when the moments at each end are at their maximum, also known as the probable moment. The moment capacity of a column depends on the magnitude of the axial load. To avoid shear failures, the design should focus on the axial load that produces the largest moment capacity. The P-M interaction diagram shows this range of axial loads for an example column.

## Slide 20: Structural Behavior Joints
Notes: This slide presents the structural behavior of beam-column joint.
Another location in frames where premature failures must be precluded is the beam-column joints. This slide shows joint actions. The left figure shows forces (stresses) imposed on a typical exterior joint, and the right shows cracks. Upon reversal of direction, perpendicular cracks form. The anchorage of the reinforcement can be compromised. The important aspects of joint design are ensuring proper bar development and precluding shear failures in the joint. This can be accomplished through proper detailing of hoop reinforcement and bar hooks.

## Slide 21: Hysteretic Behavior of Joint with Hoops
Notes: This figure shows a typical hysteresis loop for a joint with hoops. The joint shows good performance under repeated reversed loads.

## Slide 22: Hysteretic Behavior of Joint without Hoops
Notes: This figure shows a typical hysteresis loop of a joint without confining hoops.
Note the rapid deterioration of the joint.

## Slide 23: Summary of Concrete Behavior
Compressive Ductility
  Strong in compression but brittle
  Confinement improves ductility by
    Maintaining concrete core integrity
    Preventing longitudinal bar buckling
Flexural Ductility
  Longitudinal steel provides monotonic ductility at low reinforcement ratios
  Transverse steel needed to maintain ductility through reverse cycles and at very high strains (hinge development)
Notes: This slide presents a summary of concrete behavior under seismic loading.
We will now review reinforced concrete behavior.
Concrete is strong in compression but brittle. Confinement improves compressive ductility by limiting transverse expansion in the concrete. As the transverse steel ties take the strain in tension, the concrete core maintains its integrity. Closely spacing the ties will limit longitudinal bar buckling and thus contribute to improved compressive ductility. Longitudinal steel provides flexural ductility at low reinforcement ratios for a single overload. Transverse steel is needed to maintain integrity of the concrete core (which carries compression and shear), and prevent longitudinal bar buckling after the cover has spalled and crossing cracks form. A relative balance of tension and compression steel aids flexural ductility. The amount of longitudinal tension steel must be limited to insure a tension-type failure mode.

## Slide 24: Summary of Concrete Behavior
Damping
  Well cracked: moderately high damping
  Uncracked (e.g. prestressed): low damping
Potential Problems
  Shear failures are brittle and abrupt and must be avoided
  Degrading strength/stiffness with repeat cycles
    Limit degradation through adequate hinge development
Notes: This slide presents a summary of concrete behavior under seismic loading.
The level of damping in concrete structures depends on the amount of cracking. It is important to avoid potential problems in concrete structures: Shear failures in concrete are brittle and abrupt and must be avoided; repeated loadings degrade strength and stiffness as concrete cracks and steel yields. Degradation can be limited by assuring adequate hinge development.

## Slide 25: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 26: Reference Standards
16
Notes: This slide shows photos of the covers of reference standards ASCE 7-16 and ACI 318-14

## Slide 27: Modifications to Reference Standards
Notes: This slide shows cover of FEMA P-1050 and proposed modifications to ASCE 7 Section 14.2.

## Slide 28: Reference Standards
ASCE 7-16: Defines systems and classifications Provides design coefficients ACI 318-14: Provides system design and detailing requirements consistent with ASCE 7-16 system criteria Modified by ASCE 7-16
Notes: This slide provides summary of the scope of the two main reference standards

## Slide 29: Seismic-Force-Resisting Systems
Moment Frames
Cast-in-Place
Special
Intermediate
Ordinary
Precast
Special
Shear walls
Cast-in-Place
Special
Ordinary
Detailed plain
Ordinary plain
Precast
Intermediate
Ordinary
Dual Systems
Notes: The figure shows two common seismic-force-resisting systems using reinforced concrete, moment frames and structural walls.
This slides presents a list of seismic-force-resisting systems included in ACI 318-14.
The two common seismic-force-resisting systems using reinforced concrete are moment frames and structural walls. A combination of structural walls and moment frames can be considered a dual system when certain criteria are met.
ASCE 7 Section 12.2 presents design coefficients and system limitations for various Seismic Design Categories. Precast walls can be used, however they will not be addressed in detail in this session.
The system classifications relate to detailing requirements and associated the ductility of the structural systems. The system ductility relates to the basic reinforced concrete behavior covered previously.

## Slide 30: Use of Reference Standards
ACI 318
  Chapter 18, Earthquake-Resistant Structures
ASCE 7-16 and Provisions Section 14.2
  Modifications to ACI 318
  Detailing requirements for concrete piles
Provisions supersede ASCE 7-10 modifications
Notes: This slide presents use of reference standards.
ACI 318-14 Chapter 18 contains all the design provisions for earthquake-resistant structures. Provisions and ASCE 7 Section 14.2 presents some modifications to ACI 318 Chapter 18 as well as some additional reinforced concrete structure requirements. This presentation will not cover the precast concrete provisions in any detail.

## Slide 31: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 32: Performance Objectives
Special Moment Frames
  Strong column
    Avoid story mechanism
  Hinge development
    Confined concrete core
    Prevent rebar buckling
    Prevent shear failure
  Member shear strength
  Joint shear strength
  Rebar development and splices (confined)
Notes: This slide presents Performance Objectives of Special Moment Frame system.
The requirements of Special Moment Frames in ACI 318 Chapter 18 are intended to ensure the performance objectives listed on this slide. The strong column-weak beam design avoids forming a mechanism in a single story (the story mechanism presented earlier). Adequate hinge development is needed for ductility and is accomplished by the use of transverse reinforcement which confines the concrete core and prevents rebar buckling. Shear strength must be adequate to avoid abrupt failures in members and joints. Requirements for rebar anchorage and splicing (such as 135 degree hooks) are intended to maintain the integrity of the design.

## Slide 33: Performance Objectives
Intermediate Moment Frames
  Avoid shear failures in beams and columns
  Plastic hinge development in beams and columns
  Toughness requirements for two-way slabs without beams
Ordinary Moment Frames
  Minimum ductility and toughness
  Continuous top and bottom beam reinforcement
  Minimum column shear failure protection
Notes: This slide presents Performance Objectives of Special Moment Frame system (continued).
Intermediate frames have less ductility, with detailing requirements to prevent the most significant types of failures, namely shear failures, and they requirements provide a moderate level of ductility and toughness.
Ordinary moment frames have very few detailing requirements, only those associated with minimal ductility.

## Slide 34: Special Moment Frames
General detailing requirements
Beams
Joints
Columns
Example problem
Notes: This slide provides a summary of the design features of Special moment frames that will be covered in this section.

## Slide 35: Frame Mechanisms “strong column – weak beam”
Story mechanism
Sway mechanism
Notes: This figure presents failure mechanisms of frame due to lateral load, story mechanism and sway mechanism.
This slide presents failure mechanisms of frame due to lateral load.
As discussed previously, strong column-weak beam design is required for special moment frames. This slide reiterates the advantages. For a system with weak columns, a mechanism is created when the columns of only one story reach their flexural capacities (less dissipation of seismic energy prior to collapse). For a system with strong columns and weak beams, a mechanism is created when ALL beams on ALL stories yield (much more seismic energy dissipated prior to collapse).

## Slide 36: Required Column Strength
M
M
M
M
nc1
nc2
nb2
nb1
Notes: This figure presents the required column strength with respect to beam strength.
To ensure that the beams develop plastic hinges before the columns, the sum of the flexural strengths of the columns at a joint must exceed 120% of the sum of the flexural strengths of the beams. This requirement protects against premature development of a story mechanism, but due to the realities of dynamic response, it does not assure a full building mechanism.

## Slide 37: Hinge Development
Tightly Spaced Hoops
  Provide confinement to increase concrete strength and usable compressive strain
  Provide lateral support to compression bars to prevent buckling
  Act as shear reinforcement and preclude shear failures
  Control splitting cracks from high bar bond stresses
Notes: This slide presents information regarding hinge development.
It is also important in this type of system to ensure proper hinge development. The hinges must be able to form and then undergo large rotations and load reversals without significant reduction in strength. In this way, plasticity and hinging will be able to spread throughout the frame. Tightly spaced hoops are required to ensure proper hinge development and behavior. Some of the functions of the hoops are presented in this slide.

## Slide 38: Hinge Development
Before
spalling
After
spalling
Notes: This figure presents some of the mechanics of hinge development, before spalling and after spalling.
Prior to spalling, the familiar stress diagram is present, with tension in the bottom steel, compression in a roughly parabolic distribution in the concrete, and some compressive stress in the top steel. Upon spalling, the stress distribution changes, The compression block of the concrete moves lower in the cross section, and the stresses in the compression steel are greatly increased. To maintain section integrity, material component failures must be avoided. Concrete crushing and compression bar buckling can be prevented by transverse reinforcement. Closely spaced hoop steel limits lateral strain in the concrete and allows greater useful strains in the concrete and hence improved ductility. Proper spacing of hoops also prevents longitudinal bar buckling.

## Slide 39: Hinge Development
Bidirectional cracking
Spalled cover
Notes: The figure shows that under reverse load applications, hinge development affects both the top and bottom faces of beams. This leads to bidirectional cracking and spalling of cover on the top and bottom of the beam.
This slide presents some of the mechanics of hinge development (continued).

## Slide 40: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 41: Performance Objectives
Special R/C structural walls
  Resist axial forces, flexure and shear
  Boundary members
    Where compression stress/strain is large, maintain capacity
  Development of rebar in panel
  Ductile coupling beams
Ordinary R/C structural walls
  No seismic requirements, Ch. 18 does not apply
Notes: This slide presents performance objectives of structural walls.
Design of structural walls for seismic resistance includes designing to resist axial forces, flexure, and shear. Special boundary confinement is required at the ends of walls where the maximum compressive stress associated with flexural and axial loads are high.
In additional to structural walls, ACI 318 provides detailing requirements for coupling beams.
Since ACI 318 Chapter 18 does not have any seismic provisions for Ordinary structural walls, they are not covered in this presentation.

## Slide 42: Design Philosophy
Flexural yielding will occur in predetermined flexural hinging regions
Brittle failure mechanisms will be precluded
  Diagonal tension
  Sliding hinges
  Local buckling
  Shear failures in coupling beams
Notes: This slide presents design philosophy of structural walls.
The design philosophy for walls is to ensure a ductile, flexural failure mechanism and preclude all brittle mechanisms.

## Slide 43: ACI 318, Overview of Special Walls: General Requirements
Shear plane, Acv =
web thickness x
length of wall
 = perpendicular
to shear plane
t = parallel to shear plane
Notes: This slide presents some of the ACI 318 notation for dimensions and reinforcing ratios in special structural walls.

## Slide 44: ACI 318, Overview of Special Walls: General Requirements
 and t not less than 0.0025
unless
then per Sec.11.6
Spacing not to exceed 18 in.
Reinforcement contributing to Vn shall be continuous and distributed across the shear plane
Notes: This slide presents some of the minimum reinforcing requirements for special structural walls.

## Slide 45: ACI 318, Overview of Special Walls: General Requirements
Two curtains of reinforcing required if:
Design shear force determined from lateral load analysis
Notes: This slide presents more requirements for special structural walls.

## Slide 46: ACI 318, Overview of Special Walls: General Requirements
c = 3.0 for hw/w1.5
c = 2.0 for hw/w2.0
Linear interpolation between
Shear strength:
Walls must have reinforcement in two orthogonal directions
Notes: This slide presents requirements for shear strength of the special structural walls.
The equation for shear strength of walls recognizes the higher shear strength of walls with high shear-to-moment ratios. For stout walls,  shall not be less than t.

## Slide 47: ACI 318, Overview of Special Walls: General Requirements
P
M
For axial load and flexure, design like a column to determine axial load – moment interaction
Notes: The figure shows a wall under load P and moment M.
This slide presents design requirements of special wall considering axial load –moment interaction.
To determine the required longitudinal reinforcement, the wall is treated like a column. An interaction diagram can be developed for the selected reinforcing layout, and checked against combinations of axial load and moment as determined from analysis.

## Slide 48: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 49: Members Not Part of LFRS
In frame members not designated as part of the lateral-force-resisting system in regions of high seismic risk:
  Must be able to support gravity loads while subjected to the design displacement
  Transverse reinforcement increases depending on:
Forces induced by drift
Axial force in member
Notes: This slides presents requirements for members not part of lateral force resisting system.
ACI 318 has provisions to ensure that gravity members can accommodate the expected seismic drift while maintaining their ability to support the design gravity loads.

## Slide 50: Diaphragms
Check:
Shear strength and reinforcement (min. slab reinf.)
Chords (boundary members)
- Force = M/d Reinforced for tension
(Usually don’t require boundary members)
Load from analysis in accordance
With design load combinations
Collectors, if req’d to transfer force
from diaphragm to structural walls
Shear walls
Diaphragm
Notes: This figure shows a view of a diaphragm.
The slide shows where collectors might be needed to transfer forces from a long diaphragm into a narrow structural wall. The design load is to be from seismic analysis in accordance with the design load combinations. Slab reinforcement is based on shear stress or slab reinforcement minima (same as for slender structural walls). The chord (boundary element) of a diaphragm is designed to resist tension and compression of M/d. Diaphragms rarely require confined chords. There are also special considerations for topped and untopped precast diaphragms.

## Slide 51: Struts and Trusses: Performance Objectives
All members have axial load (not flexure), so ductility is more difficult to achieve
Full length confinement
Notes: This slide presents performance objectives of strut and truss systems.
Truss systems of reinforced concrete are rarely used. Ductility, usually developed in flexure, is difficult to achieve. Every member in a truss is axially loaded; therefore, every member is designed and reinforced as a column. Full height confinement is used in all members. Anchorage is extremely important to assure adequate post yield response.

## Slide 52: Precast Concrete: Performance Objectives
Ductile connections
Inelastic action at field splice
Strong connections
Configure system so that hinges occur in factory cast members away from field splices
Field connections
must yield
Field connections
at points of low
stress
Notes: The top left figure shows field connections at points of low stress, and top right figure shows the filed connections must yield.
This slide presents performance objectives of precast concrete systems.
Frames can be based on one of two basic modes of behavior in precast buildings:
Precast that emulates monolithic construction used for frames (strong connections). For this type of system, field connections are made at points of low stress, and the hinges will occur in factory cast members, not field splices.
Jointed precast with ductile connections. For this type of system, yielding occurs in the field connections.
In the NEHRP Provisions, acceptance of special precast structural walls is based on validation testing.

## Slide 53: Quality Assurance: Rebar Inspection
Special inspection
  Rebar placement
  Prestressing tendon placement, stressing, grouting
  Concrete placement
Testing
  Rebar (ratio of yield to ultimate)
  Concrete
Notes: This slide presents quality assurance requirements in ASCE 7.
Quality assurance is covered in ASCE 7 Chapter 11A. However, this chapter is often not adopted by the local building code, so the QA requirements are often those contained in the model building code.
A quality assurance plan is generally required for most seismic force resisting systems.
This slide contains a general list of the types of testing and inspection required for concrete buildings.

## Slide 54: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples from FEMA P-751
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 55: Special Moment Frame Example
5 @ 20’ = 100’
7 @ 30’ = 210’
A
A’
B
C
C’
D
1
2
3
4
5
6
7
8
N
Located in Berkeley, California
12-story concrete building
N-S direction: SMF
E-W direction: dual system
Seismic Design Category D
Modal Analysis Procedure
Typical Floor Plan
Notes: The figure shows a typical floor plan.
This slide includes descriptions on the design example of special moment frame.
We will now work through a design example. This moment frame example is found in Chapter 7 of the NEHRP Recommended Provisions: Design Examples (FEMA P-751). In the North-South direction, the seismic force resisting system is a special moment frame. In the East-West direction, it is a dual system with moment resisting frames on Column Lines 1, 2, 7, and 8, and structural walls between Column Lines B and C along Lines 3-6. Note that Column Lines 1 and 8 have 6 columns while Column Lines 2 and 7 have only 4 columns. The example will focus on beams, columns and joints in the frame on Column Line 1.

## Slide 56: Frame Elevations
Grid Lines 2 and 7
Grid Lines 3 to 6
Notes: This figure shows the elevation views of the frames on Column Lines 2 and 3.
Note the structural wall on Column Lines 3 to 6.
The concrete used in the majority of the building is normal-weight concrete with f’c = 5,000 psi. To perform the analysis, initial member sizes were estimated then adjusted as the design process required.

## Slide 57: Story Shears: E-W Loading
Notes: This figure presents the story shears on Frames Lines 1, 2, and 3.
All of the structural wall lines (grid 3-6 are similar to grid 3). Note the locations where story shears are negative for Frames 2 and 3. Also note that the frame line with the structural wall attracts the greatest portion of the seismic shear.
Note also that the story shears are the greatest at Frame 1 at Level 7 due to the interaction between the frames and walls. Therefore, this example focuses on the elements at Level 7.

## Slide 58: Seismic Analysis: Dual Systems
25% forces w/o
structural wall
100% forces with
structural wall
For dual systems, moment frame must be designed to resist at least 25% of design seismic forces (ASCE 7, Sec. 12.2.5.1)
Notes: The figure shows the story shear with two cases, 100% forces with structural wall, and 25% forces without structural wall.
This slide presents requirement and story force profiles of dual system.
ASCE 7 Section 12.2.5.1 requires that for dual systems the moment frame without walls must be capable of resisting at least 25% of the design forces. The building was reanalyzed with the walls removed and 25% of the equivalent seismic forces applied. This slide compares story shears from the original analysis with the 25% rule. Note that this rule controls the design for the ground level frames.

## Slide 59: Layout of Reinforcement
30”
24”
32”
29.5”
28.5”
4
#4 stirrup
#8 bar, assumed
Notes: This figure shows the layout of reinforcement for beams intersecting at Column Line 4 for Frame 1. The typical beams are 24 inches wide by 32 inches deep.
Note the different values of d for beams in each direction.

## Slide 60: Design Strengths
Design Aspect | Strength Used
Beam flexure | Design strength
Beam shear | Maximum probable strength
Beam-column joint | Maximum probable strength
Column flexure | 1.2 times nominal beam strength
Column shear | Maximum probable strength
Notes: This slide reviews how strengths are calculated for various aspects of design.
Maximum probable strength is used when a higher strength than the design strength causes more severe effects. Column strength is modified by the strong column-weak beam rule.

## Slide 61: Bending Moment Envelopes: Frame 1 Beams, 7th Floor
Notes: This figure shows the bending moment envelopes for beams in Frame 1 at Level 7.
The structure and the moment envelopes are symmetric about the centerline.
The combinations are:
1.2D + 1.6L
1.2D + 1.0E + 0.5L
0.9D + 1.0E
With E defined as QE ± 0.2SDSD with SDS=1.1 and =1.0. QE is the effect from horizontal seismic forces.

## Slide 62: Beam Reinforcement: Longitudinal (continued)
Minimum of two bars continuous top and bottom: | OK (three #8 bars continuous top OK (four #8 bars continuous top and bottom)
Positive moment strength greater than 50 percent negative moment strength at a joint: | OK (at all joints)
Minimum strength along member greater than 0.25 maximum strength: | OK (As provided = four #8 bars is more than 25 percent of reinforcement provided at joints)
Check additional requirements:
Notes: This slide presents design of longitudinal reinforcement in the beam (continued).
In addition to the computed strength requirements and minimum reinforcement ratios described in the previous slides, the final layout of reinforcing steel also must satisfy the additional requirements from ACI 318

## Slide 63: Beam Reinforcement: Layout
1
4
4
Notes: This figure presents layout of longitudinal reinforcement for Frame 1, in the elevation of beams between gridlines A and D.
The other beams can be checked in a similar manner.

## Slide 64: Determine Beam Design Shear
Probable moment
strength, Mpr (k-in)
Vu,grav = 34.1 kips
B
C
20’ – 30”
= 17’-6”=210”
7,929
6,841
Assumed
hinging
mechanism
Notes: The top right figure shows the hinging mechanism in which the maximum probable negative moment is developed at one end of the beam and the maximum probable positive moment is developed at the other end. The bottom left figure show the shear distribution between B and C.
Next we will determine the design shear forces for the beams. These shears are based on the illustrated hinging mechanism in which the maximum probable negative moment is developed at one end of the beam and the maximum probable positive moment is developed at the other end. The shears from the probable moments are then combined with the gravity shear to determine the total design shear.

## Slide 65: Beam Shear Force
Design shear
Factored
gravity shear
Seismic shear
Beam moments
Hinge locations
Notes: This figure shows the shear calculations, from defining the hinge locations, calculating beam moments, seismic shear and factored gravity shear, and finally the design shear by combining seismic and gravity shears.
The design shear is the gravity plus the seismic shear. Seismic shear is computed based on the flexural strength (Mpr) of the beams based on an assumed hinging pattern.

## Slide 66: Beam Reinforcement: Transverse
Check maximum spacing of hoops within plastic hinge length (2h)
  d/4 = 7.4 in.
  6db = 6.0 in.
  6 in.
  Therefore, 6.0 in. spacing at ends is adequate
  At beam rebar splices, s = 4.0 in.
Notes: This slide presents detailing of transverse reinforcement in the beam.
After calculating the required spacing to provide adequate shear strength, the spacing is checked against the maximum allowable spacing as shown in this slide. In this case the required spacing for shear strength governs.

## Slide 67: Frame 1 Column Design
Design column using standard P-M interaction curve
then:
Column:
30"
Level 7
Level 6
20'-0"
20'-0"
32"
32"
P
L
= 78 kips Includes
P
D
= 367 kips level 7
13'-0"
A
A'
B
Notes: The figure shows the floor plan at level 6 and level 7.
This slide presents column design example.
Finally, we will consider the design of a representative column, in this case the Frame 1 column on grid A’ just below the 7th floor. Recall that ACI considers a member to be a “column” where the factored axial demand exceeds 0.1Agf’c. The column design is based on a P-M analysis and the sum of the column moment capacities must exceed the beam moment capacities at each joint.

## Slide 68: Column Design Moments Design for strong column based on nominal beam moment strengths
Column moments (Level 7), assume uniform distribution top and bottom
Beam moments (Level 7)
A
A'
B
6,406
5,498
7,142
7,142
Notes: This figure shows the calculation of the column design moments from beam flexural capacities and strong column-weak beam rule.
This method assumes an inflection point at midheight of the column which is reasonable in most cases for regular frame layouts.

## Slide 69: Column Transverse Reinforcement
nl: number of longitudinal bars that are laterally supported by the corner of hoops or by seismic hooks
Notes: This slide presents requirements for column transverse reinforcement.
Next the necessary column transverse reinforcement to provide confinement of the concrete core is calculated. The equation on the slide that results in the larger amount of confining steel will govern.

## Slide 70: Column Transverse Reinforcement Maximum spacing is smallest of: h/4 = 30/4 = 7.5 in. 6db = 6*1.0 = 6.0 in. (#8 bars) so calculated as follows: for 12 #8 vertical bars and #4 hoops, hx = 8.33 in. and so = 5.72 in. Next, check confinement requirements……
Notes: This slide presents the rules to calculate maximum hoop spacing within the potential hinge region.

## Slide 71: Column Transverse Reinforcement Therefore, use #4 bar hoops with 4 legs Ash = 0.80 in2
Assume 4 in. hoop spacing:
fc' < 10,000 psi and Pu< 0.3fc'Ag Equation (c) was not required.
Notes: This slide presents design of column transverse reinforcement.
For most columns in Special moment frames, 4 inch hoop spacing is a reasonable assumption, so we start there.

## Slide 72: Determine Column Shear Based on probable moment strength of columns and can be limited by probable moment strength of beams
Mpr,2
Mpr,4
Mpr,1
Mpr,3
n
Mpr,top
Mpr,bottom
Vseismic
Vseismic
Notes: The figures shows the free-body diagram of a column and the shear stress distribution along the height.
The seismic shear in the columns can based on the probable flexural strength of the columns themselves or by the probably flexural strength of the beams that frame into the column at the top and the bottom.
Using the column moment strengths is conservative, but if the amount of shear reinforcement is governed by the confinement requirements, there may be adequate shear capacity for the conservative but more simple method.
If the probable moments in the beams are used, the column moments above and below the joint are determined based on their relative flexibilities. Then the shear in the column is calculated based on the moments at the top and the bottom of the column and the column clear height.

## Slide 73: Column Shear Design
Vc can be included in shear calculation
Mpr,col = 14,940 k-in (12 #8 vert and Pmax)
Based on column moments:
Notes: This slide presents calculation of column shear demend.
In this slide the shear demand in the column is calculated based on the column moment strengths.
Note that since there is significant axial compression in the column, concrete shear strength may be used.

## Slide 74: Column Shear Design Assume 6 in. max hoop spacing at mid-height of column
4 legs #4
s = 6 in. max
Hoops:
Notes: The figure shows hoops spaced at 6 inches in the middle of the column.
This slide shows the calculation of the concrete contribution to column shear strength.
Then the required shear strength to be provided by the steel is determined. The shear strength provided by the hoops spaced at 6 inches in the middle of the column (4 inch spacing is required spacing for confinement at the column ends) is shown to be more than adequate. Therefore, the final hoop layout within the plastic hinge lengths at the tops and bottoms of the columns is set.

## Slide 75: Column Reinforcement
Confinement length, lo, greater of:
  h = 30 in.
  Hc/6 = (156-32)/6 = 20.7 in.
  18 in.
  Therefore, use 30 in.
Notes: This figure shows the final column reinforcing layout.
Outside of the plastic hinge length, the spacing of the hoops can be increased to 6 inches.

## Slide 76: Summary of Seismic Detailing for Frames
Issue | Ordinary | Intermediate | Special
Hinge development and confinement |  | minor | full
Bar buckling |  | lesser | full
Member shear |  | lesser | full
Joint shear | minor | minor | full
Strong column |  |  | full
Rebar development | lesser | lesser | full
Load reversal | minor | lesser | full
Notes: This slide summarizes the differences in detailing requirements for the three types of moment frames. More details of the design example can be found in the FEMA P-1051, design examples.
Special moment frames require special attention to each of the performance objectives. Intermediate frames have less strict requirements on all counts. Ordinary frames have very few requirements beyond those of gravity frames designed using ACI 318. Note that the detailing to avoid rebar congestion is important in special moment frames (use scaled drawings of joints for this task).

## Slide 77: Questions
Notes: 508 note: Slide to prompt questions from participants.

## Slide 78: DISCLAIMER
NOTICE: Any opinions, findings, conclusions, or recommendations expressed in this publication do not necessarily reflect the views of the Federal Emergency Management Agency. Additionally, neither FEMA nor any of its employees make any warranty, expressed or implied, nor assume any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, product or process included in this publication.
The opinions expressed herein regarding the requirements of the NEHRP Recommended Seismic Provisions, the referenced standards, and the building codes are not to be used for design purposes. Rather the user should consult the jurisdiction’s building official who has the authority to render interpretation of the code.
Any modifications made to the file represent the presenters' opinion only.