SECTION 09251 - GYPSUM BOARD - ASBESTOS ENCLOSURES

PART 1 - GENERAL

1.1	RELATED DOCUMENTS:

A.	Drawings and general provisions of Contract, including General and Supplementary Conditions and Division-1 Specification sections, apply to work of this section.

1.2	DESCRIPTION OF WORK:

A.	Types of work include enclosure of Asbestos-Containing Materials (ACM) by the following methods:

ADJUST LISTING BELOW TO PROJECT.

1.	Gypsum board including screw-type metal support system

2.	Gypsum board directly applied to solid (continuous) substrates

3.	Gypsum board applied to wood framing and furring

4.	Drywall finishing (joint tape-and-compound treatment)

5.	Wood framing and furring are specified in Division 6

1.3	DEFINITIONS:

A.	"Enclosure":

1.	An air-tight, impermeable, permanent barrier around asbestos-containing material to control the release of asbestos fibers into the air.

2.	A space, within which asbestos abatement operations are performed, whose limits are defined by rigid or non-rigid barriers for the purpose of controlling access and limiting fiber escape.

1.4	QUALITY ASSURANCE:

A.	Fire-Resistance Rating:  Where gypsum board systems with fire-resistance ratings are indicated, provide materials and installations which are identical with those of applicable assemblies tested per ASTM E 119 by fire testing laboratories acceptable to authorities having jurisdiction.

DELETE OR REVISE BELOW IF NOT APPLICABLE TO ASSEMBLIES INDICATED. COORDINATE WITH INDICATIONS ON DRAWINGS.

1.	Provide fire-resistance rated assemblies identical to those indicated by reference to GA File Nos. in GA "Fire Resistance Design Manual" or to design designations in UL "Fire Resistance Directory" or in test reports of other testing and agencies acceptable to authorities having jurisdiction.

B.	Gypsum Board Terminology Standard:  GA-505 by Gypsum Association.

1.5	SUBMITTALS:

A.	Product Data: Submit manufacturer's product literature for each gypsum board component, including other data as may be required to show compliance with these specifications.

1.6	DELIVERY, STORAGE AND HANDLING:

A.	Deliver materials in original packages, containers or bundles bearing  brand  name and identification of manufacturer or supplier.

B.	Store materials inside under cover and in manner to keep them dry, protected from weather, direct sunlight, surface contamination, corrosion and damage from construction traffic and other causes. Neatly stack gypsum boards flat to prevent sagging.

C.	Handle gypsum boards to prevent damage to edges, ends or surfaces.  Protect metal corner beads and trim from being bent or damaged.

1.7	PROJECT CONDITIONS:

A.	Environmental Requirements, General:  Comply with requirements of referenced gypsum board application standards and recommendations of gypsum board manufacturer, for environmental conditions before, during and after application of gypsum board.

B.	Cold Weather Protection:  When ambient outdoor temperatures are below 50 degrees F (10 degrees C) maintain continuous, uniform, comfortable building working temperatures of not less than 50 degrees F (10 degrees C) for a minimum period of 48 hours prior to, during and following application of gypsum board and joint treatment materials or bonding of adhesives.

C.	Ventilation:  Ventilate building spaces as required to remove water in excess of that required for drying of joint treatment material immediately after its application.  Avoid drafts during dry, hot weather to prevent too rapid drying.

1.	Use HEPA filtered fan units as described in section 01513 for ventilation if required prior to clearance of work area in accordance with Section 01711.

PART 2 - PRODUCTS

2.1	METAL SUPPORT MATERIALS:

A.	Ceiling Support Materials and Systems:

DELETE THIS SUB-ARTICLE IF NO SUSPENSION OR FURRING MEMBERS REQUIRED.

1.	General: Size ceiling support components to comply with ASTM C 754 unless otherwise indicated.

2.	Main Runners: Steel channels with rust-inhibitive finish, hot or cold-rolled.

DELETE ABOVE IF CEILING CAN BE DIRECTLY FURRED TO STRUCTURAL MEMBERS (BAR JOISTS, ETC.) OR DIRECT SUSPENSION SYSTEM IS SELECTED.

3.	Hanger Wire: ASTM A 641, soft, Class 1 galvanized.

USUALLY RETAIN ABOVE WHICH COVERS 8 THROUGH 16 GAGE WIRE. DELETE ABOVE AND RETAIN BELOW WHERE REQUIRED BY LOCAL BUILDING CODE OR BY LOADING.

4.	Hanger Rods and Flats: Mild steel with zinc or equally rust inhibitive coating for rods and zinc or rust-inhibitive paint finish for flats.

5.	Hanger Anchorage Devices: Screws, clips, bolts, or other devices applicable to the indicated method of structural anchorage for ceiling hangers and whose suitability for use intended has been proven through standard construction practices or by certified test data.  Size devices for 3 x calculated load supported except size direct pull-out concrete inserts for 5 x calculated loads.

DELETE ABOVE ONLY IF HANGERS ARE INDICATED TO BE DIRECTLY TIED TO STRUCTURAL MEMBERS OR CONCRETE REINFORCEMENT.

6.	Furring Members:  ASTM C 645; 0.0179 inch (0.455 mm) min. thickness of base metal, hat-shaped.

a.	Where shown as "Resilient", provide manufacturer's special type designed to reduce sound transmission.

ABOVE HAS A SINGLE OR DOUBLE FLANGE, WHICH MUST BE NAILED/SCREWED TO STRUCTURAL JOIST, ETC. (NOT DIRECTLY TO 25 GAGE STUDS).

7.	Furring Members: ASTM C 645; 0.0179 inch (0.455 mm) min. thickness of base metal, C-shaped studs.

ABOVE USED FOR SPANS OF MORE THAN FOUR (4) FEET (1200 MM) .

8.	Furring Anchorages: 16 gage galvanized wire ties, manufacturer's standard wire-type clips, bolts, nails or screws as recommended by furring manufacturer and complying with ASTM C 754.

9.	Direct Suspension Systems:  Manufacturer's standard zinc-coated or painted steel system of furring runners, furring tees, and accessories designed for concealed support of gypsum board ceilings; of proper type for use intended.

CHECK MANUFACTURER'S LITERATURE FOR TYPES AND FINISHES AVAILABLE.

B.	Wall/Partition Support Materials:

DELETE THIS SUB-ARTICLE IF NO STEEL STUDS OR FURRING REQUIRED.

1.	Studs: ASTM C 645; 0.0179 inch (0.455 mm) min. thickness of base metal unless otherwise indicated.

REVISE ABOVE AND BELOW AS DESIRED. COORDINATE WITH CONTRACT DRAWINGS, 1-5/8 INCH (40 MM) OR 2-1/2 INCH (63.5 MM) MAY ALSO BE USED.

a.	Depth of Section: 3-5/8 inch (90 mm), except as otherwise indicated.

2.	Runners:  Match studs; type recommended by stud manufacturer for floor and ceiling support of studs, and for vertical abutment of drywall work at other work.

3.	Furring Members:  ASTM C 645; 0.0179 inch (0.455 mm) min. thickness of base metal, hat-shaped.

a.	Where shown as "Resilient," provide manufacturer's special type designed to reduce sound transmission.

ABOVE HAS A SINGLE OR DOUBLE FLANGE, WHICH MUST BE NAILED/SCREWED TO STRUCTURAL JOIST, ETC.

4.	Fasteners for Furring Members:  Type and size recommended by furring manufacturer for substrate and application indicated.

2.2	GYPSUM BOARD PRODUCTS:

THE FOLLOWING ARE TYPICAL MATERIALS AND CHOICES.

A.	Gypsum Wallboard:  ASTM C 36, of types, edge configuration and thickness indicated below; in maximum lengths available to minimize end-to-end butt joints.

DELETE TYPES BELOW NOT REQUIRED. INDICATE ON DRAWINGS WHERE FOIL-BACKED AND FIRE-RESISTANT TYPES OCCUR.

1.	Type:  Regular, unless otherwise indicated

2.	Type:  Foil-backed where indicated

3.	Type:  Type X for fire-resistant rated assemblies and where indicated

4.	Edges:  Tapered

5.	Edges:  Tapered and featured (rounded or beveled) for prefilling

SELECT ONE REQUIREMENT FOR EDGE (ABOVE) AND THICKNESS (BELOW).

6.	Thickness:  5/8 inch (16 mm), unless otherwise indicated

7.	Thickness:   inch (13 mm), unless otherwise indicated

8.	Thickness:  3/8 inch (10 mm), unless otherwise indicated

9.	Thickness:  as indicated, or if not otherwise indicated, as required to comply with ASTM C 840 for application system and support spacing indicated

DELETE BELOW IF NO MULTI-LAYER APPLICATIONS.

B.	Gypsum Backing Board for Multi-Layer Applications:  ASTM C 442 or, where backing board is not available from manufacturer, gypsum wallboard, ASTM C 36, of type, edge configuration and thickness indicated below; in maximum lengths available to minimize end-to-end joints.

DELETE TYPES BELOW NOT REQUIRED. INDICATE ON DRAWINGS WHERE FOIL-BACKED AND TYPE X BOARDS OCCUR.

1.	Type:  Regular, unless otherwise indicated

2.	Type:  Foil-backed where indicated

3.	Type: Type X for fire-resistance rated assemblies and where indicated

4.	Edges:  Manufacturer's standard

DELETE ABOVE OR BELOW. BELOW BEST FOR LAMINATED APPLICATION BUT GENERALLY ONLY PRODUCED IN ASTM C 442 MATERIAL. VERIFY AVAILABILITY.

5.	Edges:  Square, non-tapered; or V-tongue and groove

SELECT ONE THICKNESS REQUIREMENT FROM BELOW.

6.	Thickness:  5/8 inch (16 mm), unless otherwise indicated

7.	Thickness:   inch (13 mm), unless otherwise indicated

8.	Thickness:  3/8 inch (10 mm), unless otherwise indicated

9.	Thickness: As indicated, or if not otherwise indicated, as required to comply with ASTM C 840 for application system and support spacing indicated

PRODUCT BELOW NOT SUITABLE FOR CEILING APPLICATIONS.

C.	Water-Resistant Gypsum Backing Board:  ASTM C 630, with tapered edges and of type and thickness indicated below; in maximum lengths available to minimize end-to-end butt joints.

RETAIN TYPE OR TYPES BELOW REQUIRED. INDICATE ON DRAWINGS WHERE FIRE-RESISTANT TYPE OCCURS.

1.	Type:  Regular, unless otherwise indicated

2.	Type:  Type X for fire-resistant rated assemblies and where indicated

3.	Thickness:  5/8 inch (16 mm), unless otherwise indicated

4.	Thickness:   inch (13 mm), unless otherwise indicated

5.	Thickness:  As indicated, or if not otherwise indicated, 5/8 inch (16 mm)

RETAIN BELOW FOR EXTERIOR SOFFITS INDIRECTLY EXPOSED TO WEATHER. SEE MANUFACTURER'S LITERATURE FOR LIMITATIONS.

D.	Exterior Gypsum Soffit Board:  ASTM C 931, with manufacturer's standard edges, of type and thickness indicated below:

DELETE TYPES BELOW NOT REQUIRED.

1.	Type:  Regular, unless otherwise indicated

2.	Type:  Type X for fire-resistance rated assemblies and where indicated

CHECK THE AVAILABILITY OF THICKNESSES OF TYPE X GYPSUM BOARD IN THE PROJECT LOCALITY AND EDIT BELOW TO SUIT PROJECT REQUIREMENTS.

3.	Thickness:  5/8 inch (16 mm), unless otherwise indicated

4.	Thickness:   inch (13 mm), unless otherwise indicated

CONSIDER REFERENCING ASTM C 1047-86 FOR ACCESSORIES FOR GYPSUM BOARD. EDIT BELOW ACCORDINGLY.

2.3	TRIM ACCESSORIES:

A.	General: Provide manufacturer's standard trim accessories of types indicated for drywall work, formed of galvanized steel unless otherwise indicated, with either knurled and perforated or expanded flanges for nailing or stapling, and beaded for concealment of flanges in joint compound.  Provide corner beads, L-type edge trim-beads, U-type edge trim-beads, special L-kerf-type edge trim-beads, and one-piece control joint beads.

B.	Semi-Finishing Type:  manufacturer's standard trim units which are not to be finished with joint compound (non-beaded).

C.	Plastic Edge Trim:  manufacturer's standard rigid or semi-rigid PVC moldings of the semi-finished type, shaped to provide resilient contact of gypsum board edges with other work; friction-fit, or pressure-sensitive adhesive mounting.

USUALLY DELETE BELOW (IF EXPOSURE IS SEVERE, GYPSUM BOARD SHOULD NOT BE USED).

2.4	JOINT TREATMENT MATERIALS:

A.	General:  ASTM C 475; type recommended by the manufacturer for the application indicated, except as otherwise indicated.

B.	Joint Tape:  Paper reinforcing tape

EXAMPLES BELOW ARE THE USUAL RANGE OF CHOICES.

C.	Joint Compound:  Vinyl-type powder for interior use

D.	Joint Compound:  Ready-mixed vinyl-type for interior use

USUALLY RETAIN ONE OF 2 ABOVE AND ONE OF 2 BELOW; OR THE SUBSEQUENT SELECTION.

1.	A single multi-purpose type, for entire application

2.	2 separate types; one specifically for bedding tapes and filling depressions, and one for topping and sanding

E.	Joint Compound:  on interior work provide chemical-hardening-type for bedding and filling, ready-mixed vinyl-type or vinyl-type powder type for topping.

2.5	MISCELLANEOUS MATERIALS:

A.	General: Provide auxiliary materials for gypsum board work of the type and grade recommended by the manufacturer of the gypsum board.

DELETE MATERIALS BELOW NOT APPLICABLE TO INSTALLATION METHOD SELECTED.

B.	Laminating Adhesive:  Special adhesive or joint compound specifically recommended for laminating gypsum boards

C.	Fastening Adhesive (for Wood): ASTM C 557

D.	Gypsum Board Screws:  Comply with ASTM C 1002

E.	Gypsum Board Nails:  Comply with ASTM C 514

F.	Concealed Acoustical Sealant:  Non-drying, non-hardening, non-skinning, non-staining, non-bleeding, gunnable sealant for concealed applications per ASTM C 919

G.	Exposed Acoustical Sealant:  Non-oxidizing, skinnable, paintable, gunnable sealant for exposed applications per ASTM C 919

H.	Sound Attenuation Blankets:  FS HH-I-521, Type I; semi-rigid mineral fiber blanket without membrane, Class 25 flame-spread, thicknesses as indicated

I.	Ceramic Tile Adhesive:  Type I organic adhesive for ceramic tile complying with ANSI A136.1

PART 3 - EXECUTION

3.1	PREPARATION FOR METAL SUPPORT SYSTEMS

USE FOLLOWING IF WORK INVOLVES ATTACHING SUPPORT SYSTEM FOR CEILING WORK DIRECTLY TO ACM.

A.	Ceiling Anchorages:  Before starting work of this section complete the following:

1.	Section 01513 - Temporary Pressure Differential & Air Circulation System

2.	Section 01563 - Decontamination Units

3.	Section 01526 - Temporary Enclosures

4.	Section 01560 - Worker Protection - Asbestos Abatement

5.	Section 01562 - Respiratory Protection

USE FOLLOWING IF WORK INVOLVES ATTACHED SUPPORT SYSTEM FOR CEILING TO "T" BARS OF EXISTING SUSPENDED CEILINGS.

B.	Ceiling Anchorages:  Before starting of work of this section complete the following:

1.	Section 01527 - Regulated Areas

2.	Section 01561 - Worker Protection - Repair & Maintenance

3.	Section 01562 - Respiratory Protection

USE FOLLOWING IF WORK INVOLVES WALL SYSTEMS ENCLOSING ACM WITH SUPPORT FASTENED TO OR THROUGH ACM.

C.	Wall Anchorages:  Before starting work of this section complete the following:

1.	Section 01513 - Temporary Pressure Differential & Air Circulation System

2.	Section 01563 - Decontamination Units

3.	Section 01526 - Temporary Enclosures

4.	Section 01560 - Worker Protection - Asbestos Abatement

5.	Section 01562 - Respiratory Protection

USE FOLLOWING IF WORK INVOLVES WALL SYSTEMS WHICH DO NOT COME IN CONTACT OR ONLY INCIDENTALLY CONTACT ACM.

D.	Wall Anchorages:  Before starting work of this section complete the following:

1.	Section 01527 - Regulated Areas

2.	Section 01561 - Worker Protection - Repair & Maintenance

3.	Section 01562 - Respiratory Protection

3.2	INSTALLATION OF METAL SUPPORT SYSTEMS:

A.	General:

B.	ACM:  In disturbing ACM comply with the following:

1.	Section 01046 - Cutting and Patching Asbestos-Containing Materials

2.	Section 01529 - Mini Enclosures and Glovebags

C.	Metal Support Installation Standard:  Comply with ASTM C 754.

1.	Do not bridge building expansion joints with support system.  Frame both sides of joints with furring and other support as indicated.  Provide air tight seal between partition and adjacent surfaces.

2.	Nail or screw furring members to wood framing as indicated.

DELETE ABOVE IF NO WOOD FRAMING (CEILING JOISTS/BEAMS, STUDS, ETC.).

D.	Ceiling Support Suspension Systems:

1.	Secure hangers to structural support by connecting directly to structure where possible while avoiding contact with ACM; otherwise connect to inserts, clips or other anchorage devices or fasteners as indicated.

2.	Space main runners 4 feet (1200 mm) o.c. and space hangers 4 feet (1200 mm) o.c. along runners, except as otherwise shown.

REVISE ABOVE TO COORDINATE WITH STRUCTURE AS DESIRED.

3.	Level main runners to a tolerance of 1/4 inch (6 mm) in 12 feet (3600 mm), measured both lengthwise on each runner and transversely between parallel runners.

4.	Wire-tie or clip furring members to main runners and to other structural supports as indicated.

FOLLOWING IS THE PREFERRED METHOD OF SUPPORT WHERE POSSIBLE.

E0	Direct-hung Metal Support System: Attach perimeter wall track or angle wherever support system meets vertical surfaces.  Mechanically join support members to each other and butt-cut to fit into wall track.

1	Space furring member 16 inches (400 mm) o.c., except as otherwise indicated.

TYPICAL INSTALLATIONS OF BELOW SHOULD BE FULLY DETAILED.

2	Install auxiliary framing at termination of drywall work, and at openings for light fixtures and similar work, as required for support of both the drywall construction and other work indicated for support thereon.

F0	Wall/Partition Support Systems:

INSTALLATION OF FRAMING FOR BELOW SHOULD BE FULLY DETAILED.

1	Install supplementary framing, blocking and bracing at terminations in the work and for support of fixtures, equipment services, heavy trim, grab bars, toilet accessories, furnishings, and similar work to comply with details indicated or, if not otherwise indicated, to comply with applicable published recommendations of gypsum board manufacturer.

2	Isolate stud system from transfer of structural loading to system, both horizontally and vertically. Provide slip or cushioned type joints to attain lateral support and avoid axial loading.

3	Install runner tracks at floors, ceilings and structural walls and columns where gypsum board stud system abuts other work, except as otherwise indicated.

4	Extend partition stud system through acoustical ceilings and elsewhere as indicated to the structural support or substrate above the ceiling.

5	Space studs 16 inches (400 mm) o.c., unless otherwise indicated.

DELETE EITHER ABOVE OR BELOW.

6	Space studs 24 inches (600 mm) o.c., unless otherwise indicated.

DELETE FOLLOWING IF NO DOORS IN THE WORK. LIMITED INFORMATION IS AVAILABLE FROM MANUFACTURERS. ADEQUATE DETAILS SHOULD BE SHOWN ON THE DRAWINGS.

7	Frame door openings to comply with detail indicated or, if not otherwise indicated, to comply with applicable published recommendations of gypsum board manufacturer.   Attach vertical studs at jambs with screws either directly to frames or to jamb anchor clips on door frames; install runner track section (for jack studs) at head and secure to jamb studs.

RETAIN BELOW IF SUSPENSION CEILINGS NOT CAPABLE OF WITHSTANDING DOOR OPENING AND CLOSING FORCES.

8	Extend vertical jamb studs through suspended ceilings and attach to underside of floor or roof structure above, unless otherwise indicated.

9	Frame openings other than door openings to comply with details indicated or, if not indicated, in same manner as required for door openings; install framing below sills of openings to match framing required above door heads.

FURRING CHANNELS ATTACHED TO ACM SHOULD GENERALLY BE AVOIDED IN FAVOR OF "FREE-STANDING" STUD WALL SYSTEMS.

10	Space wall furring members 16 inches (400 mm) o.c., unless otherwise indicated.

DELETE EITHER ABOVE OR BELOW.

11	Space wall furring members 24 inches (600 mm) o.c., unless otherwise indicated.

3.3	GENERAL GYPSUM BOARD INSTALLATION REQUIREMENTS:

A0	Gypsum Board Application and Finishing Standards:  ASTM C 840 and GA 216.

1	Locate exposed end-butt joints as far from center of walls and ceilings as possible, and stagger not less than 1foot (300 mm)  in alternate courses of board.

2	Install ceiling boards in the direction and manner which will minimize the number of end-butt joints, and which will avoid end joints in the central area of each ceiling. Stagger end joints at least 1 foot (300 mm).

3	Install wall/partition boards vertically or horizontally to avoid end-butt joints wherever possible. At stairwells and similar high walls, install boards horizontally with end joints staggered over studs.

4	Install exposed gypsum board with face side out. Do not install imperfect, damaged or damp boards. Butt boards together for a light contact at edges and ends with not more than 1/16 inch (1.6 mm) open space between boards.  Do not force into place.

5	Locate either edge or end joints over supports, except in horizontal applications where intermediate supports or gypsum board back-blocking is provided behind end joints. Position boards so that like edges abut, tapered edges against tapered edges and mill-cut or field-cut ends against mill-cut or field- cut ends. Do not place tapered edges against cut edges or ends. Stagger vertical joints over different studs on opposite sides of partitions.

6	Attach gypsum board to supplementary framing and blocking;  Provide for additional support at openings and cutouts.

7	Form control joints and expansion joints with space between edges of boards, prepared to receive trim accessories.  Provide air tight seal.

8	Cover both faces of steel stud partition framing with gypsum board in concealed spaces (above ceilings, etc.), except in chase walls which are properly braced internally.

9	Except where concealed application is required for sound, fire, air or smoke ratings, coverage may be accomplished with scraps of not less than 8 sq. ft.  (0.75 sq meters) in area, and may be limited to not less than 75 percent of full coverage.

10	Isolate perimeter of non-load-bearing drywall partitions at structural abutments. Provide 1/4 inch  to  inch  (6 mm to 13 mm) space and trim edge with J-type semi-finishing edge trim.   Provide air tight seal.

BELOW IS FEASIBLE ONLY WITH WOOD FRAMING WHERE FIRE RATINGS ARE NOT REQUIRED. DELETE FOR METAL-FRAMED GYPSUM BOARD.

B0	Floating Construction:  Where feasible, including where recommended by manufacturer, install gypsum board over wood framing, with "floating" internal corner construction.

C0	Air-Tight Seal:  Provide air-tight seal at perimeters, control and expansion joints, openings and penetrations with a continuous bead of acoustical sealant including a bead at both faces of partitions.  Comply with ASTM C 919 and manufacturer's recommendations for location of beads, and seal flanking paths around or through the work, including sealing of partitions above acoustical ceilings.

1	Space fasteners in gypsum boards in accordance with referenced standards and manufacturer's recommendations, except as otherwise indicated.

3.4	METHODS OF GYPSUM BOARD APPLICATION:

A0	Single-layer Application:  Install gypsum wallboard.

DELETE BELOW PROVISION IF NO GYPSUM BOARD CEILINGS.

1	On ceilings;  Apply gypsum board prior to wall/partition board application to the greatest extent possible.

2	On partitions/walls:  Apply gypsum board either vertically (parallel) or horizontally, unless otherwise indicated, and provide sheet lengths which will minimize end joints.  Select method which will eliminate gaps in enclosure that cannot be closed with sealant.

3	Wall Tile Base:  Where gypsum board is base for thin-set ceramic tile and similar rigid applied wall finishes, install water resistant gypsum backing board.

4	At showers, tubs and similar "wet" areas, install water-resistant backing boards.  Apply with un-cut long edge at bottom of work, and space 1/4 inch (6 mm) above fixture lips.  Seal ends, cut-edges and penetrations of each piece with water-resistant adhesive.

5	Acoustical Tile Base:  Where gypsum board is base for adhesively-applied acoustical tile, install gypsum backing board.

6	Provide either V-joint type backing board or tape-and-compound treatment of joints (2 coats unsanded).

B0	Double-Layer Application:  Install gypsum backing board for base layer and exposed gypsum board for face layer.

DELETE BELOW IF NO GYPSUM BOARD CEILINGS.

1	On ceilings:  Apply base layer prior to base layer application on walls/partitions; apply face layers in same sequence.  Offset joints between layers at least 10 inches  (250 mm).  Apply base layers at right angles to supports unless otherwise indicated.

REVISE BELOW IF WALL CONDITIONS PERMIT ECONOMICAL USE OF HORIZONTAL APPLICATION OF BASE LAYER AND LAMINATED ATTACHMENT IS METHOD USED.

2	On partition/walls:  Apply base layer and face layers vertically (parallel) with joints of base layer over supports and face layer joints offset at least 10 inches (250 mm) with base layer joints.

C0	Single-Layer Fastening Methods:  Apply gypsum boards to supports as follows:

RETAIN ONE OF THE FOLLOWING. SCREWS SUITABLE FOR METAL OR WOOD OR METAL SUPPORT SYSTEMS.

1	Fasten with screws

2	Fasten to wood supports with adhesive and supplementary screws

D0	Double-Layer Fastening Methods:  Apply base layer of gypsum board and face layer to base layer as follows:

RETAIN ONE OF THE FOLLOWING.

1	Fasten both base layers and face layers separately to supports with screws.

ABOVE AND BELOW SUITABLE FOR METAL OR WOOD SUPPORTS ABOVE METHOD REQUIRED FOR CERTAIN FIRE-RESISTANCE RATED ASSEMBLIES.

2	Fasten base layers with screws and face layer with adhesive and supplementary fasteners.

3	Fasten base layers to wood supports with nails and face layer with adhesive and supplementary fasteners.

INSERT SPECIFIC REQUIREMENTS (IF KNOWN) FOR THE PARTICULAR SUBSTRATE OF THE SYSTEM.

3.5	INSTALLATION OF DRYWALL TRIM ACCESSORIES:

A0	General: Where feasible, use the same fasteners to anchor trim accessory flanges as required to fasten gypsum board to the supports. Otherwise, fasten flanges in accordance with manufacturer's instructions and recommendations.

THE FOLLOWING ARE ONLY EXAMPLES OF "UNIVERSAL" SCOPE DEFINITIONS FOR THE USE OF TRIM. REVISE AS DESIRED OR SHOW BY DETAILS ON DRAWINGS.

1	Install corner beads at external corners of drywall work.

2	Install edge trim whenever edge of gypsum board would otherwise be exposed or semi-exposed, and except where plastic trim is indicated.  Provide type with face flange to receive joint compound except where semi-finishing type is indicated. Install L-type trim where work is tightly abutted to other work, and install special kerf-type where other work is kerfed to receive long leg of L-type trim. Install U-type trim where edge is exposed, revealed, gasketed, or sealant-filled (including expansion joints).

DELETE BELOW IF NO EXTERIOR BOARD OR JOINTS ARE REQUIRED TO BE FINISHED.

3	Install semi-finishing trim where indicated, and where exterior gypsum board edges are not covered by applied moldings or indicated to receive trim with face flanges covered with joint compound.

4	Install edge trim where indicated on wall panels at juncture with ceilings.

5	Install control joint (beaded-type) where indicated.

3.6	INSTALLATION OF DRYWALL FINISHING:

A0	General:  Apply treatment at gypsum board joints (both directions), flanges of trim accessories, penetrations, fastener heads, surface defects and elsewhere as required to prepare work for decoration.  Prefill open joints and rounded or beveled edges, if any, using type of compound recommended by manufacturer.

1	Apply joint tape at joints between gypsum boards, except where a trim accessory is indicated.

2	Apply joint compound in 3 coats (not including prefill of openings in base), and sand or sponge between last 2 coats and after last coat.

DELETE BELOW IF NOT DESIRED OR NOT APPLICABLE. V-JOINT BACKING BOARD USUALLY DOES NOT REQUIRE TAPING.

B0	Base for Acoustical Tile:  Where gypsum board is indicated as a base for adhesively-applied acoustical tile, install tape and 2-coat compound treatment, without sanding.

C0	Water-Resistant Gypsum Backing Board Base for Ceramic Tile:  Comply with recommendations of gypsum backing board manufacturer for treatment of joints behind ceramic tile.

D0	Regular Gypsum Board Base for Ceramic Tile: In areas to be tiled using organic adhesive, tape joints and apply 4 inch (100 mm) wide coat of joint compound.

E0	Partial Finishing: Omit third coat (if specified) and sanding on concealed drywall work which is indicated for drywall finishing or which requires finishing to achieve fire-resistance rating, sound rating or to act as air or smoke barrier.

1	Refer to sections on painting, coatings and wall-coverings in Division-9 for decorative finishes to be applied to drywall work.

3.7	PROTECTION OF WORK:

A0	Provide final protection and maintain conditions, in a manner suitable to Installer, which ensures gypsum board work being without damage or deterioration at time of substantial completion.

3.8	CLEANING AND DECONTAMINATION:

A0	At completion of all work clean and decontaminate the work area in accordance with Section 01712 - Cleaning and Decontamination Procedures

USE ABOVE IF SECTION 01527 "LOCAL AREA PROTECTION" IS USED. USE BELOW IF SECTION 01526 "TEMPORARY ENCLOSURES" IS USED.

B0	At completion of all work clean and decontaminate the Work Area in accordance with Section 01711 - Project Decontamination

END OF SECTION - 09251

This Page Intentionally Blank