SECTION 05582 - SHEET METAL ENCLOSURES - LEAD-BASED PAINT

PART

1 - GENERAL

1.1	RELATED DOCUMENTS

A.	Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2	SUMMARY

A.	This Section includes aluminum sheet metal enclosures of lead-based painted trim.

B.	Related Sections:  The following Sections contain requirements that relate to this Section:

1.	Section 01505 - Exterior Regulated Areas

2.	Section 01555 - Worker Protection

3.	Section 01556 - Respiratory protection

1.3	SUBMITTALS

A.	Product data for each type of product specified.

B.	Samples for initial selection purposes in form of manufacturer's color charts showing full range of colors, textures, and patterns available for each type of sheet metal fabrication indicated.

1.4	DELIVERY, STORAGE, AND HANDLING

A.	Deliver sheet metal materials and fabrications  with protective crating and covering.

B.	Store products on elevated platforms in a dry location.

1.5	PROJECT CONDITIONS

A.	Field Measurements:  Verify size, location, and placement of sheet metal fabrications with adjoining construction prior to fabrication.

PART 2 - PRODUCTS

2.1	SHEET METALS

A.	General:  Provide sheet metals selected for their surface flatness, smoothness and freedom from surface blemishes where exposed to view in the finished unit.  Do not use materials whose exposed surfaces exhibit pitting, seam marks, roller marks, variations in flatness exceeding those permitted by referenced standards for stretcher-leveled metal sheet, stains, discoloration or other imperfections.

B.	Aluminum Sheet:  Alloy and temper recommended by manufacturer for use intended and as suitable for application of finish indicated, but with not less than the strength and durability properties specified in ASTM B 209 for 5005-H15.

2.2	MISCELLANEOUS MATERIALS

A.	Fasteners:  Of same basic metal and alloy as fastened metal, unless otherwise indicated.  Do not use metals which are corrosive or incompatible with metals joined.

1.	Provide concealed fasteners for interconnection of sheet metal fabrications and for their attachment to other work except where exposed fasteners are unavoidable or are the standard fastening method.

2.3	CLOSURES AND TRIM

A.	Form closures and trim members from sheet metal of type and minimum nominal thickness as indicated below.  Incorporate components required for support and installation of closures and trim.  Fabricate closures and trim to tightly close with adjoining construction.

1.	Aluminum sheet, 0.0625 inch.

B.	Conceal fasteners where possible; otherwise locate where they will be as inconspicuous as possible.  Size fasteners to support closures and trim, with fasteners spaced to prevent buckling or waviness in finished surfaces.

C.	Support joints with concealed stiffeners as required to hold exposed faces of adjoining sheets in flush alignment.

D.	Miter or cope trim members at corners to form tight joint.

2.4	FINISHES

A.	Comply with NAAMM "Metal Finishes Manual" and  Aluminum Association for recommendations relative to application of finishes.

B.	Baked Enamel Finish:  AA-C12C42R1x (Chemical Finish: cleaned with inhibited chemicals; Chemical Finish: chemical conversion coating, acid chromate-fluoride-phosphate pretreatment; Organic Coating:  as specified below).  Apply baked enamel in compliance with paint manufacturer's specifications for cleaning, conversion coating, and painting.

1.	Organic Coating:  Thermosetting modified acrylic enamel primer/topcoat system standard with manufacturer, with minimum dry film thickness of 1.5 mils, medium gloss.

2.	Color:  As indicated by reference to manufacturer's standard color designations.

3.	Color:  Match Designer's samples.

4.	Color:  As selected by Designer from manufacturer's standard colors.

PART 3 - EXECUTION

3.1	GENERAL

A.	Before starting work of this section, complete the following:

1.	Section 01505 - Exterior Regulated Areas

2.	Section 01555 - Worker Protection

3.	Section 01556 - Respiratory protection

3.2	EXAMINATION

A.	Examine substrates for compliance with requirements for substrates, installation tolerances, and other conditions affecting performance of siding.  Do not proceed with installation until unsatisfactory conditions have been corrected.

3.3	PREPARATION

A.	Prior to installation of enclosure carefully remove flaking and loose areas of lead-based paint by wet scraping.  Allow paint with good adhesion to remain.

B.	Affix 3" x 5" (76 x 127 mm) warning labels every 4 feet (1.22 m) on surface reading "Lead-Based Paint" or using an indelible marker write "Lead-Based Paint" every 4 feet (1.22 m) prior to installing air infiltration barrier or siding .

C.	Clean substrates of projections and substances detrimental to application.

3.4	INSTALLATION

A.	Locate and place sheet metal fabrications plumb, level and in alignment with adjacent construction.

B.	Back caulk at perimeter of sheet metal enclosure seal seams to form a continuously sealed  enclosure.

C.	Form tight joints with exposed connections accurately fitted together.  Provide reveals and openings for sealants and joint fillers, as indicated.

D.	Provide sealants,  flashing, and install as the installation progresses to make installations weather-tight and sealed.

END OF SECTION 05582