SECTION 09952 - MECHANICAL REMOVAL OF  LEAD-BASED PAINT

PART 1 - GENERAL

1.1	RELATED DOCUMENTS:

A.	Drawings and general provisions of the Contract,

including General and Supplementary Conditions and other Division-1 Specification sections, apply to work of this section.

1.2	SUMMARY OF WORK:  Work of this section includes removal and

disposal of lead-based paint.

A.	The following substrates require Mechanical paint

removal:

1.    Steel lintels

2.    Metal door frames

3.    Steel columns

4.    Concrete walls

5.    Wrought iron rails.

1.3	GENERAL:  Prohibited lead hazard removal methods.

A.	Open flame burning;

B.	Chemical stripping with  methylene chloride based paint

strippers;

C.	Uncontained abrasive blasting;

D.	Uncontained power washing;

E.	Dry sanding or scraping;

F.	Power sanding without HEPA attachment;

G.	Sanding of wood after chemical stripping.

1.4	SUBMITTALS:  Before start of work: Submit the following to the

Designer for review.  Do not start work until these submittals are returned with Designer action stamp indicating that the submittal is returned for unrestricted use.

A.	Manufacturer's Product Data on removal equipment to be

used.

B.	Description of removal methods to be used for each

substrate condition including manufacturer's operating instructions and recommendations for equipment usage.

PART 2 - PRODUCTS

2.1.  TOOLS AND EQUIPMENT

A.	Portable power sanders with HEPA vacuum attachment.

B.	Needle gun with HEPA vacuum attachment

C.	Vacuum blasting equipment with HEPA vacuum attachment

D.	Flameless heat guns and heat grid with maximum

temperature setting of 700 degrees fahrenheit.

E.	Paint scrapers

F.	Wet/dry sand paper

PART 3 - EXECUTION

3.1	RELATED WORK SPECIFIED ELSEWHERE:

A.	Section 01504 - Temporary Facilities

B.	Section 01505 - Exterior Regulated Areas

C.	Section 01506 - Work Area Containment (Interior)

D.	Section 01555 - Worker Protection

E.	Section 01556 - Respiratory Protection

F.	Section 02067 - Disposal of Waste Materials - Lead-Based

Paint

3.2	MECHANICAL REMOVAL OF LEAD-BASED PAINT

A.	Portable Power Sanders:  Maintain HEPA vacuum attachment

in operation during sanding operations.  Sanding surface shall be held flat to surface.  Conduct sanding operations on flat surfaces only.  Do not allow sanding pad surface to extend beyond surface being sanded.

C.	Needle Gun: Maintain HEPA vacuum attachment in operation

during removal operation.  Select proper shroud to match the configuration of the surface being treated.

D.	Vacuum Blasting: conduct abrasive removal of exterior

surfaces only using machine blasting equipment mounted with a fully contained, coaxially mounted local exhaust hood with HEPA-Vacuuming capability and using either recyclable or dry ice (co2) abrasive media.

1.	Conduct blasting on flat surfaces or surfaces

compatible with available blast heads as provided by equipment manufacturer.

2.	Maintain blast head in contact with surface to

provide maximum containment of dust, debris, etc. created by blasting operation.

E.	Flameless Heat Gun/Heat Grid:  Provide proper respiratory

and worker protection prior to use.  Soften paint surface with heat gun/heat grid.  Use putty knife to scrape paint from surface.  Collect sludge and properly containerize

in accordance with Section 02067 - Disposal of Waste Materials - Lead-Based Paint .

F.	Paint Scrapers:  Use wet scraping methods only.  Lightly

mist surface to be scraped.  Properly containerize waste in accordance with Section 02067 - Disposal of Waste

Materials - Lead-Based Paint.

G.	Wet/Dry Sand Paper:  Use wet sanding methods only.  Do

not allow removed paint to accumulate.  Properly containerize waste in accordance with Section 02067 Disposal of Waste Materials - Lead-Based Paint.

END OF SECTION  09952