SECTION 02065 - REMOVAL OF LEAD-BASED PAINTED SUBSTRATES

PART 1 - GENERAL

1.1	RELATED DOCUMENTS:

A.	Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division-1 Specification sections, apply to work of this section.

1.2	Summary of Work:  Work of this section includes the removal and off site disposal of the following lead-based painted substrates.

A.	 Plaster and lath walls and ceilings

B.	 Door jambs at boiler rooms.

C.	 Wood baseboards and chair rails.

D.	Door jambs on the rear entrance of each apartment.

E.	Exterior thresholds.

F.	Entrance doors.

G.	 Porch ceilings.

H.	Wrought iron railings.

1.3.	RELATED WORK SPECIFIED ELSEWHERE:  Removal of lead-based painted windows, related trim, cabinets and other millwork items are specified in section 06402-Carpentry and Trim Work.

PART 2 - PRODUCTS

2.1	DISPOSAL BAGS/PLASTIC SHEETING:  Provide 6 mil polyethylene disposal bags or wrap substrates to be disposed of in 6 mil polyethylene, sealed with duct tape.

2.3	Wet Detergent Wash:  Provide detergent with a high phosphate content (at least 5%) trisodium phosphate (TSP).  Follow dilution ratio recommended by the manufacturer's instructions.

Wet Detergent Wash:  Provide detergent or cleaning agent formulated to be effective in removing lead dust.  Follow dilution ratio recommended by the manufacturer's instructions.

PART 3 - EXECUTION

3.1	BEFORE STARTING WORK OF THIS SECTION, COMPLETE THE FOLLOWING:

A.	Section 01504 - Temporary Facilities - Lead-Based Paint

B.	Section 01505 - Exterior Regulated Areas - Lead Based Paint

C.	Section 01506 - Work Area Containment - Lead Based Paint

D.	Section 01555 - Worker Protection - Lead Based Paint

E.	Section 01556 - Respiratory Protection - Lead-Based Paint

3.2	GENERAL

A.	Score paint at edges, corners etc. to reduce chipping of paint.  Carefully remove by wet scraping loose and flaking paint prior to removal of substrate in accordance with the following procedure:

1.	Fine mist surface with wet wash detergent or water using plant mister or garden sprayer.

2.	Carefully scrape loose and flaking material.

3.	Clean up paint chips and flakes by wet sweeping or pick up with wet towels.

B.	Care shall be taken to avoid damage to adjacent areas during the removal of substrates.

C.	Carefully remove the lead based painted substrates to minimize the disturbance of lead based paint and the generation of lead dust.

D.	HEPA vacuum and/or wet wipe to remove all paint chips, debris and dust generated during the work.  Do not allow dust or debris to accumulate.

E.	Substrates that are removed shall be wrapped , labeled and disposal or disposed of in accordance with section 02067 - Disposal of Waste Materials - Lead-Based-Paint.

F.	Complete interior abatement prior to removal of exterior doors to allow unrestricted access to the apartment unit for inspections, etc.

3.3	DAMAGES:	Protect areas adjacent to substrates that are removed for replacement from damage caused by this work.  Damages to non-protected areas or from lack of care shall be repaired or replaced at the Contractor's expense.

3.4	SECURITY:	Install temporary 3/4" plywood and stud framing in openings where entrance doors or windows are removed.  Provide temporary lockable doors where egress is required.

END OF SECTION  02065